RUBBER PROCESSING

The production of rubber goods involves two basic operations – compounding and curing. Rubber polymers behave as viscoelastic fluids when sheared at elevated temperatures. This enables the incorporation of the various fillers and chemical additives in the process of compounding.

Mastication

The first step in rubber compounding is mastication or polymer “breakdown”. This is essentially development of the polymer's viscoelasticity to make it receptive to the additives. Most synthetic elastomers are produced with the uniformity in chemistry, viscosity and stability that minimizes or precludes the need for mastication. This step is, nevertheless, usually necessary for compounds containing a blend of polymers to provide a uniform mixture prior to further compounding. Natural rubber is characteristically widely variable in viscosity from lot to lot, so that several lots are usually blended and masticated to control viscosity and physical properties of the compound. The breakdown of natural rubber promotes viscoelasticity by extending or disentangling the polymer chains or by severing the chains. Breakdown cycles for both natural and synthetic rubber are often facilitated by the inclusion of plasticizers.

Polymer breakdown and subsequent compounding was historically accomplished on open roll mills, although today these operations are almost always performed in an internal mixer. The open mill consists of two metal rolls which are jacketed for temperature control. These rolls turn toward each other at fixed separations and often at different speeds. This provides high shear mixing forces. Banbury® Mixers are the most commonly used internal mixers today. They consist of two rotor blades turning toward each

other in an enclosed metal cavity. The cavity is fed from a loading chute through which the rubber and in later steps the fillers and compounding chemicals are added. Mixing shear, and consequent mixing time, is determined by rotor shape, size, and speed. A large Banbury can produce 500 kg of finished compound in a matter of minutes.

Masterbatching

As a compounding process, masterbatching means incorporation of the other compounding ingredients into the rubber, except for the curing system. By omitting the cure system, the masterbatch may be intensively mixed without fear that the high temperatures generated will cause premature vulcanization. The objectives of masterbatching are homogeneous blending of polymer and chemical additives, the best possible deagglomeration and dispersion of fillers, and the development of the proper final viscosity. This viscosity, in turn, is a function of the homogeneity achieved in the mixing of the polymer and additives. Because considerable heat is generated during milling, the masterbatch operation must often be terminated before its objectives are attained. This is to avoid heat degradation. In such cases, the compound is remilled before addition of the curing system. Masterbatches are typically prepared in a Banbury mixer, after which they are ejected and cooled.

Separate from the compounding process, masterbatches are often prepared of individual additives that are difficult to disperse during compounding, zinc oxide for example. A concentrated dispersion of the additives in polymer is preformed. This can then be added to the rubber compound for faster incorporation since the additive is predispersed.

Remilling

If the masterbatch shows inadequate dispersion or is too high in viscosity for finish mixing, it is remilled to prepare it for the next step. Remilling is most commonly required with high carbon black, low oil natural rubber tire compounds.

Finish Mixing

The finish mixing step completes the rubber compound by the incorporation of the curing system. This is usually done in an internal mixer where mixing rate and time are balanced to ensure homogeneity without generating temperatures which will cause premature curing.

Extruding

Screw-type extruders are used both in the compounding operations and to form articles for vulcanization. In masterbatching, remilling, and finish mixing, the hot batch of rubber generally goes directly to an extruder. The extruder screw will force the rubber through a die to form pellets, or through a pair of rolls to form a slab or sheet. In either case, the extrusion operation allows the compound to cool down while it is turned into a more easily handled form.

Heated mixing extruders can be fitted to batch mixers to improve compound uniformity and reduce viscosity, and they can warm up material for calender feed. This type of extruder can also be used to take cold finished compound in strip, pellet, or slab form, heat it, blend it, and extrude it in the desired shape. This can be a finished shape, such as a rubber hose, which can be continuously vulcanized right after the extruder. Where the shape must be very precise, the compound may be first warmed on a mill or warm-up extruder and then fed to a shaping extruder.

Calendering

Rubber calenders consist of at least three rolls which can be adjusted for gap, speed and temperature. They are used to form sheeting to required lengths and thickness for subsequent building operations. They are also used for frictioning or skim coating fabrics. Cord and wire are coated in this way for making plies used in the construction of tires and conveyor belts.

Vulcanization

After the rubber compound has been processed and formed, it is vulcanized. This process involves three stages: induction, curing, and reversion or overcure. The induction period is the time at vulcanization temperature during which no measurable crosslinking occurs. It determines the safety margin of the compound against “scorch” during the processing steps preceding crosslinking. Scorch is premature vulcanization that can occur due to the effects of heat and time. Because these effects are cumulative, the time until scorch will slowly decrease with each processing step. Scorching results in a tough and unworkable batch, which must be scrapped. The time to scorch is dictated by the processing and the additives used, so that a well designed compound will have a scorch time slightly longer than the equivalent of its maximum anticipated cumulative heat history.

The amount of time the compound must be cured, the cure time, is determined in part by the “rate of cure”. This is the rate at which crosslinking and the consequent development of stiffness (modulus) occurs. Cure time is also a function of the desired “state of cure”. As vulcanization (crosslinking) proceeds, the various properties developed by vulcanization are not optimized simultaneously. At any given time during vulcanization, the state of cure is a measure of the development of these properties. Cure time is the time required for the compound to reach a state of cure where the desired balance of properties has been attained.

When a compound is cured beyond the point where its balance of properties has been optimized it becomes overcured. For most elastomers, overcure means the compound becomes harder, weaker and less elastic. With other elastomers, particularly most natural rubber compounds, overcure results in reversion. The compound softens, becoming less elastic and more plastic.

Preparation – Rubber stocks about to be assembled for vulcanization may be in a number of forms, such as calendered strips or sheets, plied up slabs, extruded tubes or partially combined with fabrics. Tires, tubes, hose, belts, footwear, rolls and many other articles are built to proximate finished form before vulcanization. The various stocks that are combined to form such articles must be dimensionally stable, and possess the required building tack, all of which depend upon proper compounding and processing.

Vulcanization or curing may be accomplished by a number of methods, depending on the compound in process, and the size, shape and overall structure of the finished article.

Press Curing – Press curing includes the molding of articles by compression, transfer, or injection methods. Blocked-in articles which are cured directly between press platens also come under this classification, as well as unblocked slabs. The heat source is generally saturated steam. Electrically heated platens are also used in some installations. Radio frequency waves have been suggested as a means of curing or for preheating blanks to reduce the press cure time.

Compounds for press curing must be carefully designed to flow properly without scorching before the desired shape is reached, and to cure rapidly so that a maximum turnover is obtained. They must be easily removed from the molds after cure and exhibit attractive surfaces in the finished form. The flow characteristics depend on the plasticity of the uncured stock as well as selection of the proper acceleration to permit complete filing of the cavity before the cure begins.

Flat Belting and Slab Cures – In articles of this type, the press platens and side strips control the dimensions of the finished article. Belting structures of both transmission and conveyor types are built to their approximate finished shapes before curing. The fabrics they contain have been dried and stretched before frictioning and skim coating, and an additional stretch is applied to each section in the press prior to and during cure.

Slabs for soling, tile, or matting must possess suitable flow characteristics and they must be properly accelerated to permit “cycling” in multistage presses without developing porosity as the pressure is released and reapplied during cure. Slabs for such articles are built to their approximate finished thickness on the calender or sheeting mill.

Open Steam Curing – Open steam curing is used in the production of hose, wire and cable, and other extruded articles. With this method, the article may be in direct contact with the steam, wrapped with fabric tape. Equipment may consist of a jacketed autoclave or a closed chamber in which the articles are placed and steam is introduced.

Another method of open steam curing is used in the production of insulated wire and cable. This method, known as the CV (continuous vulcanization) process, utilizes jacketed tubes which may be 60 meters (200 feet) in length and operate under internal steam pressure upward of 1.4 MPa (200 psi) as compared to the 200 to 550 kPa (30 to 80 psi) range of the conventional steam vulcanizer.

In operating a closed-chamber steam vulcanizer, the curing cycle consists of a rise to a predetermined pressure, a holding period at the required curing pressure, and a blow down to atmospheric pressure. In the CV process, extruded wire or cable covering goes directly from a tuber into steam at curing pressure and, with the latest equipment design, passes through a water or condensation seal prior to emerging from the tube at atmospheric pressure.