3.7 SEMICONDUCTING CERAMICS

Semiconductors have a small Eg as shown in Figure 3.2. In semiconductors σ is proportional to n and μ (for both electrons and holes). In general, there are three ways free electrons and holes may be generated in ceramics:

- Excitation across the band gap (intrinsic semiconductors)

- Introduction of impurities/dopants (extrinsic semiconductors)

- Departures from stoichiometry (nonstoichiometric semiconductors)

Most oxide semiconductors are either doped to create extrinsic defects or are annealed under conditions in which they become nonstoichiometric.

Intrinsic Semiconductors

For every electron that is excited into the conduction band, a hole is produced in the valence band. The number of electrons in the conduction band is

(3.16)

Similarly, the number of holes in the valence band is

(3.17)

The densities of states are given by

(3.18)

(3.19)

Where m*e and m*h are the effective masses of the electrons and holes, respectively. For many ceramics m*e and m*h are not known and we make the (often incorrect) assumption that me =m*e =m*h, where me is the rest mass of the electron. If we use the subscript i to denote intrinsic carrier concentrations, we can write

(3.20)

(3.21)

Therefore

(3.22)

If Nc = Nv then

(3.23)

The intrinsic conductivity is given by

(3.24)

Equation 3.24 is similar to Eq. 3.2, but we are now considering μe and μh.

The intrinsic conductivity of many pure oxide semiconductors is generally very low because of their large Eg compared to Si and GaAs. To illustrate this point we will compare the room temperature conductivities of Cu2O, a semiconducting oxide Eg=2.1 eV, and GaAs, III–V semiconductor Eg =1.4 eV.

The applications of intrinsic semiconductors: X-ray detectors on transmission electron microscopes (TEMs) and scanning electron microscopes (SEMs) for chemical analysis.

Extrinsic and Nonstoichiometric Semiconductors

An extrinsic semiconductor contains impurities that are present either accidentally or, as is most often the case that have been intentionally added. The effect of these impurities on the energy band diagram is that they introduce additional energy levels into the band gap as illustrated in Figure3.9. These new energy levels are often close to the band edges. If the impurity level is just above the valence band the impurity is an “acceptor” because it can accept electrons leaving holes in the valence band. If the impurity can supply electrons into the conduction band it is a “donor” and the level is located just below the bottom of the conduction band. If the impurity acts as an electron donor the semiconductor is known as an n-type semiconductor because the electrons (or negatively charged species) are the majority charge carriers. If the impurity acts as an electron acceptor then the semiconductor is known as a p-type semiconductor because holes (or positively charged species) act as the majority charge carriers.

At low temperatures the number of charge carriers is determined by the donor and acceptor ionization energies. At sufficiently high temperatures full ionization of the impurities is achieved and the carrier densities become independent of temperature. This region is called the “exhaustion” or “saturation” region. At even higher temperatures the thermal energy is enough to excite electrons across the energy band gap and the material behaves like an intrinsic semiconductor. These three regions are shown in Figure 3.10.

Nonstoichiometric semiconductors are very similar to extrinsic semiconductors, and can really be considered together. The main difference is that the electronic defects rather than being due to impurity atoms are the result of changes in the stoichiometry of the crystal. We still use the designations n- and p-type to describe the majority charge carrier and the defect adds levels into the band gap that lead to increased levels of conductivity, particularly at room temperature and below.

FIGURE 3.9 Effect of doping on band structure.

FIGURE 3.10 Temperature dependence of σ for an extrinsic semiconductor. The dashed lines show the individual contributions of n and to .