3.1 CERAMICS AS ELECTRICAL CONDUCTORS

The insulating properties of ceramics have often been one of their most important properties, many ceramics are actually very good electrical conductors and some are even superconductors. Ceramics show the broadest range of electrical properties of any of the classes of material. Table 3.1 lists the important parameters that are used in discussions of electrical conductivity.

The conduction mechanisms in ceramics can be quite complex and may involve the movement of electrons, holes, and ions; in some cases they may be “mixed,” with more than one type of charge carrier responsible for current flow.

In comparing values of σ and ρ it is useful to remember the simple relationship between them:

(3.1)

TABLE 3.1 Terms and Units Used

3.2 CONDUCTION MECHANISMS IN CERAMICS

Electrical conductivity is given by

(3.2)

The importance of Eq. 3.2 is that it applies to all materials and it shows that the two factors affecting σ are

- Number of charge carriers, n

- Their mobility, μ

When we consider the effect of variables such as composition, structure, and temperature on σ we are concerned with their effect on n and μ. If more than one type of charge carrier is contributing to σ then we can define a partial conductivity for each. For example, if σ were due to the movement of electrons and cations with a charge Z, then for electrons

(3.3)

and for cations

(3.4)

The total is

(3.5)

If a ceramic is an electron conductor, i.e., te =1, then to determine n we need to know Eg. We usually consider the three situations shown in Figure 3.2, where the band gap is either zero, narrow, or wide.

FIGURE 3.2 Schematic of electron energy bands in solids. The valence band (VB) and conduction band (CB) are indicated.

When Eg is zero, as in the case of most metals, there are free electrons present at any temperature above 0 K. The total number of free electrons is equal to the number of valence electrons per atom multiplied by the number of atoms in the metal. Eg in a metal is not zero, but it is very small. For example, if we have a metal crystal consisting of 1023 atoms and the width of the energy band is 1 eV then the separation between the energy levels would be only 10−23 eV (1.6 *10−42 J). This would be the minimum amount of energy required to excite an electron into a vacant level.

A narrow band gap is usually defined as being in the range of 0.02 to about 2.5 eV. When Eg is toward the lowest end of this range there is a significant fraction of electrons in the conduction band. Materials with a narrow band gap are usually referred to as semiconductors.

- Silicon: Eg =1.12 eV

- Gallium arsenide: Eg =1.42 eV (Both Si and GaAs are ceramics).

Materials with a wide band gap (>2.5 eV) are considered to be electrical insulators because the probability of an electron being in the conduction band at room temperature is extremely small. However, the probability is not zero and so we should think of these materials as wideband- gap semiconductors. SiC (Eg =2.6–3.0) is an example of a wide-band-gap semiconductor.

●TRANSFERENCE NUMBER

The transference or transport number is the fraction of σtot contributed by each charge carrier.

For electrons: te = σe/σtot

For cations: t+=σ+ /σtot

3.3 ELECTRON MOBILITY

As electrons move through a solid under the influence of ξ they experience a number of collisions (in a process called scattering) that decreases μ. There are three scattering mechanisms:

- Phonon. This is the major factor affecting μ (of both electrons and holes). A phonon is the quantum unit of lattice vibrational energy. The higher the temperature the greater the vibrational amplitude of the atoms in the lattice and the greater the number of phonons. As a result, scattering increases and μ decreases with increasing temperature.                                                                              (3.10)

- Electron–electron. At room temperature, the mean distance between electron–electron collisions is about 10 times that of electron–phonon collisions so electron– phonon scattering is dominant.

- Polaron. This mechanism occurs only in ionic crystals and involves the interaction between the electron and the ions in the crystal. The electron can cause local distortion of the lattice known as a polaron as illustrated in Figure 3.3. When the interaction is sufficiently strong (small polaron), the electron may be trapped at a particular lattice site, reducing μ and decreasing σ.

FIGURE 3.3 Illustration of (a) a large polaron of radius R, formed in a metal oxide MO and (b) a small polaron, showing the distortion of the lattice around an electron trapped at a metal

3.4 EFFECT OF TEMPERATURE

For a material where Eg = 0, i.e., one in which n does not vary significantly with T, σ decreases with increasing temperature because of the decrease in μ:

(3.11)

For materials where Eg = 0 (i.e., materials that we would classify as semiconductors or insulators), σ rises with T because of the temperature dependence of n:

(3.12)

Figure 3.4 shows the typical T dependence of σ for the three broad classes of electrical behavior. Because it is possible to make practical use of the variation in σ or ρ with T it is often beneficial to classify materials based on this variation. The temperature dependence of resistivity may be expressed by an empirical equation

(3.13)

Where ρ1 is the resistivity at T1 and ρ2 is the resistivity at T2. The parameter αR is known as the temperature coefficient of resistivity or TCR. For materials where Eg =0 the TCR is typically positive. These materials are called positive temperature coefficient (PTC) materials. Most materials that show semiconducting or insulating properties are negative temperature coefficient (NTC) materials. Some ceramics, for example BaTiO3, that do have energy band gaps are actually PTC materials. This type of behavior has nothing to do with conduction across the band gap but is actually a grain boundary (GB) effect.

FIGURE 3.4 Conductivity variations with temperature for the different classes of electrical conductor. The shading indicates the range of values at room temperature.