3.12 CERAMIC INSULATORS

More typically we think of ceramics as being good electrical insulators and there are many ceramics that have ρ>1014Ω·cm. Examples of common ceramic insulators include

- Aluminum oxide (Al2O3)

- Mullite (3Al2O3 · 2SiO2)

- Forsterite (2MgO · SiO2)

- Beryllium oxide (BeO)

- Aluminum nitride (AlN)

In an electrical insulator, there is a wide energy gap between the bottom of the conduction band and the top of the valence band. Figure 3.16 shows the energy band diagram for MgO. The valence band is formed by the 2p energy levels of oxygen (O2-ions) and the conduction band is formed from the empty 3s orbitals of the Mg2+ ions. The energy band gap is ~8 eV and the concentration of thermally excited electrons in the conduction band of MgO is low right up to its melting point, 2800°C. MgO is therefore an excellent high temperature insulator. Very wide energy band gaps (>6eV) are associated with compounds that have high fractions of ionic character in their bonding. Ions have a stable noble gas electron configuration. To excite an electron from the valence band to the conduction band involves making the electron configuration of the ions different from those of the noble gases. This process is energetically unfavorable. In general, compounds with wide band gaps have

- Predominantly ionic bonding

- Consist of atoms (ions) of low Z

No entirely satisfactory relationship has been established between the ionic character of the bond and the atom size on Eg. In a homologous series of oxides, such as the oxides of the alkaline-earth metals, Eg increases with increasing ionic potential, Φ, of the cation as shown in Figure 3.17.

FIGURE 3.17 Effect of bond ionicity on Eg for metal oxides MO (Φ=Z/r)

FIGURE 3.16 Energy band diagram for MgO

In a series of isoelectronic compounds (i.e., compounds with an identical total number of electrons) Eg increases with the increasing ionic character of the interatomic bond as shown in Figure 3.18. Understanding this relationship is quite straightforward. As the fraction of covalent character in a bond increases the electrons in that bond are more equally shared and hence electron transfer becomes easier. The presence of point defects in the lattice can be viewed as being donor or acceptor species in the same way that we considered defects in semiconductor crystals. Figure 3.19 shows another version of an energy band diagram for MgO, this time with the estimated defect energy levels included. If the crystal contains oxygen vacancies (i.e., it has been reduced) these can become ionized:

(3.37)

The energy for ionization is 0.5 eV and can be represented as a level just below the bottom of the conduction band—the oxygen vacancy is behaving as a donor. The oxygen vacancy can become doubly ionized:

(3.38)

The energy for this second ionization process is ~2 eV and can be represented as another donor level. In a similar way we can represent acceptor sites within the band diagram for MgO as being due to the oxidation of MgO, i.e., the introduction of magnesium vacancies and corresponding holes. The following reactions show the origin of the acceptor levels:

(3.39)

and

(3.40)

The energies for these two processes are 0.5 eV and ~1.5 eV, respectively. Even though these ionization energies are relatively small compared to the band gap, the concentration of these defects is extremely low. Even at temperatures >2000°C the number of cation and anion vacancies in MgO is only about one per billion lattice sites. The addition of substitutional and interstitial point defects can also introduce additional energy levels.

FIGURE 3.18 Correlation of Eg and electronegativity difference (∆EN).

FIGURE 3.19 Defect levels in MgO

Stoichiometric oxides such as MgO are very difficult to reduce and it is strongly to the right throughout all accessible ranges of temperature and oxygen activity. Even highly doped compositions are not electrically conductive at room temperature.

The defects with a positive effective charge are donors; these have given up an electron to become ionized positively relative to the perfect lattice site. Correspondingly, defects with a negative effect charge are acceptors, having accepted electrons relative to the perfect lattice. Dislocations are defects that also create additional energy levels within the band gap. They act as acceptors as shown in Figure 3.20. Note that the dislocation-acceptor levels are usually in the upper half of the band gap.

Dislocations are particularly deleterious to the behavior of semiconductors. One of the main factors that limited the increase in the size of silicon wafers has been the need to grow dislocation-free single crystals.  The dislocation creates dangling bonds, which act as electron traps to satisfy the requirement of each silicon atom to achieve a noble gas electron configuration.

Ceramics with high ρ are important for a number of applications, many of which utilize more than just the high ρ. Other properties such as high strength, stability at elevated temperature, high thermal conductivity, and hermeticity (impervious to the environment) are also important.

FIGURE 3.20 Effect of dislocations on the energy band diagram of a semiconductor.