3.6 CERAMICS WITH METAL-LIKE CONDUCTIVITY

The general electrical characteristics of metals are

- σ ≥ 104 S/m

- te =1

- n =1022–1023cm−3

- dσ/dT is small and negative.

Remember that Ω−1 (ohm−1) is S (siemens). Some ceramics, for example TiO and VO, show metallic like electronic conductivity where the conduction is due to the movement of free electrons. To explain this behavior we will consider the example of TiO. TiO has a structure based on rock salt with vacancies in both the metal and oxygen sublattices. One-sixth of the titanium and one-sixth of the oxygen are missing .The 2p orbitals from the oxygen atoms form a filled valence band. The bands formed by the 4s and 4p orbitals on the Ti are at a much higher energy. The metal d orbitals form a band below that of the metal s and p orbitals as illustrated in Figure 3.5.

FIGURE 3.5 Energy bands of a transition metal oxide: (a) d band empty; (b) metallic oxide with d band partially filled.

The divalent titanium ion, Ti2+, in TiO has two 3d electrons and so the metal d band shown in Figure 3.5 is partially filled. It is this partially filled band, which you will notice resembles the energy level diagram for a metal shown in Figure 3.2, which leads to metallic conductivity in TiO. Looking at Figure 3.5 it is easy to see why titanium dioxide, TiO2, is an insulator. In the formation of the Ti4+ion, both the two 4s electrons and the two 3d electrons are given up to form oxygen ions. So the 3d band (the conduction band in the solid) is empty at T =0 K. The band gap, Eg, in TiO2 is 3eV. This is a relatively small Eg for an insulator and indicates some covalent character in the Ti–O bond.

So why aren’t MnO, CoO, and NiO, which are also monoxides of the first row transition metals and have the rock salt structure, metallic-like conductors?

To answer this question we need to consider the interaction between the d orbitals and the formation of the d band in metal oxides. In the rock salt, structure the dxy, dyz, and dxz orbitals on adjacent metal atoms overlap. The extent of the overlap is less than it would be in the pure metal because in the oxides the metal atoms are not nearest neighbors. Consequently, the d bands are narrower than they would be for the metal. As we go across the first row transition elements (from Ti to Ni), there is an increase in nuclear charge and a corresponding contraction in the size of the d orbitals.

As the d orbitals become smaller the extent of overlap decreases and the 3d band becomes narrower, eventually forming a localized state as illustrated in Figure 3.6.

Some oxides of the second and third row transition elements also exhibit metallic-like properties, for example, ReO2 and ReO3. In these compounds, the metal electron energy levels of interest are the 5d, rather than the 3d as in the case of the first row transition metals. For some of the oxides we have already mentioned, e.g., ReO3, TiO, CrO2, and ReO2, dσ/dT is small and negative, just like it is for most metals.

There are many applications for ceramics that have metal like conductivity, like Resistors, Electrodes.

●ELECTRON CONFIGURATIONS

Ti     1s22s22p63s23p63d24s2

Ti2+  1s22s22p63s23p63d2

Ti4+  1s22s22p63s23p6

FIGURE 3.6 Electronic energy levels of some 3d monoxides, deduced from spectroscopic measurements. The energy zero has been taken as the top of the oxygen 2p valence band.