3.10 ION CONDUCTION

Ion movement can make a major contribution to σ, particularly if the material has a large Eg. Conductivity resulting from ion migration is important in several ceramics. It is also the major conduction mechanism in ionic salts such as the halides. When we describe the mobility of ions we often use the absolute mobility, B:

(3.32)

Where v is the drift velocity and F is the applied force (which in this case is the electrical potential, i.e., F =Zqξ, where Z is the charge on the ion.)

B is related to μ:                                                                         (3.33)

Substituting Eq. 3.33 into Eq. 3.2 gives

(3.34)

The absolute mobility, and hence σ is directly related to the diffusion coefficient, D, through the Nernst–Einstein equation:

(3.35)

The diffusion coefficient is given by an Arrhenius equation, which means that there is an activation energy that must be overcome for the ions to move through the material as illustrated in Figure 3.15. We can then give σ in terms of D:

(3.36)

The following factors contribute to ionic mobility:

- Size. It is easier to move a small ion than a large one.

- Charge. A highly charged ion will polarize, and be polarized by ions of opposite charge as it moves past them. This will increase EA.

- Lattice geometry. Some structures contain channels that facilitate the ion movement. A large number of vacant sites can help.

FIGURE 3.15 Potential energy barriers to ion movement. (a) In the absence of an applied field and (b) with an applied field. EA is the activation energy and a jump distance between ion sites.

3.11 FAST ION CONDUCTORS

Materials that show exceptionally high ionic conductivity are referred to as “fast ion” conductors or “superionic” conductors. The conductivities are comparable to those of electrolyte solutions, but are still low compared with metal-like electron conductivity. There are two important types of fast ion conductor:

1. The β-aluminas: nonstoichiometric aluminates, for example

- Na2O · 11Al2O3 (β-alumina)

- Na2O · 8Al2O3 (β′-alumina)

- Na2O · 5Al2O3 (β′′-alumina)

They all have a layer structure that is composed of spinel blocks of close packed O2− ions with Al+3 in tetrahedral and octahedral interstices. Planes containing Na and O2− ions separate the spinel blocks. It is within these planes that the mobility of the Na+ ions is high. The conductivity is highly anisotropic; it is high within the Na+-containing planes and negligible in the perpendicular direction.

2. Cubic stabilized zirconia stabilized usually with either CaO or Y2O3.

These materials have oxygen ion transport numbers very close to 1.0. To understand how they are able to conduct large oxygen ions it is necessary to consider their defect structure. The correct composition of an oxide with the fluorite structure oxide would be MO2. The addition of CaO to ZrO2, for example, drops the metal-to-oxygen ratio below 2.0, and the formula of the oxide becomes CaxZr1−xO2−x. As, the Ca2+ ions substitute for Zr4+ ions and we have compensating oxygen vacancies. For each substitution Ca2+, we must create one anion vacancy. The result of this enormous defect population is to greatly increase the diffusion coefficient for oxygen to the extent that this material becomes a very fast oxygen-ion conductor. Stable ceramics that have completely ionic conductivity can be used as solid-state electrolytes. Two examples are the Na–S battery and the solid oxide fuel cell.