- Electrical Properties of Materials

- Why Study the Electrical Properties of Materials?

Consideration of the electrical properties of materials is often important when materials selection and processing decisions are being made during the design of a component or structure. The electrical behaviors of the various materials are diverse. Some need to be highly electrically conductive (e.g., connecting wires), whereas electrical insulativity is required of others (e.g., the protective package encapsulation).

- Electrical Conduction

OHM’S LAW

One of the most important electrical characteristics of a solid material is the ease with which it transmits an electric current. Ohm’s law relates the current I—or time rate of charge passage—to the applied voltage V as follows:

where R is the resistance of the material through which the current is passing. The units for V, I, and R are, respectively, volts (J/C), amperes (C/s), and ohms V/A.

The value of R is influenced by specimen configuration, and for many materials is independent of current. The resistivity is independent of specimen geometry but related to R through the expression:

- Figure 1. Schematic representation of the apparatus used to measure electrical resistivity.

where l is the distance between the two points at which the voltage is measured, and A is the cross-sectional area perpendicular to the direction of the current. The units for are ohm-meters ( -m). From the expression for Ohm’s law and Equation:

- Electrical conductivity

Sometimes, electrical conductivity is used to specify the electrical character of a material. It is simply the reciprocal of the resistivity, or

and is indicative of the ease with which a material is capable of conducting an electric current. The units for are reciprocal ohm-meters [( -m) or ohm/m]. The following discussions on electrical properties use both resistivity and conductivity, Ohm’s law may be expressed as

in which J is the current density, the current per unit of specimen area IA, and is the electric field intensity, or the voltage difference between two points divided by the distance separating them; that is

- Electronic and Ionic Conduction

An electric current results from the motion of electrically charged particles in response to forces that act on them from an externally applied electric field. Positively charged particles are accelerated in the field direction, negatively charged particles in the direction opposite. Within most solid materials a current arises from the flow of electrons, which is termed electronic conduction. In addition, for ionic materials a net motion of charged ions is possible that produces a current; such is termed ionic conduction.

Energy band structure in solids

In all conductors, semiconductors, and many insulating materials, only electronic conduction exists, and the magnitude of the electrical conductivity is strongly dependent on the number of electrons available to participate in the conduction process. However, not all electrons in every atom will accelerate in the presence of an electric field. The number of electrons available for electrical conduction in a particular material is related to the arrangement of electron states or levels with respect to energy, and then the manner in which these states are occupied by electrons.

Electronic and Ionic Conduction

For most materials, an electric current results from the motion of free  electrons, electrons which are accelerated in response to an applied electric field. The number of these free electrons depends on the electron energy band structure of the material. An electron band is just a series of electron states that are closely spaced with respect to energy, and one such band may exist for each electron sub shell found in the isolated atom. By “electron energy band structure” is meant the manner in which the outermost bands are arranged relative to one another and then filled with electrons

A distinctive band structure type exists for metals, for semiconductors, and for insulators.

An electron becomes free by being excited from a filled state in one band

to an available empty state above the Fermi energy(the energy of the highest filled state is called Fermi energy). Relatively small energies are required for electron excitations in metals, giving rise to large numbers of free electrons. Larger energies are required for electron excitations in semiconductors and insulators, which accounts for their lower free electron concentrations and smaller conductivity values, primarly four types of bandstructure exist in solids.

- Electron Mobility

Free electrons being acted on by an electric field are scattered by imperfections in the crystal lattice. The magnitude of electron mobility is indicative of the frequencyof these scattering events. In many materials, the electrical conductivity is proportional to the product of the electron concentration and the mobility.

Electrical Resistivity of Metals

For metallic materials, electrical resistivity increases with temperature, impurity content, and plastic deformation. The contribution of each to the total resistivity is additive.

.

QUESTIONS AND PROBLEMS

a) Compute the electrical conductivity of - 1

specimen 57 mm long in

which a current of 0.25 A passes in an axial

direction. A voltage of 24 V is measured

across two probes that are separated by

mm..45

(b) Compute the resistance over the entire

57mm  of the specimen

----------------------------------------------------------------

An aluminum wire 10 m long must experience 2-

a voltage drop of less than 1.0 V when

a current of 5 A passes through it. Using the

data in Table 18.1, compute the minimum

diameter of the wire

-------------------------------------------------------------------

A plain carbon steel wire 3 mm in diameter 3-

is to offer a resistance of no more than 20

Using the data in Table 18.1, compute the

maximum wire length

-----------------------------------------------------------------------

Demonstrate that the two Ohm’s law expressions 4-

Equations 18.1 and 18.5, are equivalent

(a) Using the data in Table 18.1, compute

the resistance of an aluminum wire 5 mm

in diameter and 5 m  long.

b) What would be the current flow if the

potential drop across the ends of the wire

is 0.04 V? (c) What is the current density

d) What is the magnitude of the electric

field across the ends of the wire

?

- Electronic and Ionic Conduction

What is the distinction between electronic 5-

and ionic conduction?

Energy Band Structures in Solids

How does the electron structure of an isolated 6-

atom differ from that of a solid material?

Conduction in Terms of Band and

Atomic Bonding Models

In terms of electron energy band structure 7-

discuss reasons for the difference in electrical

conductivity between metals, semiconductors

and insulators.

Electrical conductivity and resistivity are:

--material parameters.

--geometry independent.

•  Electrical resistance is:

--a geometry and material dependent parameter.

•  Conductors, semiconductors, and insulators...

--different in whether there are accessible energy

states for conductance electrons.

•  For metals, conductivity is increased by

--reducing deformation

--reducing imperfections

--decreasing temperature.

•  For pure semiconductors, conductivity is increased by

--increasing temperature

--doping (e.g., adding B to Si (p-type) or P to Si (n-type).