###### Effect of Thickness and annealing Temperature on (C-V) Characterization of  CdS/Si Heterojunction Preparing by DC Planar Magnetron Sputtering Technique and study of D.C. Electrical Conductivity.

Nahida B. Hasan	               Ahmed S. Hussian

Department of Physics, College of Science, University of Babylon

Kadhim A. Aadim

Department of Physics, College of Science, University of Baghdad

Abstract

The thin films of CdS deposited on silicon wafers substrate by ) dc planar magnetron sputtering techniques) . and they are study photovoltaic characteristics of (n-CdS/p-Si) Heterojunction, then we found type of heterojunction is abrupt type , also we calculated built-in potential (Vbi) at (400 kHz) and for thickness (100,200 and 300) nm for different  temperatures (303,373 and 473) K and study the variation junction capacitance with bias voltage, variation voltage with reciprocal of square capacitance , and the width of depletion layer can be calculated and study of the variation of electrical conductivity as a function of temperature for different thicknesses , it is clear from this study that the conductivity for all deposited films increases with thickness, and increases with temperature . Also its observed that the conductivity of the films decreases with increasing of annealing temperatures and we found there are tow activation energy can be calculated in this study.

الخلاصة

أن أغشية كبريتيد الكادميوم تم ترسيبها على أرضيات رقائق من السليكون بتقنية الترذيذ المغناطيسي المستمر وتم دراسة الخواص الفوتوفولتائية للمفرق ألهجيني المذكور وتم من خلال الدراسة معرفة نوع المفرق ألهجيني وتبين انه من النوع الحاد وكذلك تم معرفة جهد البناء الداخلي لتردد (400) كيلو هيرتز ولسمك ( 300,200,100) نانو متر على التوالي ولدرجات حرارة مختلفة تراوحت بين ( 473,373,303) كلفن على التوالي وكذلك تم دراسة تغير سعة المفرق مع فولتية الانحياز العكسي وتغير الفولتية مع مقلوب مربع السعة وكذلك تم حساب عرض منطقة النضوب . ودراسة تغير التوصيلية الكهربائية كدالة لدرجة الحرارة ولمختلف الأسماك , ويبدو واضحا من هذه الدراسة أن التوصيلية الكهربائية لكل ترسيبات الأغشية تزداد مع السمك ومع درجة الحرارة . كذلك نلاحظ أن التوصيلية الكهربائية تقل بزيادة درجة حرارة التلدين . وكذلك تم  حساب طاقة التنشيط ووجد أن هنالك طاقتان للتنشيط .

- 1. Introduction

Cadmium sulfide is an n-type semiconductor that has been used extensively in many applications, including  photo resistance sensors, low cost solar cells for energy conversion, light emitting diodes, laser materials, optical waveguides and nonlinear optical devices. Different techniques have been used to fabricate cadmium sulfide thin films, such as vacuum evaporation, chemical bath deposition, sputtering, spray pyrolysis and recently pulsed laser deposition [S.M. Mahdavi et. al, 2008] . CdS/Si Heterojunctions are important for the fabrication of photovoltaic and optoelectronic devices. In spite of the huge lattice mismatch the efficiencies of n-CdS/p-Si solar cells [T.D. Dzhafarov et. al , 2009] . CdS thin films are regarded as one of the most promising materials for Heterojunction thin film solar cells. Wide band CdS         (Eg=2.42eV) has been used as the window material together with several semiconductors such as CdTe, Cu2S and InP with 14-16% efficiency . However, due to the high cost of this material, studies were developed towards polycrystalline compound semiconductors and particularly thin polycrystalline films [ C. Santiago  et al, 2008]. There has been considerable interest in recent years directed towards the development of Heterojunction solar cells. Such interestis based on the fact that Heterojunction devices have a number of advantages over diffused p-n junction solar cells include: (i) a lower junction formation  temperature, (ii) higher  spectral response at short wavelengths, and (iii) many of deposited layers have the right indices of refraction to act as antireflection coating [Raid A. Ismail et. al , 2005]  Cadmium sulfide a direct band gap II–VI semiconductor is widely used as a window material in Heterojunction solar cells with various narrow band gap semiconductor like CdS  CdTe, CuInSe2, Cu(In,Ga)Se2, etc. mainly because of its favorable optical properties [A. A. Ibrahim ,2010].                                                                 .

CdS is considered at present one of the most promising materials for photonic devices. It has also high absorption coefficient in the visible range of the solar spectrum and its band gap is close to the optimum value for efficient solar energy conversion [Gamnit Gaewdang ,2004] , and electrical properties makes it as one of the ideal material for their application to solar cell fabrication ,CdS is one of the important materials for application in electro-optic devices such as photo conducting cells, photo sensors, transducers, laser materials, optical wave-guides and non-linear integrated optical devices, also used as photo catalyst  [Dipalee J. Desale ,2011].

2-Experimental

Single-crystal silicon wafers of p-type with (100)  (hkl) orientation are  used as substrates they have Resistivity in the range of (10-20 Ω.cm) and diameter of (76 mm) and thickness (381 µm ) doping with boron , and one face of the wafer is polished to the mirror-like surface. Prior to deposition of CdS, the wafers were chemically etched in dilute hydrofluoric acid to remove native oxides. Then back contact metallization was accomplished by DC planar magnetron sputtering techniques depositing 300 nm , the variation of the junction capacitance versus bias voltage at frequency (400 kHz) , are studied and from the linear  relationship between reciprocal of square capacitance versus bias voltage (1/C2-V ) we found that the junction is an abrupt type . D.C electrical conductivity of CdS films which are deposited on glass substrate with different thickness (100,200 and 300) nm and annealing at different temperature (303,373 and 473) K is present.

Results and Discussion-3

1- C-V measurement

We found from the fig. (1-a ,1-b,1-c) its demonstrates the variation of the junction capacitance versus reverse bias voltage in the range of (0-1) Volt at frequency equal to (400 kHz ) for CdS/Si heterojunction at different thickness and annealing temperatures . It is clear that the capacitance decreases with increasing of the reverse bias voltage and annealing temperatures and the decreasing was non – linear such behavior is attributed to the increasing in the depletion region width which leads to increase of the value of built – in voltage. We can observe from Table (1) that the capacitance at zero bias voltage (Co) decreases with the increasing of the annealing temperatures for all prepared junctions and this is attributed to the decrease in the surface states which leads to an increase in the depletion layer and a decrease of the capacitance. We can notice from Table (1) that the depletion width increases with increasing of the annealing temperature which is due to the decreasing in the carrier concentration which leads to a decrease of the capacitance as given in Table (1).The effect of thickness as well as annealing temperatures are shown in fig. (2),we observe that the capacitance is decreases with increasing of CdS thickness. We relate such data as behavior due to the increasing of the depletion region.                                  .

b))

a))

Fig. (2) Variation of zero bias capacitance as a function of thickness (100, 200 and 300) nm for CdS/Si  heterojunction at different annealing temperatures .

Fig.(1) Variation of capacitance as a function of reverse bias voltage for  CdS/Si heterojunction at  thicknesses  a- (100) nm  b-(200) nm  c- (300) nm and different annealing temperatures .

c))

We found from the fig. (3-a , 3-b,3-c) shows the inverse capacitance square is plotted against applied reverse bias voltage for CdS/Si heterojunction at different thicknesses and annealing temperatures. The plots revealed straight line relationship which  means that the junction was of an abrupt type. The interception of the straight line with the voltage axis at (1/C2=0), represents the built – in voltage . We observed from Table (1) that the built – in voltage increases with increasing of Ta as a result of the decrease in the capacitance value and the increases of the depletion width. Also we can observe that the effect of increasing of the thickness causes an increase in the built–in voltage as given in Table (1) .

Fig. (3) Variation of 1/C2 as a function of reverse bias voltage for CdS/Si heterojunction at thicknesses  a- (100) nm  b- (200) nm  c- (300) nm  and different annealing temperatures .

(a)

(b)

(c)

thicknesses and annealing temperatures .

| Vbi (Volt) | W (μm) | Co (nF) | Ta (K) | Thickness (nm) |
| --- | --- | --- | --- | --- |
| 0.52 | 1.227 | 0.482 | 303 | 100 |
| 0.65 | 1.884 | 0.314 | 373 |  |
| 0.7 | 2.357 | 0.251 | 473 |  |
| 0.65 | 1.517 | 0.39 | 303 | 200 |
| 1.05 | 2.258 | 0.262 | 373 |  |
| 1.5 | 3.817 | 0.155 | 473 |  |
| 1.15 | 2.465 | 0.24 | 303 | 300 |
| 1.7 | 3.817 | 0.155 | 373 |  |
| 1.9 | 5.916 | 0.1 | 473 |  |

2- D.C. electrical conductivity measurement

The variation of electrical conductivity as a function of temperature for different thicknesses and Ta is shown in fig. (4-a ,4-b,4-c) . It is clear from this fig. that the conductivity for all deposited films increases with thickness. Also it is observed that the conductivity of the films decreases with increasing of Ta from (303-473)K . This variation is thought to be due to the changes in the crystallization.

(a)

Fig.(4) σ versus T for CdS films at thickness a-(300) nm   b-(200) nm  c-(300) nm and different   annealing temperatures (303,373 and 473) K.

(b)

(c)

The plots of Ln σ versus 103/T for CdS films in the range (303- 473)K at different thicknesses and annealing temperatures , are shown in Fig. (5-a ,5-b , 5-c) . It is clear from this figures that there are tow transport mechanisms , giving rise to two activation energies Ea1 and Ea2 . The conduction mechanism is due to carriers excitation into localized state at the edge of the band, Table (2) show the effect of thickness and annealing temperature on both activation energies Ea1 and Ea2 for CdS films . It is clear that the activation energies decrease with increasing of the thickness but increase with increasing of annealing temperatures. The decreasing in the activation energy with increasing of thickness may be due to the increase of the absorption and the decrease of energy gap with increasing of thickness .

Fig. (5) Ln σ versus 1000/ T for CdS films at thickness  a- (100) nm     b - (200) nm   c- (300) nm and different annealing  temperatures

(303,373 and 473) K.

(a)

(b)

(c)

Table (2) D.C. conductivity parameters for CdS films at different thicknesses and annealing temperatures .

| Temp.Range K | Ea2 (eV) | Temp.Range K | Ea1 (eV) | σ (Ω.cm) -1 | T (K) | Thickness (nm) |
| --- | --- | --- | --- | --- | --- | --- |
| 385- 473 | 0.25 | 303-385 | 0.089 | 0.03 | 303 | 100 |
| 377- 473 | 0.26 | 303-377 | 0.095 | 0.02 | 373 |  |
| 385- 473 | 0.33 | 303-385 | 0.104 | 0.01 | 473 |  |
| 370- 473 | 0.161 | 303-370 | 0.078 | 0.18 | 303 | 200 |
| 364- 473 | 0.169 | 303-364 | 0.087 | 0.08 | 373 |  |
| 377- 473 | 0.173 | 303-377 | 0.091 | 0.05 | 473 |  |
| 385- 473 | 0.156 | 303-385 | 0.06 | 0.45 | 303 | 300 |
| 392- 473 | 0.163 | 303-392 | 0.065 | 0.22 | 373 |  |
| 370- 473 | 0.170 | 303-370 | 0.066 | 0.06 | 473 |  |

4- Conclusions

In this studies we found decrease in the capacitance value and the increases of the depletion width with increasing of annealing temperature. Also we can observe that the effect of increasing of the thickness causes an increase in the built – in voltage. D.C electrical conductivity for all deposited films increases as the thickness increases and temperature but decreases with increasing of annealing temperature from 303 K to 473 K. It is clear that the activation energies decrease with increasing of the thickness but increase with increasing of annealing temperatures.

References

A. A. Ibrahim, (2010) " Electrical properties of the CdS/InP solar cell for photovoltaic applications ", J Mater Sci: Mater Electron , 21, pp . 491- 495.

C. Santiago Tepantl´an , A.M. P´erez Gonz´alez and I. Valeriano Arreola  , (2008), " Structural, optical and electrical properties of CdS thin films obtained by spray pyrolysis ",  REVISTA MEXICANA DE FI´SICA, 54 (2) , pp 112- 117 .

Dipalee J. Desalea, Shaeed Shaikha, Farha Siddiquia Arindam Ghosha,

Ravikiran Birajdara, Anil Ghuleb, Ramphal Sharmaa, (2011)," Effect of annealing on structural and optoelectronic properties of CdS thin film by SILAR method",

Advances in Applied Science Research, 2 (4), pp. 417 – 425.

Ngamnit Gaewdang and Thitinai Gaewdang, ( 2004), " Thickness Dependence of Structural, Optical and Electrical Properties of CdS and CdS:In Films Prepared by Thermal Evaporation ", Technical Digest of the international PVSEC-14, Bangkok , Thailand , p .123 .

Raid A. Ismail , Abdul-Majeed E. Al-Samar ai and Omar A. A. Sultan, (2005),           "  p-CdS/n-Si AnIsotype Heterojunction solar cells With Efficiency of 6.4% ", Qatar Univ – Sci, j,  25, pp .31 – 39.

S.M. Mahdavi, A. Irajizad1, A. Azarian1 and R.M. Tilaki1  , (2008), " Optical and Structural Properties of Copper Doped CdS Thin Films Prepared by Pulsed Laser Deposition ", Scientia Iranica, ,  Vol. 15, No. 3, pp.  360-365 .

Salwan K. J. Al-Ani Raid A. Ismail  Hana F. A. Al-Ta’ay , (2006), " Optoelectronic properties n:CdS:In/p-Si Heterojunction Photodetector", J Mater Sci: Mater Electron  17 , pp.819–824.

T.D. Dzhafarov. , F. Ongul., S. Aydin Yuksel., ( 2009)," Effect of indium diffusion on characteristics of CdS films and nCdS/pSi Heterojunctions ", Volume 84, Issue 2, 18 September  , pp . 310-314 .