Improvement of Some Electrical Properties for PS-TiO2 Composite.

Abd-ALraheem Khadim Abdd-Ali                      Hassan Jassim Mutlak

Faculty of Materials Engineering         Department of Electrical Engineering

Israa Ali Hussien

Faculty of Materials Engineering

Abstract :

In this research the effect of filler content on improving some electrical properties of polystyrene filled with TiO2 powder has been studied. For that purpose, the  polystyrene (PS) samples with TiO2 additive prepared with different percentages (0,5,10,15,20,25,30) wt.% . The results show that the  D.C electrical conductivity of such composite improved about 52% when the concentration of TiO2 is increased.

Also the results show that the dielectric constant, dielectric loss, are improved about 51%,77% respectively,and A.C electrical resistivity are changed with changing the concentration of the filler and frequency of applied electrical field, that means the A.C electrical conductivity of  PS-TiO2 is improved about 86%. The results  show good improvement in electrical properties of this research that agreed with theoretical principles.

الخلاصة:

في هذا البحث  تم دراسة تاثير اضافة اوكسيد التيتانيوم على تحسين بعض الخواص الكهربائية للبولي ستايرين المقوى بمسحوق اوكسيد التيتانيوم .لذلك تم تحضير عينات من من البولي ستايرين المضاف له اوكسيد التيتانيوم بنسب وزنية مختلفة وهي %wt(30,25,20,15,10, 5,0)  .النتائج أظهرت ان الموصلية الكهربائية المستمرة تتحسن مع زيادة تركيز اوكسيد التيتانيوم بمقدار 52% .كما اظهرت النتائج ان ثابت العزل والفقدان العزلي يتحسنان بمقدار 51% ,77% على التوالي وكذلك المقاومة الكهربائية بالتيارالكهربائي المتناوب تتغير مما يدل على إن الموصلية الكهربائية المتناوبة تتحسن بمقدار 86%  مع تغيير تركيز اوكسيد التيتانيوم المضاف وتردد المجال الكهربائي المسلط. النتائج اظهرت تحسن جيد في الخواص الكهربائية لهذا البحث مما يتفق مع المبادئ النظرية.

Introduction

Composite materials, which are usually fabricated with an emphasis on properties such as mechanical strength, have also been used in electronic applications One such class of composite materials is particulate- filled conductive polymer matrix composites . Because of the technological importance of these composites, their electrical properties have been widely studied.( (Vishal Singh et al., 2003). Recently polymer matrix-ceramic filler composites are receiving increased attention due to their interesting electrical and electronic properties. Integrated decoupling capacitors, angular acceleration accelerometers, acoustic emission sensors electronic packaging, and organic solar cells are some potential applications(Janne Halme, 2002). Ceramic materials are typically brittle, possess low dielectric strength and in many cases are difficult to be processed requiring high temperature. On the other hand, polymers are flexible, can be easily processed at low temperatures and exhibit high dielectric at low temperatures and exhibit high dielectric break-down fields (Kontos et al., 2007). Polystyrene is a preferred material in electronic  technology due to its dielectric and mechanical properties and its low costs .A surprising property of filled polymer composites is their conductivity profile as a function of filler concentration it is found that their conductivity does not increase continuously with increasing  filler content, but shows a sudden jump to higher conductivity. This conductivity behavior resulting a sudden insulator – conductor transition is a scribed to percolation process, and the critical filler concentration at which the conductivity jump occurs is called percolation threshold (Bhatlacharya et al., 2008). Kontos et al., (2007) studied The dielectric response of polymer composites consisting of an epoxy resin matrix and rutile TiO2 ceramic filler The relaxation phenomena  recorded include contributions from both the polymeric matrix and the reinforcing phase resin. . The DC electrical conductivity of all samples was evaluated at 0.1 Hz, where a leveling off of the corresponding curves is observed at the relatively high temperatures. DC electrical conductivity increases with increasing temperature following the VTF model . Vishal Singh et al.,(2003) studied Dielectric properties of Al–epoxy composites were characterized as a function of composition,  frequency, and temperature The dielectric constant increased smoothly with an increase in the concentration of aluminum An increase in dielectric constant was also observed with an increase in temperature as well as with a decrease in frequency. In general, dissipation factor values for composites with higher concentrations of aluminum were greater than those with lower volume content of aluminum. Also, the dissipation factor showed an increase both with a decrease in frequency and an increase in temperature. Bahaa et al.,(2010) studied the effect of the addition of TiO2 on some electrical properties of poly-methyl methacrylate . They show that the D.C. electrical conductivity changes when the concentration of additional TiO2 increases and when the temperature increases. Also the activation energy changes when the additional TiO2 increases. The aim of this work deals with the effect of TiO2 on improvement some electrical properties of polystyrene.

Experimental work

The material used in the present paper is the polystyrene as matrix and TiO2 as a filler with purity about 99.8%. Electronic balances of accuracy 10–4 have been used to obtain a weight amount of TiO2 powder and polymer powder. These are mixed by hand lay up and the microscopic examination is used to obtain homogenized mixture. The weight percentages of TiO2 are (0, 5, 10, 15, 20,25,30) wt.% The Hot Press method is used to press the powder mixture. The mixture of different TiO2 percentages have been compacted at temperature 175oC under a pressure of 100 par for 10 minutes. It is cooled to room temperature, the samples were disc shaped of a diameter of about 15 mm and thickness ranging between (1.055-1.52) mm .The coating unite(Edwared coating System E3C6A) has been used for deposition of thin film Aluminum electrode on both sides of each sample. The volume electrical conductivity σν is defined as:(Posh, et al.,1972)

σν                                                            (1)

where:

A = guard electrode effective area.

R = volume resistance (Ohm).

L = average thickness of sample (cm).

In this model the electrodes have circular area A=D2π/4 where D=1.1 cm.

The dielectric properties of PS-TiO2 composite were measured using (Agilent impedance analyzer 4294A).

In the frequency(f) range (25×102-5×106) Hz at room temperature. The measured capacitance (w) was used to calculate the dielectric constant ,έ(w) using the following expression:

έ(w) =C(w) d/A ε0                             (2)

Where d is sample thickness and A is surface area of the sample . whereas for dielectric loss

ε"(w):

ε"(w) = έ(w) × tanδ(w)                                       (3)

Where: tanδ(w) is dissipation factor

Results and Discussion

Figure 1 shows the electrical volume conductivity enhancement of the composite by increasing the concentration of TiO2 filler . The increase of conductivity with increasing concentration of TiO2 is due to the increase of the charge carriers, which increase with the increase of filler contact, where the TiO2 particles at low concentrations are represented by small darker regions. They become large when the TiO2 content increases and the networks connect each other as illustrated in the microscopic photographs in Fig. 5 taken for samples of different concentrations (Szczepanik et al.,2009, Srivastava and Mehra, 2009).

-1

Fig(1):Variation of  D.C Electrical Conductivity with TiO2 concentration

for PS-TiO2 composite

.

The variation of dielectric constant for PS- TiO2 composites of different Titian concentration as function of frequency at room temperature is shown in figure (2). At low frequency region in addition to polarization due to PS and TiO2 , the space charge polarization plays a major role in increasing dielectric constant of composite [Hamzah et al, 2009]. The space charge polarization arises from the PS/ TiO2 interfaces. The dielectric constant increases with weight fraction of TiO2. The increase in dielectric constant with weight fraction of TiO2 supports the fact of the space charge polarization contribution. The dielectric constant of composite increases with addition of TiO2  reflects the formation of capacitance network of TiO2 (M. Revanasiddappa, 2008).

Fig(2): Variation of Dielectric Constant with frequency for PS-TiO2 Composite.

The variation of the dielectric loss of PS-TiO2 composites as a function of frequency at room temperature is shown in figure (3) , the values of dielectric loss are high for frequencies, and decreasing with frequency and increases to reach maximum. The oscillatory behavior of dielectric loss may be due to some relaxation processes which usually occur in heterogeneous system. The relaxation peak at W=3.5 MHz is appears clearly in all low TiO2 concentration on specimens. The increasing of TiO2 concentrationincreases the height of the peak and increasing its broadness for these specimens. This is due to the overlapping of relaxation process which are attributed to some structural changes that take place in the composite as result of filler addition . The increasing of the peak height of dielectric loss  with increasing TiO2 concentration indicates the enhancement of conductivity in these specimens , i.e. enhancement of losses (Raghavendra et al,2007, Pillal,1980).

Fig(3): Variation of Dielectric Loss with frequency for PS-TiO2 Composite.

The variation of A.C electrical resistivity as a function of frequency for (PS-TiO2) composites at 303K is given in figure (4). The figure shows that in low, intermediate and higher frequency region the electrical resistivity for all (PS-TiO2) composites is decreasing with The D.C and A.C Electrical Properties of (PS-TiO2) Composite  frequency. We conclude from that the A.C electrical conductivity is increased with increasing the frequency. The increasing of A.C electrical conductivity in high frequency region can be related to the electronic polarization as well as to the hopping of charge carrier over a small barrier height. The figure also indicates that σA.C is increasing with increasing TiO2wt.% content, a result which supports the suggestion of hopping of charge carrier conduction mechanism. The increasing of A.C electrical conductivity with angular frequency in the low frequency region can be attributed to the interfacial polarization  (Hamzah et al., 2009).

Fig( 4): Variation of A.C Electrical Resistivity with frequency of PS-TiO2 Composite.

-cm

Conclusion

- The D.C electrical conductivity of the polystyrene increases by

increasing the TiO2 concentrations and the temperature.

- The dielectric constant decreasing with the frequency and increase with TiO2 wt.% content .

- The dielectric loss is oscillatory in the whole frequency region and increase with increasing TiO2 wt.% content .

4.The A.C electrical resistivity of PS-TiO2 composites is decreasing  with

increasing frequency of applied electrical field and TiO2 wt.% content. We

conclude that  the A.C electrical conductivity is increased with increasing the

frequency of applied electrical field and TiO2 wt.% content. As we mention in

equation (1)

b-

a-

a-

c-

d-

e-

f-

g-

Photomicrographs for Ps-TiO2 composite  5   Fig.

TiO2, b-5% TiO2,c-10%TiO2,d-15%TiO2,e-20%TiO   %a-0
f-25%TiO2, g-30%TiO2 600X

Acknowledgments

This work was partially supported by the Ministry  of Science and Technology –Iraq –Baghdad/in Ceramic Department, and their staff  to achieve all electrical testes .

References

Vishal Singh, A. R. Kulkarni, T. R. Rama Mohan,2003," Dielectric Properties of Aluminum–Epoxy Composites" ,Journal of Applied Polymer Science, Vol. 90,pp. 3602–3608.

Kontos G. A. , Soulintzis A. L.  , Karahaliou P. K.  , Psarras G. C.  , Georga S. N.  ,

Krontiras C. A.  , Pisanias M. N.  , 2007, "Electrical relaxation dynamics in TiO2 – polymer matrix Composites", eXPRESS Polymer Letters Vol.1, No.12 ,pp.781–789.

Janne Halme,2002,"Dye-sensitized nanostructured and organic photovoltaic cells:

technical review and preliminary tests", MSc. Thesis , Helsinki University of Technology, Department of Engineering Physics and Mathematics.

Bhattacharya S., Sachdev V.K., Tandon, 2008,"Electrical properties of Graphite filled polymer composites", 2nd National Con R.P. ference Mathematical Techniques: Emerging Paradigms for Electronics and IT Industries, pp.100-101.

Bahaa Hussein, Marwa Abdul-Muhsen ,Ahmed Hashim ,2010,"Study of some electrical properties for PMMA-TiO2 composites"  ,J.  of Atti Della, Fondazione Giorgio Ronchi .

Szczepanik M.  , Stabik J. , £azarczyk M. , Dybowska A.  , 2009, "Influence of graphiteon electrical properties of polymeric composites ", Archives of Materials Science and Engineering, Vol. 37,Issue 1, pp.37-44.

Srivastava N. K.  , Mehra R. M. ,2009," Study of the electrical properties

of polystyrene–foliated graphite composite" , Materials Science-Poland, Vol. 27, No. 1,pp.109-122.

Revanasiddappa M. , Syed Khasim, Raghavendra S. C.  , Basavaraja C.  , Suresh T. and Angadi S. D , 2008,  “Electrical Conductivity Studies on Co(II), Cu(II),Ni(II) and Cd(II) Complexes of Azines”, E-J.Chem, Vol .5, No.4, pp.797-801.

Hamzah M., Saion E. , Kassim A. , Mahmud E. and Shahrim I., 2009, "J. for the advancement of Sci", Vol. 1, No. 1, pp. 9-14.

Pillal P. K. C and Rashmi , 1980"Dielectric properties of polystyrene and some Releated polymers ", Britain, Intern. J. polymeric mater , Vol. 8 , pp.255-263.

Posh F. ,Franses J. ,1972, " The Physic Principals  " , Mac grew Hill Inc.