Design and Characterization of V3+:YAG Passive Q- switched end-pumped Nd: YAG Microlaser

Jassim M. Jassim

Department of laser Physics, University of Babylon

## Abstract

Q-switched Microchip laser emitting radiation at wavelength 1342 nm was designed and characteristic study of a passively Q-switched  ( V3+:YAG) diode pumped solid state laser system is presented , An active laser part (Nd3+:YAG), and a saturable absorber (V3+:YAG, T0 = 97 %).The microchip resonator consists of dielectric mirrors directly deposited on the monolith Surfaces, the output coupler has reflecting 95% @ 1342 nm was placed on the V3+-doped part. Q-switched microchip laser was tested under pulsed laser diode, has been investigated the laser output parameters such as energy, peak power, and pulse width a comparison between theoretically calculated results and simulation results using a software which calculates the Q-switched solid state laser parameters was performed. There was a good agreement with the theoretical calculations and the simulation values.

الخلاصة

تم في هذا البحث تصميم ليزر الحالة الصلبة ذات المفتاح السلبي نوع ( V3+:YAG)  والمضخوخ بشكل طولي بواسطة ليزر أشباه الموصلات والذي يدعي (( Microchip laser لإنتاج نبضة ليزر ذات طول موجي (1342nm) باستخدام بلورة (Nd3+:YAG) كوسط فعال . المرنان البصري يتألف من مرآتين أحداهما ذات انعكاسيه تامة والمرأة الأخرى ذات انعكاسيه جزئيه 95% للطول ألموجي  1342 nm ،كما تمت  دراسة تأثير خصائص المفتاح السلبي نوع ( V3+:YAG)  ذات النفاذية (T0 = 97 %). على خصائص نبضة ليزر الحالة الصلبة نوع ( Nd:YAG)  من حيث ألقدره , الطاقة وعرض النبضة   . نتائج الحسابات التصميمية المستخلصة تمت مقارنتها مع نتائج ألتشبيهيه المستخلصة من برنامج معد لغرض حساب معلمات ليزرات الحالة الصلبة ذات مفتاح عامل نوعيه و أظهرت توافقا جيدا" فيما بينها.

1- Introduction:

Most of the solid state passive Q-switches which have been developed have operated using the 1064nm transition of Nd3+ and therefore have been based on the saturable absorption of Cr4+ ions [Swidersti 2005]. The operation of Cr4+ devices ranges from approximately 900-1100nm, depending on the host properties [Zhang 1997]. a new saturable absorber, which could operate at longer wavelengths, in particular with the 1342nm transition of Nd3+ two absorption peaks were observed at 1140nm and 1320nm, and attributed to the 3A2→1E(1D) and 3A2→3T2(3F) transitions respectively of the tetrahedrally coordinated V3+ ion [Malyarevich  1998]. The fast decay of the 1E(1D) level to 3T2(3F) has previously been measured to be 0.13ns[Jabczy  2001]. To complete our knowledge of the system we measured the lifetime of the longer-lived decay 3T2(3F) →3A2 using a pump-probe technique. Laser pulses at 1080nm with 15ps pulse duration were used for pumping and probing. The lifetime of the 3T2(3F) level was found to be (22 - 6)ns[ Sun  and Hou 2008 ].Trivalent neodymium was the first rare-earth ion to be used in a gain material, and has remained the most commonly used active ion found in solid state lasers. The intense luminescence and absorption of the narrow energy levels of Nd3+ along with a workable fluorescence lifetime have helped Nd3+ achieve its dominance. It is traditionally pumped on either the 760nm or 810nm absorption bands though it can also be pumped in the green spectral region. The two main photon decay routes from the 4F3/2 metastable level are the 4F3/2 → 4I11/2 transition (producing radiation at ~1.06µm) and the 4F3/2 →4I13/2 transition (producing radiation at ~1.3µm). Both of these are four level systems, giving efficient CW operation on these transitions at 300K and above, without significant population in the lower lasing level causing reabsorption. The third transition  4F3/2 →4I9/2 (producing radiation at ~0.9µm) is a quasi-four level system, with the lower lasing level close to the ground level, having a significant thermal population. The fourth transition is two orders of magnitude weaker, though has been shown to lase at 1.83µm [Koechner , 2006].

-Theory2

When a cw power is pumped the active medium, the population inversion  would reach a maximum value and decreases thereafter and the cavity losses are periodically switched from high to low value ,then the laser output consists of a continuous train of Q-switched pulses .During each pulse inversion falls from its initial value Ni (before Q- switching) to the final value Nf (after the Q-switched pulse) [Svelo 1998]. The population inversion is restored to its initial value Ni by the pumping process before the next Q-switched event. Since the time taken to restore the inversion is roughly equal to the upper –state lifetime (τ) of active meduim, the time between two consecutive pulses must equal or be shorter  than (τ) .The repetition rates of cw –pumped Q-switched lasers typical range from a few kilohertz to a few tens of kilohertz and for pulsed pumped the repetition rate equal repetition pumped source . For this can many expressions may be found for pulse energy ( E  ) ,pulse peak power ( Pm  ) and  real pulse duration ( W  ) and by using the following equations,[ Zhang  2000 , Degnan 1995] .

E=π∗hν∗Wo24∗γ∗σln1R∗Φinteg−−−−−−−−−−−−−1

Pm=π∗hν∗W024∗ln1R+ln1To2+L∗ln1R∗Φm−−−2

W=tr∗Δτln1R+ln1To2+L−−−−−−−−−−−−−−−−−−−3

Where:

σ       is the stimulated emission cross-section of active medium

L      is the remaining round-trip dissipative optical loss.

Wp   is the radius of the pump beam in the gain medium

Wo  is the beam waist

R     is the reflectivity of the output mirror

To    small –signal transmission of the saturable absorber is equal

Δτ     is the normalized pulse duration

Φm    is the maximum value of photon density

Φinteg  is the integral of photon density over τ from zero to infinity

h        is the Planck’s constant

γ	 is inversion reduction factor

hν 	 is the laser photon energy

A saturable absorber is designed to have large ground state absorption    (σgsa ) at the lasing wavelength this prevent laser oscillation untill the population inversion gives gain exceeding the losses provided by the output mirror and saturable absorber. The ratio of the laser saturation energy to the absorber saturation energy defined by (α ),          [Degnan 1989].

α=σgsaγ∗σ−−−−−−−−−−−−−−−−−−−4

The inversion reduction factor is equal to ( γ=fa+fb) where fa ,fb are,respectively, the Boltzman occupation factors of the upper and lower laser levels of the gain medium. For a Nd:YAG gain medium at room temperature, fa =0.19 and fb = 0.41 [Sulc  2005]. The ratio of the initial population inversion density to the threshold population inversion density can be expressed in equation (5)

N=ln1R+ln1To2+Lln1R+σesaσgsa∗ln1To2+L−−−−−−−−−−−−−−−−−5

Where:

σesa     is the excited –state absorption cross-section area of the saturable absorber.

σ gsa         is the ground-state absorption cross-section area of the  saturable  absorber.

3-The Proposed set-up of the design

A schematic set-up of the passive Q-switched device is shown in Fig.(1) It  consists of the driver unit, the laser head, which contains the pump diode laser emitting optical power about  2 W pulses of 808 nm wavelength and collimating the beam by a focusing lens of 238 μm focal length  in active medium type (Nd:YAG) .One end has a high-reflection coating for the 1342nm wavelength to function as a mirror for the resonator and an antireflection (AR) coating for the 808nm wavelength to allow the pump beam to enter the rod. The other end has an AR coating for the 1342nm .The Stimulated emission cross section (6.5 × 10 -19 cm2) and Spontaneous fluorescence lifetime (240 μs )[3]. The passive Q-switching V3+:YAG. Crystal has 0.01 mm thickness, Small Signal transmission of 97 (%) @1342nm and ground state absorption cross ( 7.2x10-18 cm2). This crystals was coated AR/AR at 1342nm to reduce losses, with 98.8 % transmission at 1342nm, and the output-coupling mirror radius of curvature of coupler mirror is 300mm with 5% transmission at 1342nm,this mirror with another plane mirror construct the optical resonator of hemispherical type having a length of 4 mm with beam waist of 121 μm.

Figure (1)   Schematic set-up of the passive Q- switched device

4-Calculations of system parameters

In the present work ,pulse energy (E), Peak power (Pm) , and Real pulse width (W) have been calculating using equations[1,2&3] are 70μj,  26KW and  2.6 ns respectively. We can shown in table (1) all parameters used for calculating the design model of passively Q- switched end pump laser system.

Table (1) design parameters

| Parameters | Value |
| --- | --- |
| Simulated emission cross section | 6.5 × 10-19 cm2 |
| Spontaneous ;putrescence lifetime | 240 μs |
| Length of the laser rod | 3 mm |
| Cavity round trip time tr | 0.026ns |
| Photon energy | 1.48× 10-19 J |
| Spot size at the laser rod | 121 μm |
| Spot size at the GaAs wafer | 100 μ m |
| Absorption Coefficient | 31.4 cm-1 @ 808 nm |
| Absorption Length | 0.32 mm @ 808 nm |
| Intrinsic Los | Less 0.3% cm-1 , @1064 nm |
| Refractive Index to saturable | 1.82 |
| Saturated Transmission Tmax @1342 nm | 97 (%) |
| Small Signal Transmission T0 @ 1342nm | 40 (%) |
| Ground State absorption Cross-Section | ( 7.2x10-18 cm2) |
| Excited State absorption Cross-Section | ( 7.4 x10-19 cm2) |
| Contrast Ratio | 10 |
| Saturation Intensity | 30 (MW/cm2) |
| Pump power | 2W pulsed |
| Optical length of resonator | 4 mm |
| Radius curvature of coupler mirror | 300 mm |
| Beam waist | 121μm |
| Focal length of afocal lens | 200 μm |
| Reflectivity of the output mirror | 0.95 |
| Inversion reduction factor | 0.6 |
| length of saturable absorber | 0.01 mm |
| the [ α ] | 20 |
| the [ Δτ ] | 14 |
| the [ Φm ] | 0.1 |
| the [ Φinteg] | 1 |

Small- signal transmission of passive Q-switched (V3+: YAG) has been investigated, figure (2) shows the relation between pulse duration with different Small- signal transmission of V: YAG passive Q-switch, the pulse duration decreasing slightly less than 1ns duration when the small- signal transmission of decreased to [90%]. When the small- signal transmission of V3+: YAG decreased this will yields decreasing in quality factors which yield   increased losses . Exceeding these losses with more pumping power means large energy store which is done by  preventing laser oscillation until the population inversion gives a high gain exceeding the losses yielding  fast oscillation and fast decreasing to the population inversion. Hence getting shorter pulse duration. In figure (3) shows the relation between peak power with different Small- signal transmission of V: YAG passive Q-switch, the peak power increased with decreased small- signal transmission. Normally when the pulse duration decreased ,the peak power increased .

Figure

(

2

)

relation between pulse duration with

various small

-

signal transmission

0

0.5

1

1.5

2

2.5

3

90

91

92

93

94

95

96

97

Small- signal transmission [ To %]

Pulse duration [ ns]

Figure

(

3

)

relation between peak power with various small

-

signal transmission

0

20

40

60

80

100

120

140

160

90

91

92

93

94

95

96

97

Peak power [ Kw ]

5-Simulation results

To check the designed calculated  results we tried to compare such results with some simulation results. Which were evaluated using a software package  for Q-switched solid state laser dynamics to evaluate the  pulse energy (E), peak power (Pm) , and pulse width (W ) .The output of such package is shown in figure (4) . The pulse energy E = 69μJ, peak power Pm =28 KW  , and real pulse width W = 2.47 ns .We can shwon all parameters used for calculating the simulation model of passively Q- switched  end pump laser system .

Laser Medium

Stimulated emission cross-section, cm^2 =7.140E-019

Peak absorption cross-section, cm^2 =7.200E-020

Absorption coefficient, cm^-1 =2.500

Degeneracy factor =1.000

Spectra overlap coefficient =0.252

Lasing wavelength, nm =1342.000

Active element refractive index =1.810

Concentration Nd, cm^-3 =1.380E+020

Tau 32, us =240.000

Tau 43, us =3.000

Tau 31, us =10000.000

Tau 21, us =0.010

Initial 1-level concentration =0.999937

Initial 2-level concentration =0.000063

Initial 3-level concentration =1.060E-024

Initial 4-level concentration =1.140E-026

Excitation quantum yield =1.000

Branching of luminescence =0.100

q1 =0.014

q =0.000064

Configuration

Cavity length, cm =0.400

Reflectivity of output coupler =0.950

Active element dissipative losses, cm^-1 =0.015

Intrinsic resonator losses =0.0040

Overlap efficiency =0.900

Lasing area, cm^2 =0.0090

La, cm =0.300

Lb, cm =0.100

Ld, cm =0.100

Pump

Pump duration, us =240.000

Pump power, W =2.000

Pump coupling optics efficiency =0.950

Pump reflectivity =0.950

Pump wavelength, nm =810

Pump scheme type =Endpump

Pumped length, cm =0.300

Pumped area, cm^2 =0.010

Average pump flow Fav, a.u. =1.019

Effective pump flow, W/cm^2 =968.301

Input intensity, W/cm^2 =950.000

Saturation pump intensity, W/cm^2 =2.255E+006

Shutter

Thickness, cm =0.010

Refractive index =1.835

Initial transmission =0.970

Shutter Type =Passive

Decay time, us =0.220

Absorption cross-section, cm^2 =10.000

SIGRESS =10.000

Shutter transmission causeed by nonresonator losses =1.000

Special Simulation period add, us =2.000

Result

Interctivity peak intensity, MW/cm^2 =99.244

Full output energy, J =0.00063

Full efficiency =0.263

Time of peak pulse, us =55.121

Output pulse duration, ns =2.472

Giant pulse output energy, J =0.000069

Giant pulse generation efficiency =0.028

Stored energy before the shutter switched on, J =0.00014

Figure (4) Laser pulse

6-Conclusions

Simplest Q-switched laser system construction and adjustment, shorter laser resonator more compact laser system, smaller sensitiveness to all mechanical disturbance, rugged and low-maintenance system, generation of shorter pulses. The  important parameter of V:YAG passive Q-switched affecting the pulse energy ,peak power and pulse duration ,which have been studied in this work is thickness. The thickness increase lead to decreased pulse duration and increased peak power.  Thus it can be concluded that a careful choice of Q-switched crystal thickness should be satisfied.

##### References

Degnan J. (1995), “Optimization of passively Q-switched lasers," IEEE J. Quantum  Electronics,  vol.31, pp. 1890-1901.

Degnan J. (1989), ‘‘Theory of the optimally coupled Q-switched laser,’’ IEEE J. Quantum Electron. vol. 25,pp. 214–220.

Jabczy J. K.( 2001) "Application of V3+:YAG crystals for Q-switching and mode-locking of 1.3-¹m diode-pumped neodymium lasers," Optical Engineering" No.40, pp. 2802.

Koechner W. (2006,) Solid state laser engeniering. Springer-Verlag, Berlin, 6th edn.

Malyarevich A. M. (1998), "V:YAG a new passive Q-switch for diode-pumped solid state lasers," Applied Physics B: Lasers and Optics 67, pp. 555.

Sun Y., and Hou X.( 2008), "Passively Q-Switched 1.32-mm Nd:YAG Laser with a V:YAG Saturable Absorber  "Laser Physics, Vol. 18, No. 4, pp. 393–395.

Sulc J. (2005), "Nd:YAG/V:YAG microchip laser operating at 1338nm" Laser Phys. Lett. 1, No. 1,pp. 1–6.

Swidersti J. (2005), ”Numerical analysis of passively Q-switched Nd:YAG laser with  a Cr+4:YAG” opto-electronics review, vol. 13, No. 1, pp. 43-50.

Svelo O. (1998) , "Principlles of Lasers" ( forth edition),Plenum Press,  New York,

Zhang X. (1997),“ Optimization of Cr –Doped Saturable-Absorber -  Q    Switched Lasers” IEEE JOURNAL OF QUANTUM ELECTRONICS, VOL. 33, NO. 12.

Zhang X. (2000), ” Modeling of passively Q-switched lasers”   J. Opt. Soc. Am. B/ Vol. 17, No. 7.