Effect of Energy Drinks on the Corrosion Behavior of Ni-Cr Dental alloys

Alia'a Saadon Abdulrazzaq       Dhifaf Mohammed Saleh

Market Research&Consumer Protection Center

Baghdad University

alia.sadon@yahoo.com

dhifaf78@yahoo.com

Abstruct

The objective of the current study was to investigate the release of Ni and Cr ions from dental casting alloys. Four commercial alloys were used in the experiments, all alloy samples rollers of identical dimensions with diameters of 10 mm and heights of 5 mm were used, made by the manufacturer. Four samples of energy drinks (Tiger, Power horse, Red bull, Jaguar) were used for each tested dental alloy and tested with  times.

The ion release from the above tested dental alloys in the above mentioned energy drinks was measured over 4 time intervals, i.e. after 0,1, 24 hours and 7 days respectively. Energy drinks were analyzed by atomic absorption spectrophotometer. Results show that the Ni-Cr alloy released great amounts of Ni and Cr ions in all four energy drinks so that on the very first times of measurement these amounts exceeded the approved daily dietary intake of this elements. Gradually, the amount of the released Ni and Cr ions increased with great variability in all energy drinks.

Keywords: Corrosion ,Ni-Cr ions, Energy drinks

الخلاصة

هدف الدراسة الحالية هو لتشخيص ترحيل ايونات النيكل Niو الكروم Crمن اطقم الاسنان . تم استعمال اربعة اطقم اسنان تجارية في التجارب و جميع اطقم الاسنان ذات ابعاد القطر  10 ملم و الارتفاع    5  ملم .و قد تم تصنيعها محلياً .

تم استعمال اربعة نماذج من مشروبات الطاقة ( تايكر  و بورهورس و ريدبول و جكوار)  في اختبارات اطقم الاسنان مع الوقت .ان ترحيل الايون من الاطقم المستخدمة في اعلاه في مشروبات الطاقة اعلاه قيست باربعة ازمنةهي : الصفر ، 1 ، 24 ساعة و 7 ايام على التوالي . مشروبات الطاقة تم تحليلها بواسطة جهاز المطياف الذري ، و قد اظهرت النتائج ان اطقم الاسنان للنيكل – كروم رحلت كميات كبيرة من ايونات النيكل

Niو الكروم Cr في جميع مشروبات الطاقة و قد كان الترحيل على اعظمه في الاوقات الاولى . و ان الترحيل لايونات النيكل Niو الكروم Cr ازداد بالتدريج في جميع مشروبات الطاقة.

الكلمات المفتاحية: التاُكل , ايونات Ni-Cr , مشروبات الطاقة

Introduction

Dental erosion has been reported to be a growing health problem -(Seow and Thong ,2005,Arnadottir  and  etal.,2003) possibly accounted for by the monumental increase in the consumption of soft drinks, fruit juices and sport drinks in the UK, US and many other countries (Hooper and etal.,2007). Erosion in the chemical dissolution of the surface of dental hard tissues by acids without the involvement of microorganisms (Zipkin and  McColure,1949). Its process can lead to reduction in size of teeth and depending upon the severity and length of exposer may lead to the total destruction of the dentition (Meurman and ten ,1996). For the first time, England included the evaluation of tooth erosion in its national dental health survey in 1993, indicating the importance of this dental problem (O'Brien ,1994).

Causative factors for tooth erosion are divided into extrinsic and intrinsic categories. Intrinsic erosion occurs from involuntary gastrointestinal disturbances such as gastro- esophageal reflux disease (GERD) and from voluntary regurgitation of gastric acids exhibited by anorexic and/or bulimic individuals .

Extrinsic tooth erosion causes include environmental factors, medicaments , life style , and diet (Gandara  and Truclove,1999, Shipley and etal.,2005). In modern societies the extrinsic factor is becoming more important , due to the increased consumption of acid drinks as soft drinks , sport drinks , fruit juices and fruit teas (Lussi and  etal.,2004).

Most people view energy drinks consumption as fairly innocuous and its consumption is not as harmless as generally believed , however, there are a number of serious health issues associated with regular consumption of energy drinks . One   peerreviewed study has reported 25 separate harmful effects associated with the consumption of carbonated soft drinks (Amato and  etal.,1997).

Dental casting alloy should not be toxic . They should also be resistant to corrosion , which means that they should not chemically react with either acids or alkaline solutions . In addition , they should have good physical and technological properties such as hardness and strength . Besides , which they should be suitable for heat processing . Furthermore ,such alloys should be available for patients at low cost . Since the price of gold rose dramatically in the 1930s , a large number of new ,non-noble alloys were developed for use in dentistry a part from the Ni – Cr alloy used for dental metal ceramic appliances are base metals or non – noble alloys ( Stipetic and  etal.,2002).

All the alloys available on the dental market should undergo the following three stages of testing : in vitro testing on laboratory animals , in vivo testing on laboratory animals and in vivo testing on patients . According to the specification of the American Dental Association the most important feature which should be tested before the alloys are available on the dental market is their biological feature that is their biocompatibility ( Stipetic and  etal.,2002).

Dental casting alloys with high and low noble metal contents are widely used dentistry . Corrosion of alloys occurs in oral environment . The biocompatibility of dental casting alloys is a critical issue because these alloys are in long – term intimate contact with oral tissues . The biocompatibility may correlate with elements of dental casting alloys(Can and  etal.,2004, Wataha ,2000) . The release of elements from dental casting alloys is directly related to adverse biological effects . Certian environmental conditions around the alloy will affect the release of elements . Areduction in PH will increase elemental release from dental alloys . This effect is especially pronounced for nickel – based alloys . The elemental release from casting alloys has also been studied extensively in vitro in short and long term experiments (Brune,1986, Wataha and Malcolm,1996).

Studies have shown that the release of elements from the alloys may correlate with different factors . Wataha and other many investigataters (Wataha and  etal.,1995, Brune,1986, Tai  and  etal.,1992, Wataha and Lockwood,1998) have been studied about the effects of the ions released . They have shown that the relationships between elemental release and toxicity are complex . Several statements can be said about release of elements from dental alloys . In the mouth , alloys may be exposed to transient PH changes either from foods or plaque .  The reduced PH would increase elemental release because it acts like corrosive medium (Can and  etal.,2007).

Aim of study

Since Ni and Cr are groups of elements which improve the soldering ability of dental alloys they are commonly added to them, at least in minimal amounts However very often the manufacturer does not state its presence .In addition, Ni and Cr are considered to be the greatest allergen. Moreover , Ni and Cr are cytotoxic and cancerogenic .The objective of this study was to investigate how different factors such as the solution type ( energy drinks )in which the alloy is submerged exposure time affect the amount of released Ni and Cr ions from above mentioned alloys .

Materials and Methods

Sample preparation:

Four specimens made from nickel – chromium ( Ni – Cr ) alloy [ Cr 49.0 , Ni 72.8 , Cu 12.3 , other 10.0, weight % ] were provided in the form of 10 mm diameter discs , 5 mm in thickness (Wataha and Lockwood,1998).Four samples of energy drinks (Tiger , power horse , Red bull , Jaguar ) used for each alloy. Ion release from the alloys was measured over the following time intervals : on the 0,1,24 hours and 7 days placed and incubated at room temperatures .

Atomic absorption spectrophotometer analysis :

Atomic absorption speotrophotometer ( AAS) (Shimadzu _ 660G Japan) was used to determine the release of elements from the alloys into energy drinks . Nickel (Ni) and chromium (Cr) were selected for analysis based on previous research which showed that they were released from dental casting alloy.  The Statistical Analysis System- SAS  was used to effect of difference factors in study parameters. The least significant test (LSD) at the comparative between means in this study (SAS,2004) .

Results :

The release amount of elements in energy drinks were determined to ng / ml = microgram / L = ppm . These data were obtained like this: ( the experimental result – the control result ).The result are illustrated in Tables 1 and 2 .

Table(1):Ni ion release from Ni-Cr alloy for each type of energy drinks

| days 7 | hr 24 | hr 1 | Control | residual Ni Type |
| --- | --- | --- | --- | --- |
| 0.027 | 0.056 | 0.016 | 0.053 | Tiger |
| 0.018 | 0.144 | 0.038 | 0.089 | Powerhouse |
| 0.085 | 0.140 | 0.144 | 0.120 | Redbull |
| 0.017 | 0.110 | 0.083 | 0.016 | Jaguar |

Table(2):Cr ion release from Ni-Cr alloy for each type of energy drinks

| days 7 | hr 24 | 1hr | Control | residual Cr Type |
| --- | --- | --- | --- | --- |
| 0.015 | 0.009 | 0.004 | 0.024 | Tiger |
| 0.004 | 0.021 | 0.017 | 0.011 | Powerhouse |
| 0.005 | 0.004 | 0.045 | 0.007 | Redbull |
| 0.025 | 0.005 | 0.006 | 0.015 | Jaguar |

The release of Ni and Cr ions were statistically significant (p<0.05) according to energy drinks , these results are illustrated in Tables 3 and 4

Table(3):ANOVA Test for Ni ion release from Ni-Cr alloy.

| Type | Time |  |  |  | LSD Value |
| --- | --- | --- | --- | --- | --- |
|  | Control | 1 hr | 24 hr | 7 days |  |
| Tiger | 0.053 ± 0.002 | 0.016 ± 0.00 | 0.056 ± 0.002 | 0.027 ± 0.003 | NS |
| Powerhouse | 0.089 ± 0.003 | 0.038 ± 0.002 | 0.144 ± 0.015 | 0.018 ± 0.002 | 0.016 * |
| Red bull | 0.120 ± 0.003 | 0.144 ± 0.015 | 0.140 ± 0.011 | 0.085 ± 0.002 | 0.026 * |
| Jaguar | 0.016 ± 0.00 | 0.083 ± 0.014 | 0.110 ± 0.020 | 0.017 ± 0.001 | 0.021 * |
| LSD Value | 0.017 * | 0.016 * | 0.017 * | 0.023 * | --- |

* (P<0.05) , NS: non-significant

Table( 4): ANOVA Test for Cr ion release from Ni-Cr alloy.

| Type | Time |  |  |  | LSD Value |
| --- | --- | --- | --- | --- | --- |
|  | Control | 1 hr | 24 hr | 7 days |  |
| Tiger | 0.024 ± 0.002 | 0.004 ± 0.00 | 0.009 ± 0.001 | 0.015 ± 0.002 | NS |
| Powerhouse | 0.011 ± 0.00 | 0.017 ± 0.002 | 0.021 ± 0.00 | 0.004 ± 0.00 | 0.002 * |
| Red bull | 0.007 ± 0.00 | 0.045 ± 0.002 | 0.004 ± 0.00 | 0.005 ± 0.00 | 0.002 * |
| Jaguar | 0.015 ± 0.003 | 0.006 ± 0.00 | 0.005 ± 0.00 | 0.025 ± 0.001 | NS |
| LSD Value | NS | NS | NS | NS | --- |

* (P<0.05), NS: non-significant.

Discussion

Dental alloys are subjected to a variety of chemical environment in the mouth. The dynamic natures of intraoral conditions cause corrosion. The release of an element from alloy depend on some factors such as the nature of element , alloy composition , multiple phases of alloy the metallurgical environment around these alloy and polished alloy . Therefore some of metal elements have an inherently higher tendency to be released from dental alloys . The biological liabilities may be related to the released elements . The release of elements from dental casting alloys has been investigated with many different material and methods by different researchers (Wataha and  etal.,1995 Brune,1986, Geis – Gerstorfer and  etal., 1991 Wataha and Lockwood,1998, Wataha and  etal.,1998).Certain environmental around the alloy affect release of elements . A reduction in PH increases elemental release from dental alloys . This effect is especially pronounced for Ni – based alloys (Wataha and Malcolm,1996 , Covington and  etal.,1985, Wataha and  etal.,1991). Although , for the Ni – based alloy , pH appeared to be the dominating factor and the composition of the solution is less important . Liability of Ni element from Ni – based alloys in acidified saliva was confirmed by Covington (Covington and  etal.,1985) . He showed that ; especially Ni tends to be released from these types of alloys in acidified saliva . (Wataha etal.,1998) in a various solution with PH ranging between 1 – 7 simulating intraoral dynamic conditions  , investigated the release of elements from Ni – based alloys in 30 minutes .The authors found that elemental release was increased in PH 1 – 4 . Wataha and Lockwood,1998  measured the release of elemental from dental alloys at monthly intervals for 10 months . The hypothesized that element release should decrease as afunction of time of exposure to the medium and that the cytotoxic effects of the alloys should also decrease . Also , they stated that the initial release rates were the highest (Wataha and  etal.,1999).

Our results revealed that Ni was more active than Cr . As expected , reduced PH dramatically increased Ni release from the Ni – based alloy in the present study . This result is essentially identical to trends seen in previous studies performed in a 72 hours period (Wataha and  etal.,1991 , Johansson and  etal.,1989),previous studies support the idea that composition of the alloy surface is critical to elemental release behavior for base – metal alloys (Bumgardner  and  Lucas,1993, Wataha and Malcolm,1996, Wataha and  etal.,2002).We expected that release of Cr would be minimal since chromium oxide layer formed corrosion . In fact , our findings confirmed this assumption . They stated that cell-culture medium was much more complex then biological medium , However , in our study the elemental release from dental casting alloy into energy drink medium was not affected as much as in artificial saliva . Our hypothesis was supported by the other studies (AL – Hiyasat and  etal.,2003 ,Wataha and  etal.,2001) .When the energy drink medium was compared to the artificial saliva , the data showed clearly that the release of Ni and Cr more lower in energy drink medium .

Conclusions

Great amount of Ni and Cr ions were released from the Ni-Ci alloy in all four energy drinks as early as the first day of the measurement .This exceeded the approved daily dietary intake of nickel . The amount of the released Ni ions increased gradually with great variability in all energy drinks . Therefore Ni –Cr alloy should be used exclusively for fabrication of   metal – ceramic appliances and should not be used for fabrication of veneer and telescopic crowns .

References

AL – Hiyasat AS , Darmani H , Bashabsheh OM . Cytotexicity of dental casting alloys after conditioning in distilled water . Int J Prosthodont . 2003 , 16 : 597 – 601 .

Amato D , Maravilla A , Garcia – Contreras F, Paniagua R . soft – drinks and health . Rev . Invest Clin . 1997 , 49 (5) : 387 – 395 .

Arnadottir IB , Saemundsson SR , Holbrook WP . Dental erosion in Icelandic Teenagers in relation to dietary and lifestyle factors . Acta Odontol Scand . 2003, 61 (1) : 25 – 28 .

Brune D . Metal release from dental biometerials. Biomaterials . 1986, 7: 163 – 175 .

Bumgardner JD , Lucas LC . Surface analysis of nickel – chromium dental alloys . Dent mater . 1993 , 9 : 252 – 259 .

Can G , Akpinar G , Aydin A . The Release of Elements from Dental casting alloy into cell – culture Medium and Artificial Saliva . Eur J Dent . 2007, 2: 86 – 90 .

Can G , Akpinar G , Can A . Effects of base – metal castings alloy cytoskeletal filaments in cultured human fibroblasts . Int J Prosthodont . 2004 , 17 : 45 – 51

Covington JS , Me Bridge MA , Slagle WF , Disney AL . Quantifications of nickel and beryllium leakage from base metal casting alloys . J Prosthet Dent. 1985 , 54 : 127 – 136 .

Gandara  BK ,Truclove EL .Diagnosis and management of dental erosion . J Cont Dent Prac . 1999 , 1 (1) : 1 – 17 .

Geis – Gerstorfer JG , Sauer KH , Passter K . Ion release for Ni – Cr – Mo and Co – Cr – Mo casting alloys . Int J Prosthodont . 1991 , 4:152 – 158 .

Hooper SM , Newcombe RG , Faller R, Eversole S, Addy M, West NX . The protective effects of toothpaste against erosion by orange juice : studies in situ and in vitro;J Dent , 2007 , 35 (6) : 476 – 481.

Johansson BI , Lemons JE , Hao SQ . Corrosion of dental copper , nickel and gold alloys in artificial saliva and saline solutions . dent Mater . 1989 ,5: 324 – 328.

Lussi A , Jaeggi T , Zero D . The role of diet in the aetiology of dental erosion . Caries Res . 2004 , 38 (suppl 1) : 34 – 44 .

Meurman JH , ten Cate JM . Pathogenesis and modifying factors of dental erosion . Eur J Oral Sci; 1996 , 104 (2) : 199-206 .

O'Brien M . children's dental health in the United kingdom 1993 . In : Report of dental survey , Office of Population Censuses and Surveys . London : Her Majesty's stationery Office ; 1994.

SAS. (2004). Statistical Analysis System, User's Guide. Statistical. Version 7th ed. SAS. Inst. Inc. Cary. N.C. USA.

Seow WK , Thong KM , Erosive effects of common beverages on extracted premolar teeth . Aust Dent J . 2005 , 50 (3) : 173 – 178 .

Shipley S , Taylor K , Mitchell W . Identifying causes of dental erosion . Gen Dent . 2005 , 53 (1) : 73 – 75 .

Stipetic J , Celebic A , Baucic I Rincic N , Catic A , Baucic M . The Release of Nickel Ions from three Different Dental Casting Alloys . Acta Stomat Croat . 2002 , 389 – 395 .

Tai y , De Long R, Good kind RJ, Douglas WH . Leaching of nickel , chromium and beryllium ions from base metal alloy in artificial oral environment . J Prosthet  Dent . 1992 , 68 : 692 – 697

Wataha JC. Biocompatibility of dental casting alloy : areview . J prosthet Dent .2000 , 83 : 223 – 234 .

Wataha JC , Craig RG , Hanks CT . The release of elements of dental casting alloys into cell  - culture medium . Dent Res . 1991 , 70 : 1014 – 1018 .

Wataha JC , Lockwood PE . Release of elements from dental casting alloys into cell – culture medium over 10 months . Dent Mater . 1998, 14 : 158 – 163 .

Wataha JC, Lockwood PE , khajotia SS , Turner R . Effect of PH on element release from dental casting alloys . J Prosthet Dent . 1998 , 8 : 691 – 698 .

Wataha JC , Lockwood PE , Nelson SK . Initial versus subsequent release of elements from dental casting alloys . J Oral Rehubil 1999 , 26 ; 798 – 803 .

Wataha JC , Lockwood PE , Noda M , Nelson SK , Mettenburg  DJ . Effect of tooth brushing on the toxicity of casting alloys . J Prosthet Dent . 2002, 87 : 94 – 98.

Wataha JC , Malcolm CT . Effect of alloy surface composition on release of elements from dental casting alloys . J Oral Rehabil . 1996 , 23 : 583 – 589 .

Wataha JC , Malcolm CT , Hanks CT . Correlation between cytotoxicity and the element release  by dental casting alloys . Int J Prosthodont . 1995 , 8 :9 – 14.

Wataha JC , Nelson SK , Lockwood PE . Elemental release from dental casting alloys into biological media with and without protein . Dent Mater . 2001 , 17 : 409 – 414 .

Zipkin I , McColure FJ . Salivary citrate and dental erosion . J Dent Res . 1949 , 28 (8) : 613 – 626    .