A Study for CNDO Efficiency for Band Structure Calculations of IV-Covalent Materials: (Sn, Ge, Si and C)

Z.Y.  Mijbil

Babylon University, College of Veterinary.

M.G. Merdan

Babylon University, College of Science, Department of Physics

Abstract

Lattice constant, cohesive energy, direct band gap and valence band width had been calculated for grey tin by using ( CNDO-LUC ) method, then we had been making a comparison with experimental and other workers results for ( C, Si, Ge and Sn ) with zinc-blende structure in order to study the efficiency of this method. The results had showed that this method is good for lattice constant and bad for other properties all at the same time.

الخلاصة

ثابت  الشبيكة، طاقة الربط، فجوة الطاقة المباشرة وعرض حزمة التكافؤ تم حسابها لمادة القصدير الرمادي بواسطة طريقة (CNDO-LUC )، كما تم مقارنة القيم مع النتائج العملية و النظرية لباحثين آخرين قاموا باستعمال نفس الطريقة و للمواد ( C، Si، Ge و Sn ) ذات التركيب الماسي و ذلك لمعرفة كفاءة هذه الطريقة. و أظهرت النتائج أنها جيدة في حساب ثابت الشبيكة إلا أنها فاشلة في حساب بقية الخواص كلها بنفس الوقت.

I. Introduction

The semiempirical methods gave us a privilege of no long time for getting results, because it had been adopted many approximations as compared with other ab-initio and numerical methods, according to that it is used in many fields ( Harker and Larkins 1979, Freund and Hohlneicher 1979, Schmid and Brodbek 1985, Vogl et al. 1983) and for along time even in the last years (Marshed 2006, Mijbil 2006, Hassan 2001), as well as papers about had been published (Thiel 2002). Nevertheless these approximations led to inaccurate data in some aspects which became a disadvantage ( Dorestt and White 2000), for this reason we made this research in order to measure the efficiency of CNDO (Complete Neglect of Differential Overlap) as one among  the primary semiempirical methods, that presented by ( Pople et al. 1965) in which he neglected  many electron-electron interactions and focused on both valence electrons and nuclei as a core of the atom ( with the other electrons) ( Pople and Beveridge 1970). Here LUC approximation ( Large Unit Cell) or ( Supercell ) ( Bredow 2000)  is used in order to minimize the size of BZ (Brillion Zone) and so to diminish the number of the special points in which the aspects of  the crystal such as band structure could be calculated ( Rogan and Lagos 2001,  Chadi and Cohen 1973).

We have firstly studied how CNDO method practically and mathematically work, and see how its parameter the orbital exponent ( ξ ), bonding parameter ( β ), s-shell electronegativity ( EES  ) and p-shell elecronegativity ( EEP ) could be changed and how this change may effect on the results, and secondly we have calculated the lattice constant, cohesive energy  valence band width and the direct band gap for the semimetal grey tin ( α-Sn) ( Myles et al. 2001, Cuenya et al. 2002) which has 50 electrons, exist at atmospheric pressure (Akdim et al. 2002, Mujica et al. 2003) and under 13oC with diamond structure ( Khan et al.1996, Cuenya et al. 2001), and compared our results with the experimental and other workers used the same method for the substance and other materials which are ( Sn, C, Si and Ge) of the same diamond structure.

II. Method

II.1. Mathematically

According to LCAO approximation ( Linear Combination of Atomic Orbitals) and LUC with eight atoms, and STO ( Slater Type Orbital ) for atomic orbitals of the form:

| Ψr,θ,ϕ=Nrn−1exp−ξrYθ,ϕ | (1) |
| --- | --- |

Where:

Ψ(r,θ,φ) is Slater type orbital. r,θ,φ are the polar spherical coordinates of the atom. N is the normalization constant. n* is the effective principal quantum number. Y(θ,φ) is the spherical harmonics ( Daudal et al. 2000).

According to that Fock-matrix element (Fss) and the total energy (E) can be calculated as ( Pople and Beveridge 1970 ):

| Fss=−EES+0.51−Pss−QAγAA+BAQBγAB | (2) |
| --- | --- |
| Fsp=βABSsp−0.5Pspγ | (3) |
| E=0.5spPspHsp−Fsp+A<BZAZBRAB−1 | (4) |

and the final result with LUC approach ( Harker and   Larkins 1979) is:

| Fss(0)=−EES+0.5γAAoo−BQB(0)vγABov+v≠oβABovSos,vp−0.5vPss(0)γAAovfx | (5) |
| --- | --- |
| Fsp(0)=vβABovSos,vp−0.5Pps(0)vγABovfx | (6) |
| E=0.5spPsp(0)Fsp(0)+Hsp(0)+0.5ABZAZBRAB−1 | (7) |

Where:

f(x) it is Szymanski enhancement function. o is a LUC. v is the other LUCs.

II.2. Practically

- We had used a computer program which is composed by the researcher [M. A. Abdulsattar ] to calculate the properties of  gery tin, and it was written with ( Fortran Power Station ) language and work on ( PC IV ).

- We had changed the four parameters of the CNDO method ξ, βAB, EES and EEP in arbitrary way until we get an amount of the lattice constant very near to the experimental value with the minimum value of the total energy of the crystal.

- Then we measure the values of the cohesive energy and all the energies of the electronic band.

- If the values of energies were in agreement with the experiment then we would stop and fix the parameters.

- If the values of the energies were bad we should change the parameters again until getting the closest values to the experiments.

The chart below shows the simple steps of CNDO method work practically, and parameters of our work and others for grey tin, silicon, diamond and germanium are listed in table (1)

We fix the parameters and the properties

Are the values near the experimental?

The calculation of the properties

Entering the parameters

Start

End

Figure (1); Shows the simple steps of CNDO method for bands calculations.

III. Results and Discussion

Our results and the others are illustrated in the tables (2, 3, 4 and 5), and it shows:

- Lattice constants for all were good with the experiments.

- All data are different from each other for the same matter.

- The values of diamond by (Abdulsattar 1997 and Al-Jelawy 2004) were generally bad, except for the lattice constant.

- Valence band widths amounts were good or approximate.

- When cohesive energy is close to the experiment the direct band gap will be far and vice verse, and all band gaps were approximate.

Point one:

Lattice constants were adjusted by the workers themselves through changing parameters, and they always try to put it in good agreement with the experiment, then they were had been measuring the rest of the properties. If  these data were bad, they would try to change the parameters again but on the basis of  adjusting the lattice constant (Abdulsattar 1997, Al-Hello 20004, Al-Jelawy,…).

Point two:

The choice of the parameters determines the values of the properties and as long as the parameters were different from each other even for slightly, then the results will be effected by that.

Point three:

The key clue of this method success is the good choice of the parameters, and according to point two, we have got that the bad results attributed to bad parameters (Harker and  Larkins 1979).

Point four:

The results of the valence band width are attributed to:

- It is calculated from symmetry points which came from LCAO, so good calculation will give good results (Ferhat et al. 1998).

- Here all workers including us had used minimal Slater orbital basis sets which deal with the valance orbitals (sp) and the inner shells, these sets give good description for valance band ( Chadi 1977).

- In CNDO the inner shells were neglected, from the other side this method focuses on valance orbitals by replacing empirical data like ξ in  (Pople and Beveridge 1970).

Point five:

Within CNDO-LUC method the variation of  βAB, EES and EEPdetemines the value of the cohesive energy ( Issa 2001) which entails a change in the direct band gap specially βAB which effected directly on the width between the bonding and the antibonding orbitals (Abdulsattar 1997), and the increasing of βAB, EES and EEP will increase the band gap and decrease the cohesive energy (Abdulsattar 1997 and Harker and  Larkins 1979), but there are additional reasons that effected on the direct band gap which are:

- No higher orbital above the valance orbitals had been taken, which increase the direct gap ( Chadi 1977).

- βAB and ξ had similar values for s-shell and p-shell.

- Neglecting of core state (i.e. neglecting its effect on the valence electrons.) (Abdulsattar 1997).

IV. Conclusions

- The random way of choosing the parameters had given random results.

- There is not a criterion in order to deal with this method’s inputs and outputs.

- It is failure method for calculating the energy bands all at the same time.

- It is unpractical method because if we want to calculate a particular property in slowly agreement with the experiment it will lead us for getting a deviation in a value of other property.

- It is inconvenient way for master degree thesis.

| Table (1); The values of CNDO’s parameters for α-Sn, Ge, Si and C. |  |  |  |  |
| --- | --- | --- | --- | --- |
| Grey tin |  |  |  |  |
| Parameter | Ref a | Present |  | Ref b |
| ξ ( eV ) | 2.05 | 1.9965 |  | 1.425 |
| -β ( eV ) | 5.35 | 5.3345 |  |  |
| -EES ( eV ) | 9.46 | 9.452 |  |  |
| -EEP ( eV ) | 4.69 | 5.632 |  |  |
| Germanium |  |  |  |  |
| Parameter | Ref a | Ref c |  | Ref b |
| ξ ( eV ) | 1.98 | 1.98 |  | 1.527 |
| -β ( eV ) | 5.35 | 5.3527 |  |  |
| -EES ( eV ) | 9.35 | 9.3571 |  |  |
| -EEP ( eV ) | 5.4 | 5.404 |  |  |
| Silicon |  |  |  |  |
| Parameter | Ref a | Ref d | Ref e | Ref b |
| ξ ( eV ) | 1.635 | 1.54 | 1.59 | 2.075 |
| -β ( eV ) | 5.45 | 6.4 | 6.2 | 13.065 |
| -EES ( eV ) | 7.25 | 6.3 | 7.25 | 10.033 |
| -EEP ( eV ) | 4.95 | 4.5 | 5 | 4.133 |
| Diamond |  |  |  |  |
| Parameter | Ref a | Ref d | Ref f | Ref b |
| ξ ( eV ) | 1.83 | 1.765 | 1.8203 | 1.652 |
| -β ( eV ) | 10 | 10.2 | 10.24 | 21 |
| -EES ( eV ) | 5.57 | 7 | 6.2205 | 14.051 |
| -EEP ( eV ) | 4.39 | 5.5 | 4.3521 | 5.572 |

a - ( Abdulsattar 1997).

b - ( Pople and Beveridge 1970).

c -  ( Baaee 2003 ).

d - ( Harker and Larkins 1979).

e - ( Al-Hello 2004).

f - ( Al-Jelawy 2004).

| Table (2); The lattice constant in (Ao) of grey tin in comparison with the others and the experimental results. |  |  |  |  |
| --- | --- | --- | --- | --- |
| Material | Theoretical |  |  | Experimental |
| C | 3.56 a | 3.5635 b | 3.56 d | 3.567 l |
| Si | 5.43 a | 5.4503 b |  | 5.431 f |
| Ge | 5.65 a | 5.65 c |  | 5.658 f |
| α-Sn | 6.64 a | 6.487 Present |  | 6.489 k |

| Table (3); The direct band gap in (eV) of grey tin in comparison with the others and the experimental results. |  |  |  |  |
| --- | --- | --- | --- | --- |
| Material | Theoretical |  |  | Experimental |
| C | 7.85 a | 9.4 b | 7.89 d | 6 g |
| Si | 4.82 a | 7 b |  | 3.44 j |
| Ge | 1.45 a | 1.42 c |  | 0.99 a |
| α-Sn | 0.979 a | 2.33 Present |  | -0.1 e |

| Table (4); The cohesive energy in (eV) of grey tin in comparison with the others and the experimental results. |  |  |  |  |
| --- | --- | --- | --- | --- |
| Material | Theoretical |  |  | Experimental |
| C | 18.99 a | 7.68 b | 19.2 d | 7.37 i |
| Si | 11.69 a | 4.71 b |  | 4.63 h |
| Ge | 10.59 a | 10.63 c |  | 3.85 h |
| α-Sn | 8.89 a | 8.96 Present |  | 3.14 e |

| Table (5); The valence band width in (eV) of grey tin in comparison with the others and the experimental results. |  |  |  |  |
| --- | --- | --- | --- | --- |
| Material | Theoretical |  |  | Experimental |
| C | 16.01 a | 22.4 b | 17.96 d | 24.2 g |
| Si | 10.08 a | 13.2 b |  | 12.4 j |
| Ge | 11.99 a | 11.97 c |  | 12.6 a |
| α-Sn | 11.85 a | 11.21 Present |  |  |

a- ( Abdulsattar 1997).

b- ( Harker and  Larkins 1979 ).

c-  ( Baaee 2003 ).

d- ( Al-Jelawy 2004).

e- ( Merdan 2005).

f- ( Wang and Ye 2002).

g- ( Calzaferri and Rytz 1996).

h- ( Lee et al. 1997).

i- ( Sekkal et al. 1998).

j - ( Al-Hello 2004).

k- ( Van Camp et al.1988).

l- ( Sun et al. 2001).

References

Abdulsattar, M.A., 1997, "Self Consistent Field Calculations Of Covalent Semiconductors", Ph.D. Thesis, University of Baghdad.

Akdim, B., Papaconsttantopoulos, D.A. and Mehl,  M.J., 2002,”Tight-Binding Description of the Electronic Structure and Total Energy of Tin”, Phil. Mag. B, Vol. 82 (1), pp. 47-61.

Al-Hello, M. M., 2004,” Study of the Effect of Pressure on the Properties of Si-Crystal Using Semiempirical Method”, M. Sc. thesis, University of Babylon.

Al-Jelawy, I.O. R., 2005,” Effect of Pressure and Temperature on Some Properties of Diamond Crystal Using Hartree-Fock Method”, M.Sc. thesis, University of Babylon.

Baaee, B. S. M., 2003, “ Theoretical Process to Study the Band Structure of  Germanium Crystal by Use the Intermediate Neglect of Differential Overlap Method.”, M.Sc. thesis, University of Babylon.

Bredow, T., Evarestov, R.A. and Jug, K., 2000, “Implementation of the Cyclic Cluster Model in Hartree-Fock LCAO Calculation of Crystalline Systems.”, Phys. Stat. Sol.,  Vol. 222(b), pp. 495-514.

Calzaferri, G. and Rytz, R., 1996, “ The Band Structure of Diamond.”, J. Phys. Chem. 100, pp. 11122-11124.

Chadi, D.J. and Cohen, M. L., 1973,” Special Points in the Brillion Zone”, Phys. Rev. B, Vol. 8(12), pp. 5747-5753.

Chadi, D.J., 1977, “ Localized-Orbital Description of Wave Function and Energy Bands in Semiconductors.”, Phys. Rev. B, Vol. 16 (8), pp. 3572-3578.

Cuenya, B.R., Doi, M. and Keune, W., 2002, “Epitaxial Growth and Interfacial Structure of Sn on Si(111)-(7 * 7)”, Surf. Sci. 506, pp. 33–46.

Cuenya, B. R., Keune, W., Sturhahn, W., Toellner, T. S. and Hu, M. Y., 2001, “Structure and Vibrational Dynamics of Interfacial Sn Layers in Sn/Si Multilayers”, Phys. Rev. B, Vol. 64, pp 235321/1-12.

Daudal, R., Leroy, G., Peeters, D. and Sana, M., 1983, " Quantum Chemistry", John Wiley and Sons.

Dorestt, H. and White, A., 2000, "Overview of Molecular Modeling and Ab initio Molecular Orbital Methods Suitable for Use with Energetic Materials", Defence Science and Technology Organization.

Ferhat, M., Bouhafs, B., Zaoui, A. and Aourag, H., 1998, “ First-Principles Study of Structural and Electronic Properties of BSb.”, J. Phys.: Cond. Matt. Vol. 10. pp. 7995-8006.

Freund, H. and Hohlneicher, G., 1979,” Calculation of Transition Metal Compounds Using an Extension of the CNDO Formalism”, Theor. Chim. Acta (Berl.) 51, pp. 145-162.

Harker, A.H. and  Larkins, F.P., 1979,” A Large Unit Cell Semiempirical Molecular Orbital Approach to the Properties of Solids II. Covalent Materials: Diamond and Silicon”, J. Phys. C: Solid State Physics, Vol. 12, pp. 2497-2507.

Harker, A.H. and  Larkins, F.P., 1979,”A Large Unit Cell Semiempirical Molecular Orbital Approach to the Properties of Solids I. General Theory”, J. Phys. C: Solid State Physics, Vol. 12, pp. 2487-2495.

Hassan, I.Z. 2001,"Semiempirical Self-Consistent Field Calculations of III-V Zinc-Blende Semiconductors", Ph. D. Thesis, University of Al-Nahrain.

Khan, A.T., Berger, P.R., Guarin, F.J. and Iyer, S.S., 1996, “Band-Edge  Photoluminescence from Pseudomorphic Si0.96Sn0.04 Alloy” , Appl. Phys. Lett., Vol. 68 (22), pp. 3105-3107.

Kittel, C.  1996, "Introduction to Solid State Physics", 7th Edition, John Wiley and Sons.

Lee, S. H., Kang, J. H. and Kang, M. H., 1997, “Structural Properties of Semiconductors in the Generalized Gradient Appproximation.”, J. Kor. Phys. Soc., Vol. 31(3), pp. 811-814.

Marshed, H. R. J., 2006,” Band Structure and Some Properties of Aluminum Phosphide Crystal Using Hartree-Fock Method.”, M.Sc. thesis, University of Babylon.

Merdan, M.G., 2005, “ Self-Consistent Field Calculations for the Effect of Pressure and Temperature on Some Properties of Grey Tin Crystal.), M.Sc. thesis, University of Babylon.

Mijbil, Z.Y., 2006,” The Effect of Pressure and Temperature on Some Properties of Cubic Boron Nitride Crystal. ”, M.Sc. thesis, University of Babylon.

Mujica, A., Rubio, A., Munoz, A.,  and Need, R.J., 2003,“High Pressure Phaces of Group-IV, III-V, and II-VI Compounds”,  Rev. Mod. Phys., Vol. 75,  pp. 863-907.

Myles, C.W., Dong, J. and Sankey, O.F., 2001, “Structural and Electronic Properties of Tin Clathrate Materials”, Phys. Rev. B, Vol. 64,  pp. 165202/1-11.

Pople, J.A. and Beveridge, D.L., 1970,"Approximate Molecular Orbital Theory", McGraw-Hill.

Pople, J.A., Santry, D.P. and Segal, G.A., 1965, “Approximate Self-Consistent Molecular Orbital Theory. I. Invariant Procedures.” The J. of Chem. Phys., Vol. 43 (10), pp. S129-S135.

Rogan, J. and Lagos, M., 2001, “ Non-Recursive Chadi-Cohen Integration over the Brillion Zone of the Cubic Crystals.”, Phil. Mag. B, Vol. 81(6), pp. 551-559.

Schmid, E. and Brodbe, E.,1985, “Raman Intensity Calculations With The Cndo Method, Part III: N,N-Dimethylamide - Water Complexes”, Can. J. Chem., Vol. 63, pp. 1365-1371.

Sekkal, W., Bouhafs, B., Aourag, A. and Certier, M., 1998, J. Phys.: Cond. Matt., Vol. 10, pp. 4975-4984.

Sun, H., Jhi, S. H., Roundy, D., Cohen, M. L. and Louie, S. G., 2001, “ Structural Forms of Cubic BC2N.”, Phys. Rev. B, Vol. 64, pp. 094108/1-6.

Thiel, W., 2000, “Semiempirical Methods”, NIC Series V3, pp. 261.

Van Camp, P. E., Van Doren, V. E. and Devreese, J. T., 1988, “ Ground-State and Electronic Properties of  Covalent Solids.” Phys. Rev., Vol. 38 (17), pp. 12675-12678.

Vogl, P., Hjalmarsons, H. P. and Dow, J. d., 1983, “A Semi-Empirical Tight-Binding Theory of the Electronic  Structure Of Semiconductors”, J. Phys. Chom. Solids, Vol. 44 (5), pp 365-378.

Wang, S. Q. and Ye, H. Q., 2002, “ Plane-Wave Pseudopotential Study on Mechanical and Electronic Properties for IV and III-V Crystalline Phases with Zinc-Blende Structure.” Phys. Rev. B, Vol. 66, pp. 235111/1-7.