Preparation of New Catalyst CoO -V2O5: Characterization , Physical properties and studying the Photochemical activity.

A. Jassim         H. Idrees       A. Al-Fatlawy

College of Sciences, Babylon University

Abstract

Cobalt oxide, Vanadium oxide and their mixture with different ratio (0.5: 2.0 , 1.0 : 2.0 , 1.5 : 2.0 , 2.0 : 2.0 , 2.0 :1.5 , 2.0 :1.0 , 2.0 : 0.5 ) were prepared from its salts ,nitrate and sulphate respectively.

The prepared catalysts were characterized by X-Ray Diffraction and IR- spectroscopy. The physical properties also studied such as: porosity, pores size, particle size, density and electrical conductivity.                             The photochemical activity of prepared catalysts were studied by oxidation of 1- octanol (6.32mole/ liter) to 1- octanal using visible light from external source through a side window of quartze inside  a pyrex reaction of 25 cm3 at 298 K. The conc. of reactants and products were detected and determined by UV-Visible. The mechanisms of 1- octanol oxidation by using new catalysts and visible light were suggested.

الخلاصة

تم تحضير اوكسيد الكوبلت , اوكسيد الفيناديوم  ومزيجهما بنسب مختلفة2.0 :1.5, 2.0 :1.0 , 2.0 : 0.5 )   0.5 : 2.0 , 1.0 : 2.0 , 1.5 : 2.0 , 2.0 : 2.0 ,) من املاحهما , نترات و كبريتات على التوالي .

شخصت العوامل المساعدة المحضرة باستخدام مطيافية حيود الاشعة السينية XRD والاشعة تحت المراء IR. درست الخواص الفيزيائية للعوامل المساعدة : المسامية ,حجم المسامة , المساحة السطحية , الكثافة والتوصيلية الكهربائية.

كذلك تم دراسة الفعالية الضوئية للعوامل المحضرة وذلك بإجراء تفاعلات   الاكسيدة الضؤية الى 1- اوكتانول وذلك بتشعيع المحاليل العالقة في خلية ضوئية سعة 25 سم3 من 1- اوكتانول  6.32 ) مول / لتر )  باستخدام الضوء المرئي الصادر من مصباح هالوجيني  محور  من خلال  نافذه من الكوارتز قطرها  2 سم  ومقارنتها مع  فعالية اوكسيد الكوبلت و اوكسيد الفيناديوم  المحضر ايضا.

تم كشف وقياس تراكيز المواد المتفاعلة و الناتجة باستخدام مطيافية الاشعة المرئية و الفوق البنفسجية وتم اقتراح ميكانيكية الاكسدة الضوئية لل-1اوكتانول باستخدام العامل المساعد V2O5 - CoO.

Introduction

When  semiconductors  were  irradiated  with light  whose  energy  is  greater than  its band gap at room temperature in O2 produced oxidative properties toward inorganic and organic compound (Formenti et al., 1973; Boonstra and Matsaers1975; Djeghri et al., 1974, Bickley et al., 1973 and Cundall et al., 1976) as in Figure 1:

Figure 1: Direct excitation of semiconductors oxide.

The photocatalytic activity of mixed oxide has been shown to be more active in the rate of degradation of an azo-dye using SnO2/TiO2 coupled semiconductors(Vinodgopal and Kamat 1995) .CHCl3 oxidation  using  of  Fe  and  Ti(Choi et al1994). Zhang et al 1998 deduced  the  photoinduced   interfacial charge transfer mechanism of TiO2/FeO3 which showed modified photovoltaic response due to cooperative effect of the hetrojunction TiO2/FeO3 interface as shown in Figure 2:

CB

TiO2

VB

VB

SnO2

CB

e¯

OH¯

OH∙

hν

.

Figure 2 :Charge separation in coupled semiconductors.

The present study deals with the preparation of new catalyst composed of  two metal oxides ( CoO - V2O5 ): Characterization, Physical properties and studying the photochemical activity by using these catalysts in photooxidation reaction of 1-octanol with visible light at  298 K.                                         .

Experimental

A- Chemicals:

1- 1- Octanol : It is supplied by Merch, with purity 99.5%.

2- 1- Octanal: It is supplied by Merch, with purity 99.5%.

3-Cobalt nitrate: It is supplied by Merch, with purity 99%

4-Vanadium sulphate:It is supplied by Aldrich with purity 99%

5-Sodium carbonate: It is supplied by  Chem: Pure Scherman Chemical L.T.D.

B-Apparatus:

1- XR-Diffraction: Type 1410120, Philips.

2- F.T.I.R. Spectra 84005: Founier – Trasform , Schemadzn.

3- UV. Visible Spectrophotometer:U.V.-1650 PC, Schemadzn.

4-Atomic Absorption spectrophotometer: Corning Flame Photometer .LtD, Halstead            England.

5- pH-meter: Multi 740, Inolab, WTW Terminal.

6- Resistance meter: hp3468A, Mutimeter, Hewlette, Packard, U.S.A.

7-Valcanization oven: Muffle furnace size two ,Gallenkamp, England.

8-Oven:Oven BS size two , Gallenkamp, England.

C-Preparation of catalysts:

Cobalt oxide ,Vanadium oxide and their mixture with different ratio (0.5 : 2.0 , 1.0 :  2.0 , 1.5 : 2.0 , 2.0 : 2.0 , 2.0 :1.5 , 2.0 :1.0 , 2.0 : 0.5 )  were prepared by co-                   precipitation of metals carbonate from the solution of nitrate and sulphate of both           metals respectively, by adding 1.0 molar of sodium carbonate  with continuous              stirring for 2 hours to change the pH of the solution from 2.9 to 8.5 for complete             precipitation of metals carbonate at 333K.                                     .                                       The precipitation were separated by filtration and washed with D.W. to reduce the      sodium concentration less than 100 ppm. Which determined by atomic absorption. The precipitation was leave 16 hours at 373 K for drying. The precipitation grinded and forming tablets 4 x 10 mm. by using a pressure of 3 tons from a piston and                 cylinder manufactured for this purpose. The  porosity,  pore  size  and  density were determined  by  liquid  impregnation (Church and Joshi191 , Bowker1998).                 .

D-Methods:

Photooxidation  of' 1 – octanol  was  carried  out  in  Pyrex static reactor with quartz

window to received the irradiation generated from lamp (400-700) nm. In all experiments  25  cm3 of mixture ( 0. 20  mol. = 8.0  mol. / lit ) 1- octanol with  CoO, V2O5 or  mixed oxides  at  298  K. The solution was suspended by a magnetic stirrer as in Figure 3.                                               .

Figure 3 : Photooxidation  cell.

Periodically 3.0 cm3 samples of reaction mixture were with drown by pipet and centrifuge to separate solid catalysts. The supernatant liquid analyzed for reaction using uv-visible spectrophotometer                           .

E- Analysis of reaction products                                            :                                                Uv-visible spectrophotometeric methods were used to determine the concentration of     aldehyde produced from the photocatalytic oxidation of 1-octanol as follow:               1- This method was used by several workers(Hussein1984), and is based on the formation of 2 , 4 - dinitrophenylhydrozone, followed by the addition of alcoholic KOH to produce a wine colour which could then be spectophotometrically measured. The absorbance was directly proportional to the amount of reaction products,whose concentration was determined from a calibration curve.The calibration curve was obtained by using standard aldehyde solution (aldehyde  + cohol) in place of reaction mixture. The calibration consisted of absorbance at             λmax. against of carbonyl compound (mole/liter) as in Figure 4 – a .

2-The uv-visible spectrophotometric method, also used directly for plotting  other         calibration curve using  the above  standard  aldehyde  solution  to  determine  the          absorbance  of  aldehyde at λmax. 298nm. as in Figure 4 – b which also directly

Absorbance

proportional to the amount of reaction products.                         .

Conc. of 1-octanal mol./lit. x 103

aa

b

Calibration curve Figure 4:

a-Using method 1          b- Using method 2

Result and Discussion

Characterization of new catalyst CoO -V2O5:

1-Specroscopical studies:

A-X-ray diffraction:

The X-ray diffraction is an essential tool for the rapid identification and quantification of mineral, compound and other crystalline phase. Table 1 shows the values of 2θ (strongest 3 peaks) for pure V2O5 , pure CoO and the prepared new catalysts V2O5-CoO .

Table 1: 2θ for standard V2O5 standard CoO and CoO - V2O5 in the catalyst.

| 2θ |  |  | Metals oxide |
| --- | --- | --- | --- |
| 45.455 | 44.381 | 44.837 | Pure V2O5 |
| 29.379 | 31.283 | 36.868 | Pure CoO |
| 29.444 | 29.743 | 28.141 | New catalysts CoO - V2O5 |

So  when  these values of 2θ of  the  new  catalyst CoO - V2O5 compared with 2θ of each standard metals oxide can see the deviation in intensity and the position of 2θ      .    These deviations may due to the interaction between pure metals oxide which leads to change in crystals lattice of each oxide as in figure 4.

Figure 4: X-ray diffraction spectrum:

1 - V2O5         2 - CoO      3 - CoO - V2O5

B-IR Spectroscopy:

Table  2 shows that the λmax. of pure V2O5 , pure CoO and λmax. for the new prepared catalysts CoO - V2O5 .

Table 2: λmax. of the pure catalysts and the new prepared catalysts

| λmax. |  |  |  |  | Metals oxide |
| --- | --- | --- | --- | --- | --- |
| 1139.9 | 941.29 | 815.92 | 696.33 | 559.38 | Pure V2O5 |
|  |  | 1373.36 | 663.53 | 572.88 | Pure CoO |
| 1139.97 | 941.29 | 815.92 | 696.33 | 559.38 | New catalysts CoO - V2O5 |

The  above  table  shows  new  λmax.  with  high  intensity  which  return  to the new bonded between crystal lattice of both oxide as in figure 5:

Figure 5: IR-Spectroscopy of:

1 - V2O5          2 - CoO       3 - CoO - V2O5

2-Physicl properties:

A-Porosity:

The porosity defined as the amount of small spaces or voids with in a solid material(14). The Figure 6-a show that the porosity of naked CoO (fixed weight 2.0 grams),  was increased remarkably after the addition successive weight of V2O5. Also the porosity of naked V2O5 (fixed weight 2.0 grams), was increased after the addition successive weight of CoO as in Figure 6-b.                               .

a

b

a

Figure 6 :The effect of metal oxide (grams) on the porosity

a - V2O5 on CoO        b - CoO on V2O5

The  above  Figure  shows  that  the  maximum  porosity  of  the  mixed  catalyst occur at, by mixing equal weight of both metal oxides (2.0 grams of each one). This might be explain that the grains of both metal oxides that were not compacted together completely. The increases of porous in material can absorb much fluid.                                                                                                                                                 B-Pore size:        The pores size defined as the size of the opening in the sample. It is usually stated in nanometers (ηm) and micrometers (μm) and refers to the diameter of particles(15). Figure 7-a shows that the pores size of naked CoO (fixed weight 2.0 grams), was increased remarkably after the addition successive weight of V2O5. Also the pores size of naked V2O5 (fixed weight 2.0 grams), was increased after the addition successive weight of CoO as in Figure 7-b.                                     .

b

a

Figure 7 : The effect of metal oxide (grams) on the pores size

a - V2O5 on CoO       b - CoO on V2O5

The above Figure shows that the maximum pores size of the mixed catalyst occur by mixing equal weights of both  catalyst (2.0 grams of each one), which may be due to forming spaces  between grains, that increase the ability of the analyte molecule to penetrate inside the  particle and interact with its inner surface and may gave a high activity of the catalysts.                                     .                                                                 C-Density:  :                                                                                                                            It is a physical property of matter, which equal to the dry mass MD of the sample divided by the total volume V of the sample. The sample must be dried long enough to remove any moisture from the voids. The relationship between density and porosity is in direct proportionality (16), that the higher the density, the lower will be the porosity of because the over-lying increase the density , which in turn decrease the amount of pore space ( porosity) of the rock through processes such as compaction.                                     The Figure 8-a  shows  that  the density of naked CoO (fixed weight 2.0 grams), decrease with addition of successive weight of V2O5. Also the density of naked V2O5 (fixed weight 2.0 grams), was decreased after the addition successive weight of CoO as in Figure 8-b.

b

a

Figure 8 : The effect of metal oxide (grams) on the density

a- V2O5 on CoO       b- CoO on V2O5

The above Figure shows a decrease in the density of both metal oxides, this might be explain that the grains of both metal oxides that were not compacted together completely. The increases of porous in material cause increase in the volume of the sample for a constant weight, which leads to decrease of density.                                     D-Electrical conductivity:                           :

The ability  of materials to conduct an electric current when an electrical potential difference is placed a cross a conductor, its movable charges flow, giving rise to an electric current (17). Also the conductivity defined as the ratio of the current density J to the electric field strength Е. Its unite of siemens per meter (s.m-1).                                                                              σ  =  J / E

Figure 9 - a shows that the electrical conductivity of naked CoO (fixed weight 2.0 grams), was increased remarkably after the addition successive weight of V2O5. Also the electrical conductivity of naked V2O5 (fixed weight 2.0 grams), was increased after the addition successive weight of CoO as in Figure 9-b.           .

b

a

.

Figure 9  The effect of metal oxide (grams) on the conductivity

a- V2O5 on CoO         b - CoO on V2O5

The above Figure show that the maximum electrical conductivity of the mixed catalyst occur  by mixing equal weight of both metal oxides (2.0 grams of each one).  This might be explain that the degree of doping in solid state semiconductors make a large difference in conductivity, more doping leads to higher conductivity.

3-Photochemical activity

A-Preliminary treatments: Several optimization experiments were  carried out to determine  the conditions  necessary for  photo-lytic oxidation of 1-octanol  to 1- octanal by using  individual metal oxide and the preparation of mixed catalysts  with visible light for 5 hr.s irradiation for each experiment at 298 K. The results as in Table3:

Table  3 : The effect of different conditions on photocatalytic oxidation of 1-octanol at 298 K   .

| Exp no. | Hydro-carbons | Experiments Conditions | Reaction Products |
| --- | --- | --- | --- |
| 123456 7 8 9 10 11 12 13 14 15 | 1-octanol 1-octanol 1-octanol 1-octanol 1-octanol 1-octanol 1-octanol 1-octanol 1-octanol 1-octanol 1-octanol 1-octanol 1-octanol 1-octanol 1-octanol | 1-octanol only 1-octanol + air 1-octanol + light 1-octanol + air + light 1-octanol + CoO 1-octanol + CoO + air 1-octanol + CoO + light 1-octanol + V2O5 1-octano l + V2O5 + air 1-octanol + V2O5 + light 1-octanol + mixed catalyst ( CoO - V2O5 ) + air 1-octanol + mixed catalyst ( CoO - V2O5 ) + light 1-octanol + mixed catalyst ( CoO - V2O5 ) + air + light 1-octanol + mixed catalyst ( CoO - V2O5 ) + N2 + light 1-octanol + mixed catalyst ( CoO - V2O5 ) + H2 + light | No Products No Products No Products No Products No Products No Products No Products No Products No Products No Products No Products No Products See significant product (Uv-visible spectroscopic characterization) No Products No Products |

The prepared mixed catalysts were improved the photooxidation of 1-octanol to 1-octanal as in experiment number 13.

The activity of mixed catalysts depended on the ability of each metal oxide to absorbed the suitable λmax.and injected its photoelectrons to the conduction band of the other metal oxide as in the Figure 2. The strong coupling of both catalysts to each other is very essential for this process in presence of air (O2) and visible light .                              The products of all experiments in above table were analyzed characterized by the following steppes.                      :                                                                                           1-The reaction of all products individually with alkaline potassium 2,4-Dinitrophenylhydrazine give negative reaction, while the products of experiment 13 give positive reaction (pink colour).                                              .                                        2-The products of all experiments was characterized and analyzed spectroscopically using Uv-visible spectra and give negative detection ,while the products of experiment 13 give positive detection for carbonyl groups such as aldehyde groups  in λmax. 293 nm. as in Figure 10. This gives important indication that the air (O2), mixed catalysts and visible light are essential conditions to the photocatalytic reaction.                      .

Fgure10:Uv-visible spectra  of the irradiated solution of experiment 13.

B-The effect of metal oxide weight (grams) in the mixed catalyst activity on the    photocatalytic oxidation of 1-octanol:

In order to study the effect of naked CoO ,V2O5 and the prepared catalyst CoO -V2O5 on the photocatalytic oxidation of 1-octanol as a model for primary alcohol. Several experiments have been carried out to find the photooxidation processes.                              For this purpose, different weight of CoO (0.5, 1.0, 1.5 and 2.0) grams were mixed individually with fixed weight of V2O5 (2.0grams). Also different weight of V2O5 (0.5, 1.0, 1.5 and 2.0) grams individually were mixed with fixed weight of CoO (2.0grams).       In all experiment used  4.2 grams of each prepared mixed catalyst were used, while the other conditions such as: particles size , flow rate of air and temperature were kept constant. It seem that the mixed catalysts prepared with equal weight of both metals oxide (2.0) grams give high efficiency in photocatalytic oxidation of 1-octanol to aldehyde (absorbance) as in Figure 11:                                  :

Conc. of 1-octanal x 10+3

V2O5  on CoO and CoO on V2O5 (grams)

a

b

Figure 11: The effect of metal oxide (grams) on photocatalytic oxidation of 1-octanol.

a- V2O5 on CoO         b - CoO on V2O5

This might be explained by that, each particles of CoO aggregate or compacted with a particles of V2O5 and formed active couple particles of the prepared catalysts , which provides the highest efficiency in absorption of light.                                                   .

C- The effect of prepared catalysts CoO - V2O5 mass on photooxidation of 1-octanol at 298K.

To find the optimum quantity of catalysts (CoO-V2O5) as the photocatalyst , there are several experiments using different weight of the catalysts in range between 0.1- 6.4 grams /liter under similar condition (rate flow of air, temperature and 5.0 hours  of visible light irradiation).                    .                                                                                    The results illustrated in Figure 12, show that the absorbance of carbonyl group (aldehyde) as a product of 1-octanol oxidation increases linearly with the weight of the catalysts up to 4.0 grams/liter.                                                                                           .

Conc. of 1-octanal x 10+3

Figure 12: The effect of catalyst ( CoO-V2O5 ) concentration on photocatalytic

oxidation of 1-octanol at 298 K.

Above this concentration of the catalysts the rate of conversion of 1-octanol reaches a plateau behavior. This might be explained that the light could penetrate through the solution in lower catalyst concentration, but at higher concentration the layers near to the light source will strongly absorb light (Pichat et al1981, Naman et al 1994). This will prevent light from reaching other successive layers in the reaction cell and this of course, will decrease the extent of excitation of the catalysts.                                       .

Proposed reaction mechanism

According to  Figure 2 , the radical reactions was suggested during the present photocatalytic  reaction :

The metal oxide ( CoO or V2O5 ) upon irradiation absorbed  visible light ( λmax.  ) and generate electrons and holes.

CoO….V2O5        visible light       ( e +h ) CoO….V2O5

If  the exited  was CoO , then injected photoelectron in conduction band of V2O5  as in equation:

( e + h ) CoO….V2O5            ( h VB ) CoO….V2O5( e cb )

The valence band photo generated holes in CoO are free to react with (OH‾ ) adsorbed on the surface to create  hydroxyl  radical (OH• ). The V2O5 conduction band electrons (GAINED) react with electron acceptors are oxygen creating oxygen radicals (O•2, O• ). These  radicals (O•2 ,O• and OH• ) present  extremely   strong  oxidizing  properties are able to abstract in initial step a hydrogen atom from  carbon of hydroxyl group.

O2  +  CoO….V2O5( e cb ) → CoO….V2O5 _ O•2

10

CoO….V2O5 – O•2+ C7 H15CH2 OH  →    CoO….V2O5 – O2H + C7H15C• HOH

The formation 1- octanal  from C7H15C • HOH could then occur in the following ways;

1 -  C7 H15C• HOH    +     HO•2                    C7 H15CHO    +  H2O2

2  -   C7 H15C• HOH   +   O•H                        C7 H15CHO   +  H2O

3 -  C7 H15C• HOH  + C7 H15C•HOH               C7 H15CHO   +   C7 H15CH2OH

Reference

Bickley, R.J.; Munuera,F. and. Stone F.S.; Photoadsorption and Photocatalysis at rutile  surface 11. photocatalytic oxidation of isopropanol, J. Catal. 31 (1973) 398   .

Boonstra, A. H. and Matsaers, C.A.H.A.; J. Phy. Chem.; 79 (1975).

Bowker, M.; (1998). ''The Basic and Heterogeneous Catalusis'', Series Sponser, Published   in   United State by Oxford University press. Inc. New York, 533.

Choi, W.; Termin, A. and Hoffmann, M.R.; J. Phy. Chem., 98 (1994) 13669   .

Church,J. M.  and Joshi , H.K.; Ind. Eng. Chem., 43, (No.8), 1804, (1951).

Conductivity from en-wikipedia.org/wiki/electrical conductivity.

Cundall,R.B.; Rudham,R. and. Salim, M.S.; J. C. S. Farady Trans.; 172 (1976) .

Density from Wiki Answer, com/ How-doses-density relate-to-porosity.

Djeghri, N.; Forment, M.; Juillet,F and Teichner,S.J.;Farady Disc., Chem. Soc.; 58 (1974)  185.

Formenti, M.; Juillet, F.; Meriaudau, P.; and Teichner,S.J.; Heterogeneous photocatalysis  for partial oxidation of paraffins, Chem. Technol.  1 (1971)680.

Hussein, F.H.;Photocatalytic dehydrogenation of liquid alcohols by platinized anatase and other catalysts; Ph.D. Thesis submitted to the Nottingham University ,U.K., 1984.

Naman,S. A.; Hussein, F.H. and Abdulsahib, A.; Photocatalytic of heavy petroleum  molecules using titanium dioxide and zeolite; J. Coll. Edu. For Women Univ.,  Baghdad, 5 ,69 (1994).

Pichat,P.; Hermman,J.M.; Courbon,H.; Disder,J. and Mozzanega, M. N.;Photocatalytic oxidation of various compounds over TiO2 and other semiconductor oxides;  mechanistic cosideration; Candian. J. Chem. Eng., 60 (1981) 27.

Pore-sizedistribution: Definition from answers.com. www.answers.com/topic/pore-   size-distribution.

Porosity from Wikipedia, the free encyclopedia :en. Wikipedia.org/ wiki/porosity  .

Vinodgopal, K. and Kamat, P.V.; Enhanced rate of photocatalytic degradation of an azo         dye using SnO2/TiO2 coupled semiconductor thin films; J. Am. Chem. Soc.; 2(1995) 9841  .

Zhang, X.; Cao, Y.; Kan, S.; Chen, Y.; Tung , J.; Jin,H.; Bai, Y.; Xias, L.; Li, T.; and                   Li,B.;  Thin Solid Films,327 , 329 (1998) 568.