Some volumetric properties of aqueous solution of Polyvinyl alcohol over temperature range 298.15-328.15K.

Ahlam Mohammed Farhan

College of Science for Women University of Baghdad

Eman Talib Kareem

College of Science University of Karbala

Ahmed Najem Abd

College of Veterinary medicine , University of Diyala

Abstract

The densities of aqueous solution of polyvinyl alcohol with molecular weight (125kg.mol-1) have been determined over temperature range298.15-328.15K.From these data, the volumes for the binary mixtures studied here were calculated .The volumes have been found linearly dependent on the solute molality (PVA), from this dependence , the partial molar volumes at infinite dilution (V2,0) were determined and it was found that the (V2,0) concentration independent and slightly increase with increasing temperature .The thermal expansion coefficient (α1,2)of aqueous solution of (PVA) at 298.15K  was calculated and it was found that the values of  (α1,2)were higher than the value (α1∘) of pure water .

الخلاصة

تم في هذه الدراسة قياس الكثافة للمحلول المائي لبوليمر الكحول الفينايلي ذو الوزن الجزيئي   (125kg.mol-1)  في مدى من درجات الحرارة 298.15-328.15 كلفن . ومن هذه القيم تم حساب الحجوم لهذه المخاليط ثنائية المكون ووجد ان الحجوم تعتمد خطياً على مولالية المذاب (( PVA  ومن هذه الاعتمادية تم حساب الحجم المولاري الجزئي المحدد عند التخفيف الى ما لانهاية )V2,0)  ولوحظ ان هذا الحجم لا يعتمد على تغير التركيز لكنة يزداد قليلاً بزيادة درجة الحرارة. تم حساب معامل التمدد الحراري (α1,2) في درجة حرارة 298.15 كلفن ولوحظ ان قيمة)  α1,2 ) للمحلول المائي لبوليمر الكحول الفينايلي هي اكبر من قيمة (α1∘)  للماء النقي .

## Introduction

The calculation of physical properties using statistical theories is still not yet possible for complicated molecules such as long chain molecules, because of the range of different conformations, which can occur and the effect of these various structures on the intermolecular interactions (Adam ,2004) . Due to intermolecular hydrogen bonds molecular self-organization is one of the most important phenomenon, which determine the structure and properties of numerous liquids (Douheret et al. , 1997) . The physical properties of these liquids and their solutions differ essentially from those of non-associated ones.

In recent years, interest lies in exploring te extent to which analysis of the composition-dependence of the thermodynamic properties of non-ionic amphiphilic-water system can help us to understand the degree and nature of their self-aggregation (Czechowski and Jadzyn ,2003)  . Volumetric properties of binary liquid mixtures have been extensively studied, as the can contribute to clarification of the various intermolecular interactions existing between the different species found in solution. In particular much effort has gone into the determination of partial molar volumes at infinite dilution where only solvent-solvent and solute-solvent interactions are present (Barbosa et al. , 2001) . Poly (vinyl alcohol) (PVA; -(CH2 –CHOH)n-)is a polymer which is soluble in water to a large degree but considerably less so in most organic solvents. Many of its applications are determined by its hydrophilicity (researches have ,for example ,worried about the water content of  PVA films  as early as 1946 (Creutz and Wilson ,1946)  . Among them are the use as hydrogel former and as material for separation membranes where research is still very active (Muller-Plathe,1998) . It is often used in pervaporation systems for the removal of water (minority component) from liquid mixtures.More recently,polymerelectrolytes such as aqueous PVA solutions attract attention in physical and biophysical chemistry (Norio et al. , 1996, Muller-Plathe,1997 , Cheng et al., 1998, Akihiko et al. , 1998, Kazuki et al., 1999, and Rongshi et al.,1999  ) .

Experimental

(a) Materials

Deionized and doubly distilled water was used . Its specific conductivity was<1×10-6 S.m-1.poly(vinyl alcohol)is available product of Aldrich Chemical Company (U.S.A) whose number average molecular weight (125)kg.mol-1. PVA used in this study is solid (powder) material and completely soluble in water.

(b)Density Measurements.

The density of the investigated solutions was measured at the temperature range studied with an Anton Paar digital densimeter (DMA60/601) with a thermostatted bath controlled to ±0.001K.The densimeter was calibrated with water ,dehumidized air and several aqueous solutions of potassium chloride. The precision in the density values measured using this densimeter is estimated to be better than 2×10 -6 g.cm -3 .

#### Results and Discussion

The experimental measured densities of (PVA+water) at 298.15, 308.15, 318.15      and 328.15 K are given in Table (1). Experimental density for the binary mixture in the molality range studied obey equation of type (Barbosa et al. , 2001) :

ρ=a+bm+cm2+−−−−……………..(1)

The a, b, and  c coefficients for the equation(1) are listed  in Table (2) together with the standard deviation σ, defined by :

σ=ρobs−ρcal2N−P12……………..(2)

Where ρobs  and ρcal are the observed and the calculated density values respectively, N  is the number of experimental points and  P is the number of  coefficients in equation(1).

The volume of the binary solution, V1,2cm3,containing (m) moles of solute per kilogram of solvent was calculated from (Klofutar et al. , 1992)  :

V1,2=1000+mM2ρ      ……………….(3)

Where M2g.mol−1 is the solute molecular weight, and ρ is the density of solution. The values of  V1,2 for investigated solution are decreased with increasing concentration, Table (3).

The concentration dependence of  V1,2can be described by (Wurzburger et al. ,1998)  :

V1,2=Vs∘+V2,0m+ν22m2+ν222m3+−−−−−− ………(4)

Where Vs∘=1000ρ1∘, ρ1∘g.cm−3 is the density of the pure solvent, V2,0cm3.mol−1is the partial molar volume of solute at infinite dilution and ν22,ν222 etc. are the virial coefficients according to McMillan-Mayer theory of solution (Dindar ,2001), and present the contribution to the excess thermodynamic properties of pair,triplet and higher aggregates.

For the investigated solution, it was found that the volume of solution at a definite temperature are linearly dependent on the concentration of solute,i.e. the relation(4) is reduced to :

V1,2=Vs∘+V2,0m  …………………(5)

The values of (V2,0)  are concentration independent and slightly increase with increasing temperature as shown in  Table (4).

The partial molecular volume at infinite dilution, ν2,0cm3.molecule−1, for the investigated solution was calculated from :

ν2,0=V2,0/NA ………………..(6)

Where NA is the Avogadro,s constant. The molecular volume of the pure liquid solute ν2∘cm3.molecule−1, was calculated from :

α1,2−α2,0   …………………..(7)

Where  ρ2∘  is the density of the pure solute. A compartion of the partial molecular volume at infinite dilution ν2,0 with molecular volume ν2∘ show that the former is smaller than the later. Values of  ν2,0 and  ν2∘ together with the values of their ν2,0ν2∘ are given in Table(4). The partial excess molecular volume was calculated from :

ν2,0exc=ν2,0−ν2∘ ………………..(8)

These values, which characterize the volume changes associated with the transfer of one molecule of solute from the pure solute to solution at infinite dilution, are negative and relatively high.

The partial molar volume at infinite dilution for investigated aqueous solution, listed in Table(4), is temperature dependent. From figure(1) it can be seen that the plots of  V2,0 against T−T∘ are linear

V2,0=a∘+a1T−T∘    …………………(9)

Where a∘   and  a1are empirical constants and T is the absolute temperature, T∘=298.15K. The coefficients a∘  and  a1 , determined by the method of least square ,are ( 51.3062 ) and ( 0.0026 ) respectively . The ratio a1a0 at the temperature range studied was ( 0.5067x10-4 ) .

As the partial molar volume of investigated solution is concentration independent and equal to the volume at infinite dilution, so the value of the partial molar expansibility of the solute E2=∂V2∂TPcm3.mol−1.K−1 is also concentration independent and equal to that value at infinite dilution E2=E2,0 .

the partial molar expansibility of the solute at infinite dilution is equal to the regression coefficient    a1 of equation(9) and the thermal expansion  coefficient of the solute at infinite dilution α2,0K−1 defined as (Klofutar et al. , 1992)  :

α2,0=1V2,0∂V2,0∂T=E2,0V2,0   …………………..(10)

Which is equal to the ratio a1a∘ at 298.15K. The values of α2,0  calculated from equation(9) are given in Table(4). The values of α2,0  tend to decrease slightly with increasing temperature. On the other hand, the thermal expansion  coefficient of solution  α1,2K−1 is defined as :

α1,2=1V1,2∂V1,2∂T  ………………..(11)

Where  V1,2  is the volume of solution containing   m  mole of solute per kilogram of solvent. Thus, the thermal expansion  coefficient of the investigated solution is calculated from :

α1,2=1V1,2103ρ1∘α1∘+mE2,0  ………….(12)

Where α1∘   is the thermal expansion  coefficient of pure water 2.1×10−4K−1 (Atkins and Paula , 2002)  .

The values of α1,2  for investigated solution at 298.15K are given in Table(4). The dependence of α1,2−α1∘ against the volume fraction of solute φ is shown in figure(2). The volume fraction was used instead of molality or mole fraction of solute to allow for the effects of size differences of solute and solvent molecules. The volume fraction of solute was calculated from :

φ=mV2,01000ρ1∘+mV2,0  ………………..(13)

From figure(2), it can be seen that the dependence of α1,2−α1∘ on φ is linear. This dependence may be expressed in the form :

α1,2−α1∘=α1,2−α2,0+α2,0−α1∘φ  …………..(14)

The values α2,0−α1∘ and α1,2−α2,0 for investigated solution at 298.15K are (0.0722x104) and (1.1619x104) respectively , it can be seen that the thermal expansion  coefficient of the investigated solution is higher than that of the pure solvent .

Table(1)Experimental Densities for Aqueous PVA at the Temperature Range Studied.

| m×10−4 (mol .kg-1) | ρ1,2×103Kg.m−3 298.15 K 308.15 K 318.15 K 328.15 K |  |  |  |
| --- | --- | --- | --- | --- |
| 0.0000 | 0.99707 | 0.99406 | 0.99025 | 0.98573 |
| 0.3224 | 0.99790 | 0.99519 | 0.99185 | 0.98630 |
| 0.4848 | 0.99820 | 0.99569 | 0.99197 | 0.98663 |
| 0.6450 | 0.99862 | 0.99622 | 0.99264 | 0.98713 |
| 0.9696 | 0.99959 | 0.99668 | 0.99312 | 0.98782 |
| 1.2913 | 1.00048 | 0.99752 | 0.99425 | 0.98871 |
| i.4570 | 1.00102 | 0.99803 | 0.99479 | 0.98925 |
| 1.6234 | 1.00144 | 0.99847 | 0.99523 | 0.98975 |
| 1.9424 | 1.00238 | 0.99930 | 0.99563 | 0.99087 |
| 2.2650 | 1.00324 | 1.00032 | 0.99704 | 0.99209 |
| 2.5991 | 1.00423 | 1.00120 | 0.99777 | 0.99306 |
| 2.7523 | 1.00468 | 1.00144 | 0.99853 | 0.99347 |
| 2.9130 | 1.00514 | 1.00205 | 0.99887 | 0.99394 |
| 3.2275 | 1.00591 | 1.00211 | 0.99927 | 0.99471 |
| 3.8951 | 1.00793 | 1.00476 | 1.00116 | 0.99671 |

Table(2)Parameters in the Equation(1),ag.cm−3,bg.cm−3.mol−1.Kg and cg.cm−3.mol−2.Kg2at the Temperature Range Studied.

| Temperature | 298.15 K | 308.15 K | 318.15 K | 328.15 K |
| --- | --- | --- | --- | --- |
| a | 0.996972 | 0.994252 | 0.990136 | 0.985513 |
| b | 0.002716 | 0.002532 | 0.003247 | 0.002840 |
| c | 0.000025 | 0.000042 | -0.000101 | 0.000011 |
| σ | 0.003274 | 0.003135 | 0.003350 | 0.003359 |

Table(3) Volume of Aqueous Solution, V1,2cm3 Containing (m) Moles of Solute per Kilogram of Solvent at the Temperature Range Studied.

| m×10−4 (mol .kg-1) | V1,2×10−5cm3 298.15 K 308.15 K 318.15 K 328.15 K |  |  |  |
| --- | --- | --- | --- | --- |
| 0.0000 | 1.8068 | 1.8123 | 1.8193 | 1.8276 |
| 0.3224 | 1.8053 | 1.8103 | 1.8175 | 1.8266 |
| 0.4848 | 1.8048 | 1.8093 | 1.8166 | 1.8260 |
| 0.6450 | 1.8041 | 1.8089 | 1.8157 | 1.8244 |
| 0.9696 | 1.8023 | 1.8076 | 1.8140 | 1.8228 |
| 1.2913 | 1.8007 | 1.8060 | 1.8120 | 1.8211 |
| i.4570 | 1.7998 | 1.8051 | 1.8110 | 1.8203 |
| 1.6234 | 1.7990 | 1.8043 | 1.8102 | 1.8194 |
| 1.9424 | 1.7973 | 1.8028 | 1.8095 | 1.8182 |
| 2.2650 | 1.7958 | 1.8010 | 1.8069 | 1.8159 |
| 2.5991 | 1.7940 | 1.7994 | 1.8056 | 1.8142 |
| 2.7523 | 1.7932 | 1.7985 | 1.8042 | 1.8134 |
| 2.9130 | 1.7924 | 1.7979 | 1.8036 | 1.8126 |
| 3.2275 | 1.7910 | 1.7963 | 1.8022 | 1.8112 |
| 3.8951 | 1.7874 | 1.7930 | 1.7995 | 1.8076 |

Table(4) Partial Molar Volume at Infinite Dilution V2,0, Partial Molecular Volume at Infinite Dilutionν2,0,  Molecular Volume of  Pure Soluteν2∘, the Ratio ν2,0ν2∘, Excess Partial molecular volume at infinite dilution ν2,0exc and Thermal Expansion Coefficients at Infinite Dilution  α2,0at the Temperature Range Studied.

| Temp. | V2,0 | ν2,0 | ν2∘ | ν2,0ν2∘ | ν2,0exc | α2,0x10-4 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 K | 51.3062 | 8.5231 | 17.4926 | 0.4872 | -8.9695 | 0.5067 |
| 308.15 K | 51.3247 | 8.5319 | 17.7028 | 0.4820 | -9.1709 | 0.5065 |
| 318.15 K | 51.3661 | 8.5502 | 17.7806 | 0.4809 | -9.2304 | 0.5061 |
| 328.15 K | 51.3795 | 8.5976 | 18.0328 | 0.4767 | -9.4352 | 0.5060 |

Table(5)Values of the Thermal Expansion  Coefficients (α1,2) and  the Volume Fraction φof the Investigated Solution at 298.15K .

| m×10−4(mol .kg-1) | φ | (α1,2)K-1 x104 |
| --- | --- | --- |
| 0.0000 | 0.0000 | 1.1623 |
| 0.3224 | 0.0162 | 1.1632 |
| 0.4848 | 0.0242 | 1.1636 |
| 0.6450 | 0.0319 | 1.1640 |
| 0.9696 | 0.0473 | 1.1652 |
| 1.2913 | 0.0620 | 1.1662 |
| i.4570 | 0.0694 | 1.1668 |
| 1.6234 | 0.0767 | 1.1673 |
| 1.9424 | 0.0904 | 1.1684 |
| 2.2650 | 0.1038 | 1.1694 |
| 2.5991 | 0.1173 | 1.1706 |
| 2.7523 | 0.1234 | 1.1711 |
| 2.9130 | 0.1297 | 1.1716 |
| 3.2275 | 0.1417 | 1.1725 |
| 3.8951 | 0.1661 | 1.1734 |

V2,0/(cm3.mo-1)

Figure (1)The temperature dependence of the partial molar volume of PVA

(α 1,2 – α 1 0 )/K-1

φ

Figure (2) Dependence of α1,2−α1∘  on volume fraction of PVA at 298.15K .

References

Adam O.E.A."Physical properties study of aqueous solutions of Glycols over temperature range 293.15-318.15K" Ph.D.Thesis, Baghdad University, (2004).

Akihiko T.  , Miki N. , Akihiro K. and Norio N.  ”Dynamic Light Scattering and Dynamic Viscoelasticity of Poly(vinyl alcohol) in Aqueous Borax Solutions. 4.Further Investigation on Polymer Concentration and Molecular Weight Dependencies”,Macromolecules, Vol.31,P.436(1998) .

Atkins P.W., and dePaula J., "Physical Chemistry",7th ed ,Oxford University Press, p.161-166,815(2002).

Barbosa E.F.G., Sousa S.M.C., Santos M.C.S., and Lampreia I.M.S., Phs.Chem.Chem Phs., 3,556(2001).

Cheng R., Shao Y., Liu M. and Lu R. ”Effect of Adsorption on the Viscosity of Dilute Polmer Solution”,Chinese J.Polm.Sci.,Vol.16,P.1(1998) .

Creutz E.   and Wilson R.  ,J.Chem.Phys.,Vol.14,P.725(1946) .

Czechowski G., and Jadzyn J., Z.Naturforsch,58a,321(2003).

Dindar C. "High-Pressure viscosity and density of polymer solutions at the critical polymer concentration in near-critical and supercritical fluid" M.Sc. Thesis, Virginia Polytechnic Institute and State University,U.S.A.(2001).

Douheret G., Davis M.I., Fjellandlanger I.J., and Hoiland H., J.Chem.Soc.,Faraday Trans., 93(10),1943(1997).

Kazuki K.  , Akihiko T.  and Norio N.  ”Dynamic Light Scattering and Dynamic Viscoelasticity of Poly(vinyl alcohol) in Aqueous Borax Solutions. 5.Temperature Effects”,Macromolecules, Vol.32,P.8872(1999) .

Klofutar C., Palijk S. and Golc-Teger S., Thermochim.Acta, 196,401(1992).

Muller-Plathe F. and Wilfred F.  ”Solvation of Poly(vinyl alcohol) in Water,Ethanol and an Equimolar Water-Ethanol Mixture:Structure and Dynamics Studied by Molecular Dynamics Simulation”,Polm.,Vol.38,P.2259(1997) .

Muller-Plathe F. ”Microscopic Dynamics in Water-Swollen Poly(vinyl alcohol)”,J.Chem.Phys.,Vol.108,P.8252(1998) .

Muller-Plathe F. ”Diffusion of Water in Swollen Poly(vinyl alcohol) Membranes Studied by Molecular Dynamics Simulation”,J.Membrane Sci.,Vol.141,P.147(1998)

Norio N.  , Akihiro K.  and Kunihiro O.  ”Dynamic Light Scattering and Dynamic Viscoelasticity of Poly(vinyl alcohol) in Aqueous Borax Solutions. 2.Polymer Concentration and Molecular Weight Effects”,Macromolecules, Vol.29,P.1445(1996) .

Rongshi C.  , Yu Y.  and Xiaohu Y.  ”The Wall Effect on Viscosity Measurement of Dilute Aqueous Solution of Poly(ethylene glycol) and Poly(vinyl alcohol) Using a Paraffin-Coated Capillary Viscometer”,Polym.,Vol.40,P.3773(1999) .

Wurzburger S., Sartorio R., Guarino G. and Nisi M., J.Chem.Soc.,Faraday Trans.1, 84,2279(1988).