Characterization   of   Permanent   Deformation   Of Subgrade   Soils   Using   Cyclic   Loading   Test

Nahla Y. Ahmad 		Ali A. Alwash

Babylon University - Civil Engineering

Anmar Faleh Degan

Engineering Researcher

Abstract

Permanent deformation of subgrade soils is the accumulation of plastic deformation in soils due to continuous repeated loads from traffic loading. The main objective of this study is to investigate some of the factors that affect the permanent deformation of subgrade soils such as soil types, compaction moisture content, applied stress and dry density. Also, to formulate regression models which have been obtained to predict the permanent strain in subgrade soils as related to moisture content , time of loading, dry density and applied stress by using STATISTICA software.

This research also established a test procedure to use cyclic load test to measure the permanent strain of subgrade soils. The permanent strains were monitored during 60 load cycles, and the accumulated permanent deformations were determined. The test procedure and test results conducted on two types of soils that cover an important geographical area of Iraq, A4 and A6 soils are presented.

الخلاصة

التشوه الدائم لترب ما تحت الأساس هو تراكمُ التشوه اللدن في الترب بسبب الأحمال المتكرّرةِ المستمرةِ الناتجة من حركة المرور. إن الهدف الرئيسي لهذه الدراسة هو التحري حول بعض العوامل التي تسبب التشوه الدائم في ترب ما تحت الأساس مثل أنواع التربة، محتوى الرطوبة ، الإجهاد المسلط والكثافة الجافة. كذلك تم صياغة  موديلات للتنبؤ بالتشوه الدائم في الترب السطحية تعتمد على محتوى الرطوبة، زمن تسليط الحمل ،الكثافة الجافة والإجهاد المسلط باستخدام برنامج .(STATISTICA)

كما إن هذا البحث قد وضع أسسا" لإجراء اختبار باستخدام  فحص الأحمال المتكررة لقياس التشوه الدائم في ترب ما تحت الأساس. تم مراقبة  التشوه الدائم خلال 60 دورة متكررة وتم حساب التشوهات الدائمية المتراكمة. إن إجراء الاختبار تم على نوعين من أنواع الترب اللذين يغطيان منطقة جغرافية مهمة من العراق وهما الترب نوع  ((A4 و ((A6.

Introduction

The major function of subgrade soils is to provide support to pavement structures. Under heavy traffic loads, subgrade soils may deform and contribute to distress in the overlying pavement structure. In asphalt pavement, this distress normally takes the form of cracking and rutting. It has been well documented that the subgrade soils plays a critical role in the initiation and propagation of permanent deformation of pavement structures and directly influences the pavement performance [Huang, 1993].The subgrade soils, in particular the weak soft subgrades, contribute a significant portion (above 40 %) of the total pavement rutting [Majidzadeh, et al. 1978]. .  All pavement layers contribute to the permanent deformation of the pavement structure. Yet, subgrade does not attract as much attention as do the asphalt surface and granular base. The last are man-made products in some sense and their properties are relatively well known and have been extensively studied for several decades. Actually, with the implementation of (super level I mixture design method), the rutting of asphalt concrete can be minimized through the proper selection of materials. As a result, subgrade becomes a weak point in the pavement structure [Elliott, et al. 1998].

Research Objectives

1. Investigate the main factors related to the permanent deformation of two Iraqi subgrade soils including the compaction moisture content, applied stress, dry density and some soil types.

2. Develop models for the permanent deformation prediction of two kinds of local subgrade soils. Also, Presenting a procedure for the prediction of the permanent deformation of some subgrade soils.

Sampling

The subgrade soil samples that are used in this research were collected from two sites that cover an important geographical area of Iraq. The first subgrade soil sample was taken from the north shoulder of Kerbala-Hilla roadway near new Kerbala university, while the second sample was taken from Al-jadrreya in Baghdad near university of Baghdad .

Cyclic Loading Test

Due to the limitation of the available testing equipments, the possible local method which could be used to characterize the subgrade soils permanent deformation is the uniaxial cyclic load compression test. The consolidation apparatus for soils manufactured by (Geonor, Oslo - Norway) is employed to perform this test. The tests were performed on cylindrical specimens, 50.8 mm ( 2 in) in diameter and 101.6 mm ( 4 in) in height, giving a height to diameter ratio of  (2) [ Puppala, et. al., 1999]. Three stresses are used for the cyclic load tests : 28 KPa, 42 KPa and 63 KPa.

Mechanism of Permanent deformation

When a shear stress is sustained on a soil specimen the stress will be carried in the first place by the non-rigid clay matrix which exhibits translations and rotations of the particles. As a result the load will be transferred to the more rigid contacts causing significant decrease in creep rates. Important changes in the structure happen during this stage, the number and size of voids are reduced, fabric defects partially closed, spacing between clay size particles decreases. As a result the structure grows stronger leading to a stable equilibrium. After this stage, the soil structure is behaving macroscopically as a viscous material with a viscosity which increases with time due to a stiffening of the contact bonds [Waker, 1969] as cited by [Kemmonr, 1986].

At low and moderate stress levels, the deformational energy stored in the specimen during the loading process is of a small order, and dissipated within a short period of time. Under high stress levels, the specimen exhibits greater primary and secondary creep. The stresses will be so high that microcracks of different orientation are liable to develop, old fissures grow and new ones appear. As a result, the specimen undergoes accelerating creep at a considerable rate leading to failure [Pusch & Felthan, 1980].

Fabrication of Specimens

1. Mixing

The soils were mixed with the desired amount of water to control the moisture content and dry density. This means that the compacted soil specimens were prepared at a various moisture content to simulate the range of moisture expected in the subgrade within a pavement.

2. Compaction

At first, the standard Proctor compaction tests were conducted on the two soil types. These tests yielded dry unit weight versus moisture content relationships. The results of the standard Proctor compaction test used to establish a various moisture content and dry unit weight levels at which soil samples prepared and tested with the cyclic load tests.

A special split of three pieces of  steel mold with ( 50.8 mm ) in diameter and (101.6 mm) in height was designed.

The strain (εp) is calculated by applying the following equation:

εp =  pd / h

Where:

εp  = axial strain (mm/mm)

Pd = axial deformation (mm)

h = specimen height (mm)

In order to investigate the effects of moisture content on the accumulation of permanent deformation , specimens were fabricated at six different moisture contents corresponding to 90% , 100% , 105% , 110% , 115% and  120%  of  optimum moisture content to simulate the field conditions of pavement subgrades.

Specimens with the same moisture content and dry density were subjected to various levels of axial stress (28 KPa, 42 KPa and 63 KPa) to explore the role of stresses in the development of subgrade deformation. The effect of limited variation in density on deformation behavior was also investigated where the specimens are compacted in different degree of dry density to investigate the effects of dry density on a permanent deformation.

Classification Tests

The results of Atterberg limits tests conducted on fractions passing sieve No. 40 indicate that the Kerbala-Hilla roadway soil samples are Low plastic soils while Al-jadrreya soil samples are Medium plastic soils. the soil specimens can be classified according to the unified soil classification system (u.s.c.s) as (clayey silt soil) for both Kerbala-Hilla roadway soil sample and Al-jadrreya soil sample. While the AASHTO classification indicates that Kerbala-Hilla roadway soil sample is (A4) soil and Al-jadrreya soil sample is (A6) soil. The physical properties of the two soils are summarized in Table (1).

Table (1) Summary of Soil Properties

| Soil | Kerbala-Hilla | Al-jadrreya |
| --- | --- | --- |
| Sampling | Kerbala-Hilla Roadway | Al-jadrreya - Baghdad |
| Location | Near New University of Kerbala | Near University of Baghdad |
| LL | 30.7 | 35.5 |
| PL | 23.6 | 24.25 |
| PI | 7.1 | 11.25 |
| Water Content (%) | 26 | 20 |
| Specific Gravity | 2.69 | 2.73 |
| Optimum Moisture Content (%) | 18.25 | 20 |
| Maximum Dry Density (gm/cm3 ) | 1.75 | 1.71 |
| % of Fines | 88.4 | 93.6 |
| AASHTO Classification | A4 | A6 |
| Unified Classification | Clayey Silt Soil | Clayey Silt Soil |

Test Results and Discussion

Permanent deformation of subgrade soils is characterized by a rapid increase in deformation during the first cycle, followed by gradual stabilization. The amount of deformation depends on the characteristics of the material and the applied load.

Effect of Moisture Content on Permanent Deformation

the permanent strain is plotted against the time of loading for all degrees of the moisture content under several levels of stress (28 KPa), (42 KPa) and (63 KPa).

Cyclic load testing results for Kerbala-Hilla roadway soil (A4 soil), are presented in Figures (1) to (3). Figure (1) illustrates test results with moisture contents corresponding to (90%, 100%, 105%, 110%, 115%, and 120%) of optimum moisture content and dry densities corresponding to 95% of maximum dry density with stress of 28 KPa. In this Figure it can be seen that when moisture content increases from 90% to 110% of optimum, the permanent strain increases by 270%.

While cyclic load testing results for Al-jadrreya soil (A6 soil), are presented in Figure (4) to (6). Figure (4) illustrates test results with moisture contents corresponding to (90%, 100%, 105%, 110%, 115%, and 120%) of optimum moisture content and dry densities corresponding to 95% of maximum dry density with stress of 28 KPa. In this Figure it can be seen that when moisture content increases from 90% to 110% of optimum, the permanent strain increases by 220%.

| Figure (1) Effect of Moisture Content on the Relationship between Loading Time and Accumulated Permanent Strain (A4 soil, stress: 28 KPa) | Figure (2) Effect of Moisture Content on the Relationship between Loading Time and Accumulated Permanent Strain (A4 soil, stress: 42 KPa) |
| --- | --- |
| Figure (3) Effect of Moisture Content on the Relationship between Loading Time and Accumulated Permanent Strain (A4 soil, stress: 63 KPa) | Figure (4) Effect of Moisture Content on the Relationship between Loading Time and Accumulated Permanent Strain (A6 soil, stress: 28 KPa) |
| Figure (5) Effect of Moisture Content on the Relationship between Loading Time and Accumulated Permanent Strain (A6 soil, stress: 42 KPa) | Figure (6) Effect of Moisture Content on the Relationship between Loading Time and Accumulated Permanent Strain (A6 soil, stress: 63KPa) |

Effect of Stress on Permanent Deformation

Specimens with the same moisture content and dry density were subjected to various levels of stresses to explore the role of stress in the development of subgrade deformation.

Figure (7) shows the accumulated permanent strain of A4 soil at 90% of the optimum moisture content at different stages of loading procedure for three levels of applied stress  (28 KPa), (42 KPa) and   (63 KPa). it can be seen that when the applied stresses increased from 28 KPa to 63 KPa, the permanent strain increased (81%) for soil A4, while in Figure (8), when the applied stresses increase from 28 KPa to 63 KPa, the permanent strain increased (100%), for soil A6.

it can be seen that at a lower applied stress there is a gradual stabilization, while at a higher applied stress, a rapid increase in strain is observed for both soils used in this research, indicating possibility of rutting accumulation over time.

| Figure (7) Effect of Stress on the Relationship between Loading Time and Accumulated Permanent Strain (A4 soil, Moisture Content 90%) | Figure (8) Effect of Stress on the Relationship between Loading Time and Accumulated Permanent Strain (A6 soil, Moisture Content 90%) |
| --- | --- |

Effect of Dry Density on Permanent Deformation

Figure (9) demonstrates the effect of the dry density on the accumulation of the permanent deformation for soil A4. Specimens are fabricated to moisture content at 100% of the optimum moisture content and the dry density increased from 93% to 96.6% of maximum with applied stress of 42 KPa, it can be seen that the permanent strain is decreased by 34%.

The effect of dry density on the accumulation of the permanent deformation for soil A6 is presented in Figure (10). Specimens are fabricated to moisture content at 100% of the optimum moisture content and the dry density increased from 94% to 96.4% of maximum with applied stress of 42 KPa, it can be seen that the permanent strain is  decreased by 17%.

| Figure (9) Effect of Dry Density on the Relationship between Loading Time and Accumulated Permanent Strain (A4 soil, Stress: 42 KPa) | Figure (10) Effect of Dry Density on the Relationship between Loading Time and Accumulated Permanent Strain (A6 soil, Stress: 42 KPa |
| --- | --- |

Effect of Soil Type on Permanent Deformation

From Figures (1), (2), (3) and Figures (4), (5), (6), it can be observed that soil A4 has more resistance to the permanent deformation than soil A6, specially for the moisture content near to the optimum with all degree of stresses. But when the moisture content increased up to more than 110% of the optimum moisture content, the permanent deformation of the two soils was approximately convergent.

By a simple comparison between the permanent deformation of the two soils (A4 and A6) for the Figures (1) and (4) with moisture content 100% and 28 KPa applied stress, it can be seen that soil A6 showed more permanent deformation than soil A4, (about 66%).

it can be observed that soil A4 has more resistance to the permanent deformation than soil A6, specially for the moisture content near to the optimum with all degree of stresses. But when the moisture content increased up to more than 110% of the optimum moisture content, the permanent deformation of the two soils was approximately convergent.

General Trend of Deformation Behavior

It can be seen that the permanent deformation under the first load application for the two subgrade soils (A4 and A6) constituted between (27.5% to 50%) of the total permanent deformation for all tests that was accumulated after 60 cycles. Table (2) and (3) indicate that the accumulated permanent strain expressed as a  percent  of  the total permanent strain during the first, tenth, twenty five and fifty  cycles for soil A4 and for soil A6 with the moisture content of 105% of the optimum moisture content and applied stresses of 28 KPa, 42 KPa and 63 KPa with dry density 95% of maximum dry density.

Table (2) Accumulation of Permanent Strain at Various Load Cycles Expressed as a Percentage of Deformation at 60 Cycles for A4 Soil (MC=105% of OMC, DD =95% of MDD)

| Stress (KPa) | 1st | 10th | 25th | 50th |
| --- | --- | --- | --- | --- |
| 28 | 35.8 | 61.6 | 77.2 | 94 |
| 42 | 37.2 | 64.8 | 81.4 | 95.4 |
| 63 | 47.5 | 69.7 | 82.5 | 95.5 |

Table (3) Accumulation of Permanent Strain at Various Load Cycles Expressed as a Percentage of Deformation at 60 Cycles for A6 Soil (MC=105% of OMC, DD= 95% of MDD)

| Stress (KPa) | 1st | 10th | 25th | 50th |
| --- | --- | --- | --- | --- |
| 28 | 31 | 48 | 65.7 | 91.6 |
| 42 | 37.8 | 60.3 | 76.5 | 95 |
| 63 | 43.2 | 64.8 | 78.8 | 94.4 |

Statistical Model

By using STATISTICA software, these variables will be obtained and determined simultaneously under each moisture content using nonlinear regression analysis on the obtained tests results.

Statistical Analysis

In a statistical modeling the overall objective is to develop a predictive equation relating a criterion variable to predictor variables. The criterion variable is the permanent strain while the predictor variables include the test conditions (stress level), and some of the soil properties (dry density, moisture content) and soil types.

Model Adequacy Assessment

There are two approaches generally used to assess the adequacy of the proposed regression models, the first one is based on the examining goodness of fit measures, where the second approach is based on the graphical analysis of the residuals, (also called diagnostic plots)     [Albayati, 2006].

Prediction Models for Permanent Strain

The adopted models structure and the terms included in these models are shown in Table (4), while in Table (5), (7) and (9) the statistical summary of these models are presented. Also Tables (6), (8) and (10) shows the nonlinear analysis for the soils.

Table (4) General Models Structure for the Permanent Strain

| Criterion Variable | Model Structure | Model No. |
| --- | --- | --- |
| εp | Co [(T DD MC ST) C1] | 1 |
| εp | Co + (TC1) + (STC2) + (MCC3) + (DDC4) | 2 |
| εp | Co + C1T + C2ST + C3MC + C4DD | 3 |
| εp | Co [(TC1) (STC2) (MCC3) (DDC4)] | 4 |

Where:

εp= accumulated permanent strain (mm/mm)

T=   time of loading (second)

DD= dry density (gm/cm3) as a percentage of maximum dry density

ST= applied stress (KPa)

MC= moisture content (%) as a percentage of optimum moisture content

Table (5) Statistical Summary for Permanent Strain Models for Soil A4

| Loss Function | Final Loss | R | Variance Explained (R2) | Model No. |
| --- | --- | --- | --- | --- |
| (OBS-PRED)**2 | 0.024990903 | 0.16610 | 2.7589% | 1 |
| (OBS-PRED)**2 | 0.009437004 | 0.79549 | 63.280% | 2 |
| (OBS-PRED)**2 | 0.008616109 | 0.81532 | 66.474% | 3 |
| (OBS-PRED)**2 | 0.001622474 | 0.96792 | 93.687% | 4 |

Table (6) Nonlinear Analysis for Soil A4

| Model: εp = Co*((T**C1)*(ST**C2)*(MC**C3)*(DD**C4)) Final loss = 0. 001622474 |  |  |  |  | Sta. Nonlin. Estimation |
| --- | --- | --- | --- | --- | --- |
| C4 | C3 | C2 | C1 | C0 | N = 1020 |
| -15.502487 | 14.856185 | 0.817165 | 0.145878 | 0.000250 | Estimate |

Where:

N = numbers of valid cases

According to Tables (5) and (6), the final form of proposed model for soil A4 is:

εp = 2.5*10-4 (T 0.145878) (ST 0.817165) (MC 14.856185) (DD -15.502487) ……..(1-1)

In this model the numbers of valid cases (N) are (1020) which represent a large number of data in order to give the model high accuracy.

it can be seen from Figure (11) that the residuals in the first plot are normally distributed, and the  second plot yields points close to the (45)° line, then the proposed regression function gives an accurate prediction of the values that are actually observed.

Figure (11) Diagnostic Plot for Permanent Strain (Model No.4) Soil A4

Table (7) Statistical Summary for Permanent Strain Models for Soil A6

| Loss Function | Final Loss | R | Variance Explained (R2) | Model No. |
| --- | --- | --- | --- | --- |
| (OBS-PRED)**2 | 0.0157 | 0.362 | 13.118% | 1 |
| (OBS-PRED)**2 | 0.0043 | 0.872 | 76.124% | 2 |
| (OBS-PRED)**2 | 0.0038 | 0.886 | 78.663% | 3 |
| (OBS-PRED)**2 | 0.00109 | 0.969 | 93.986% | 4 |

Table (8) Nonlinear Analysis for Soil A6

| Model: εp = Co*((T**C1)*(ST**C2)*(MC**C3)*(DD**C4)) Final loss: 0.001092820 |  |  |  |  | Sta. Nonlin. Estimation |
| --- | --- | --- | --- | --- | --- |
| C4 | C3 | C2 | C1 | C0 | N = 1020 |
| -9.14337 | 8.615739 | 0.676856 | 0.21570 | 0.000475 | Estimate |

According to tables (7) and (8), the final form of proposed model for A6 soil is:

εp = 4.75*10-4 (T 0.21570) (ST 0.676856) (MC 8.615739) (DD -9.14337) …..…(1-2)

As in equation (1-1), In this model the numbers of valid cases (N) are (1020) which represent a large number of data in order to give the model high accuracy. Figure (12) provides the comparisons between predicted versus measured plastic strain, shows that good correlations are obtained, which indicate that the present formulation has adequately represented the plastic strain response of soil tested under the cyclic loading test.

Figure (12) Diagnostic Plot for Permanent Strain (Model No.4) Soil A6

Equation (4-3) represents a model for both soils (A4 and A6) where the results of both soils were  collected and dealing in the statistica software with (2040) number of valid cases which represent a large number of data in order to represent the two soils in one model. Also it can be seen from Figure (13) that the residuals in the first plot are normally distributed, and the  second plot yields points close to the (45)° line, then the proposed regression function gives an accurate prediction of the values that are actually observed.

Table (9) Statistical Summary for Permanent Strain Models for Soil A6 and A4

| Loss Function | Final Loss | R | Variance Explained (R2) | Model No. |
| --- | --- | --- | --- | --- |
| (OBS-PRED)**2 | 0.041975841 | 0.25140 | 6.3200% | 1 |
| (OBS-PRED)**2 | 0.015282834 | 0.81174 | 65.892% | 2 |
| (OBS-PRED)**2 | 0.014015237 | 0.82898 | 68.721% | 3 |
| (OBS-PRED)**2 | 0.005020326 | 0.94232 | 88.796% | 4 |

Table (10) Nonlinear Analysis for Soil A6 and A4

| Model: εp = Co*((T**C1)*(ST**C2)*(MC**C3)*(DD**C4)) Final loss: 0.005020326 |  |  |  |  | Sta. Nonlin. Estimation |
| --- | --- | --- | --- | --- | --- |
| C4 | C3 | C2 | C1 | C0 | N = 2040 |
| -8.83546 | 11.19941 | 0.701858 | 0.181595 | 7*10-10 | Estimate |

According to tables (9) and (10), the final form of proposed model for both A4 and A6 soils is:

εp = 7*10-10 (T 0.181595) (ST 0.701858) (MC 11.19941) (DD --8.83546) …….…..(1-3)

Figure (13) Diagnostic Plot for Permanent Strain (Model No.4) Soil A6 and A4

Conclusions

Within the limitations of materials and testing program adopted in this work, the followings are concluded:

1) The moisture content has a significant effect on the permanent strain for A4  and A6 soils. The increase of the moisture content from 90% to 110%, has increased the permanent strain by 270%  for A4 soil and by 220% for A6 soil. Therefore, with the increase of the moisture content a considerable increase in the permanent strain is highly expected.

2) The applied stress showed a considerable influence on the permanent strain values, specially on the first cycle of loading, where the increase of stresses from 28 KPa to 63 KPa, has increased the permanent strain by (81%) for A4 soil and by (100%) for A6 soil. Therefore, High permanent strain was recorded when soils were subjected to high stresses.

3) The permanent strain results for soils A4 and A6 compacted at wet of optimum moisture content condition was higher than those compacted at dry of optimum moisture content.

4) The permanent strain results showed that A4 soil at the optimum moisture content exhibited lower plastic deformation (about 105%) compared with A6 soil for all degrees of stresses.

5) At the optimum moisture content, the permanent strain has been increased by 25%  for soil A4 and by 69.7% for soil A6 for an  increase in the applied stresses from 28 KPa to 63 KPa.

6) The effect of limited variation in dry density on deformation behavior produces a  slight increase in the permanent strain for both soils.

References

Albayati, A. H. K., (2006). "Permanent Deformation Prediction of Asphalt Concrete Under Repeated Loading", Ph. D. Thesis, University of Baghdad.

Elliott, R. P. Dennis, N. D. and Qiu, Y., (January 1998). "Permanent Deformation of Subgrade Soils (Phase I: A Test Protocol)", MBTC FR 1069, Department of Civil Engineering, University of Arkansas.

Huang, Y. H. (1993). "Pavement Analysis and Design", 1st Edition, Prentice Hall, Englewood Cliffs, New Jersey, USA.

Kemmonr, A.A., (January, 1986). "Study of Creep and Effect of Strain Rate on the Strength and Deformation of Compacted Soil-Cement Samples", M. Sc. Thesis, University of Baghdad.

Majidzadeh, K., Bayomy, F., and Khedr, S. (1978). "Rutting Evaluation of Subgrade Soils in Ohio", Transp. Res. Rec. No. 671, Transportation Research Board National Research Council, Washington, D.C.

Puppala A. J., Mohammad, L. N, and Allen A., (1999). "Permanent Deformation Characterization of Subgrade Soils from RLT Test", Journal of Materials in Civil Engineering", Vol. 11, No. 4, pp. 274-282.

Pusch, R. and Feltham, P. (1980)."A stochastic model of the Creep of Soils", Geotechnique, Vol. 30, No.4, pp. 497-506.