Determination of Monomer Reactivity Ratios of Poly ( Acrylonitrile – co – vinylacetate )

| Tariq S.Najim College of Scienc | Abdul Hussien K. Sharba College of Scienc | Nadia A. Butti College of Scienc |
| --- | --- | --- |
| University o f Al-Mustansiryah |  |  |

(NJC)

(Receivedon 15/11/2006)   (Accepted for publication on  22/8 /2007)

Abstract :

Copolymers of Acrylonitrile (AN) and Vinyl Acetate (VAc) were synthesized in dimethyl formamide (DMF) using benzoyl peroxide (BPO) as initiator at 75oC . The copolymers were analyzed by IR spectroscopy. The monomer reactivity ratios were determined by the methods of Fineman – Ross (F-R) and Kelen – TűdÖs (K-T) giving the results shown in the following table:-

| r1(AN) |  |  |  | r2(VAc) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| F-R |  | K-T |  | F-R |  | K-T |  |
| 1st | 2nd | 1st | 2nd | 1st | 2nd | 1st | 2nd |
| 2.2347 | 2.5341 | 2.3889 | 2.7087 | 0.0303 | 0.002 | 0.1038 | 0.0719 |

الخلاصة

تم تحضير البوليمر المشترك للاكريلونايتريل (AN) و الفنيل استيت (VAc) في مذيب ثنائي مثيل فورمأيد    (DMF) باستخدام بيروكسيد البنزويل كبادئ وبدرجة حرارة 75o c   . تم تحليل البوليمر المشترك بواسطة مطيافية الاشعة تحت الحمراء .

الفعالية النسبية للمونمرات تم تحديدها بواسطة طريقة فنمان و روس (F-R) وطريقة كلين-ثيودوس (K-T) و النتائج موضحة في الجدول التالي :

| r1(AN) |  |  |  | r2(VAc) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| F-R |  | K-T |  | F-R |  | K-T |  |
| 1st | 2nd | 1st | 2nd | 1st | 2nd | 1st | 2nd |
| 2.2347 | 2.5341 | 2.3889 | 2.7087 | 0.0303 | 0.002 | 0.1038 | 0.0719 |

Introduction :

Japan has recently been the leading contributor in the diversification of the production of modified acrylic fibers(1) More than 85% of acrylonitrile monomer must be incorporated into copolymer in order for it to be termed an acrylic fiber(2). Copolymerization of acrylonitrile with various comonomers produces specialty fibers for different applications. Methyl acrylate, methyl methacrylate and vinyl acetate are the commonly used “ neutral” comonomers. They increase solubillity and change the morphology of the fiber(3) . The theory of radical copolymerization leads to the conclusion that the composition of the copolymer is determined by the reactivity ratios (r1 and r2 ) which reflect the inherent tendencies of a radical  to  react with its own monomer relative to the comonomer. copolymerizations are classified according to values of the product r1r2. When r1r2= 0, an alternating copolymer is produced, when r1r2= 1, the copolymerization is said to be ideal, since r1=1r2 , the copolymer is random.

Many methods have been used to estimate reactivity ratios of a large number of comonomers but the method of increasing application are those of Fineman- Ross and Kelen – TÜdŐs (4). 1H–NMR, 13C–NMR and FTIR methodologies are used to determine the copolymer composition(5)...

The aim of the present work is to evaluate the reactivity ratios of comonomers using two methods, both of them depend on the absorption and absorptivity of certain group in the monomers and copolymers.

Experimental :

1- Materials and purification

Acrylouitrile (AN) (Aldrich) was washed with (10% NaOH) to remove inhibitors and then washed with distilled water to remove any trace of NaOH and finally distilled at reduced pressure. Vinyl acetate (VAc) was distilled before use. Dibenzoyl peroxide BPO (Aldrich ) was purified by dissolving in small amounts of chloroform followed by precipitation with n - hexane.

2- Synthesis

For copolymerization , the AN and VAc in various proportions but with the total weight maintained at 4g and the initiator BPO being  kept at concentration of ( 3×10– 4 mol/L) were dissolved in 25 ml of DMF. The content of the flask was degassed with argon for at least 2 minutes and polymerization was carried out at 75˚C for a period of 30 minutes. Each copolymer was precipitated by ethanol, washed repeatedly in methanol and dried. For the determination of  reactivity ratio, the polymer  conversions were always less than 5%. Homopolymers of AN and VAc were also prepared and their absorbances were measured using liquid cell with path length of 1cm. The IR spectra of copolymers and homopolymers were    recorded           by     Pye Unicam (SP3-100 IR) as films on KBr window, figure (1).

Results and Discussion

3-Determination of Molar Fractions (F)

The molar fractions of (AN) and (VAc) in poly (AN-co-VAc) were determined by two methods:-

a) The first method

This method depends on the absorbance of the recorded analytical absorption bands that is CN and CO for (AN) and (VAc) respectively , besides the molecular weights of the (AN) and (VAc) according to the following equations(6) :-

Where A is the absorbance of CN  and CO  at 2240,1720 cm-1 respectively. F1 and F2 are the molar fractions of (AN) and (VAc) in the copolymer respectively , M1 and M2 are the molecular weights of (AN) and (VAc) respectively.

b) The second method

This method depends on the absorbance of the recorded analytical absorption bands for CN  and CO for (AN) and (VAc) respectively, besides the molar absorptivities of the CN and CO groups according to the following equation(7).

F1 / F2 = (ACN / ACO) (εCO / εCN ) ….(3)

458

Where F1 and F2 are the molar fractions of (AN) and (VAc) in the copolymer, while εCO and εCN are the molar absorptivity of CN and CO respectively. The εCN and εCO were found to be 1.7543 and 3.2166 L.cm-1.mol-1  respectively. From the monomer feed ratio and the resultant copolymer composition, the reactivity ratios of (AN) and (VAc) were evaluated by  Fineman – Ross  and   Kelen – TüdŐs equations that are:-

Fineman - Ross

Kelen – TüdŐs

Where :

A plot of  f (F-1)/F against f2/F gives straight line, with slope = r1, and intercept= -r2.

A plot of η against ζ gives straight line the slope = r1+r2 /α  while the intercept = –r2/α  the results are presented in the following tables:-

459

%T

Fig (1) IR spectra of poly (AN – co – VAc ) , PAN and PVAc

4000       3600      3200      2800      2400        2000        1800      1600     1400        1200       1000        800         600 cm– 1

460

Table (1) IR  analysis data for determining the composition of poly (AN – co-VAc ) prepared from various  initial monomer mixture

| Copolymer | Mole Fraction of Monomer in Feed |  | IR Absorbance |  | Mole Fraction of Monomer in Copolymer |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | f1 for AN | f2 for VAc | AN | VAc | F1 for AN | F2 for VAc |
|  |  |  | CN | CO |  |  |
| A1 | 0.8295 | 0.1704 | 0.94 | 0.13 | 0.9214 | 0.0785 |
| #### A2 | #### 0.73 | #### 0.2699 | 1.33 | 0.31 | 0.87439 | 0.1256 |
| A3 | 0.6187 | 0.38129 | 0.46 | 0.16 | 0.8234 | 0.1765 |
| A4 | 0.4933 | 0.50669 | 0.378 | 0.16 | 0.7931 | 0.2068 |
| A5 | 0.351 | 0.6489 | 0.183 | 0.14 | 0.67959 | 0.3204 |
| A6 | 0.1881 | 0.8118 | 0.108 | 0.24 | 0.422 | 0.5779 |

The following table shows the values of r1 and r2: -

Table (2) : copolymerization constants r1 and r2 for poly (AN-co-VAc)

| (F-R) equation |  |  |  | (K-T) equation |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1st |  | 2nd |  | 1st |  | 2nd |  |
| r1 | r2 | r1 | r2 | r1 | r2 | r1 | r2 |
| 2.2347 | 0.0303 | 2.5341 | 0.002 | 2.3889 | 0.1038 | 2.7087 | 0.0719 |

From the values of r1 and r2 it seems that (AN) is more reactive than

(VAc) , where the macroradical prefers to add (AN) more than (VAc) .

461

Table (3) Fineman – Ross and Kelen – TüdŐs  equations parameters of poly (AN – co- VAc) in DMF  at 75oC when α1st = 0.3852  α2nd = 0.3408

| K-T Equation parameters |  | 2nd | 0.8398 | 0.7318 | 0.5943 | 0.3908 | 0.2636 | 0.1601 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 1st | 0.8397 | 0.7317 | 0.5943 | 0.39079 | 0.2636 | 0.1602 |
|  |  | 2nd | 2.11489 | 1.8578 | 1.5647 | 1.3381 | 0.681 | -0.1209 |
|  |  | 1st | 1.8523 | 1.6128 | 1.34249 | 1.138 | 0.5463 | -0.1866 |
| F-R Equation parameters | f(F-1)/F | 2nd | 4.5007 | 2.3608 | 1.3147 | 0.7487 | 0.3152 | -0.0491 |
|  |  | 1st | 4.4531 | 2.3161 | 1.2747 | 0.7196 | 0.2858 | -0.0856 |
|  | f2/F | 2nd | 1.7873 | 0.9299 | 0.4994 | 0.2187 | 0.122 | 0.065 |
|  |  | 1st | 2.0188 | 1.0508 | 0.5643 | 0.2471 | 0.1379 | 0.0735 |
| F=F1/F2 |  | 2nd | 13.2576 | 7.8663 | 5.2713 | 4.3316 | 2.3966 | 0.825 |
|  |  | 1st | 11.7375 | 6.9617 | 4.6651 | 3.8351 | 2.121 | 0.7302 |
| f=f1/f2 |  |  | 4.8679 | 2.7047 | 1.6226 | 0.9735 | 0.5409 | 0.2317 |
| Copoly-mer |  |  | A1 | A2 | A3 | A4 | A5 | A6 |

462

f(F-1)/F

f2/F

The following figures show the Plots of Fineman – Ross and Kelen – TüdŐs  equations for first and second method :

Fig (2) A plot of (F-R) ( 1st method ) for the copolymer

(AN – co – VAc)

η

ζ

Fig (3) A plot of (K-T) ( 1st method ) for the copolymer

(AN – co – VAc)

f2/F

f(F-1)/F

Fig (4) A plot of (F-R) ( 2nd  method ) for the copolymer

(AN – co – VAc)

463

η

ζ

Fig (5) A plot of (K-T) ( 2nd  method ) for the copolymer

(AN – co – VAc)

3-2 copolymerization behavior

We can predict the copolymer type (alternate, random or block) from

the product (r1r2) The values of this product are summarized in table (4 ) :-

Table (4) the values of  (r1r2) for poly(AN-co-VAc)

| r1r2 |  |  |  |
| --- | --- | --- | --- |
| (F-R) equation |  | (K-T) equation |  |
| 1st | 2nd | 1st | 2nd |
| 0.0677 | 0.005 | 0.2479 | 0.1947 |

According to these values, the nature of the copolymer sequence of poly (AN-co-VAc) system is tending to alternate since the product r1r2 closer to zero, so there is a greater tendency for (AN) and (VAc) to alternate in the copolymer poly (AN-co-VAc) due to big differences in polarity between the two monomers which leads to a transition state stabilized by resonance

464

which prefer to add either of the two monomers by the same preference.

Depending on the experimental values of rAN and rVA, the values of Q and e for each monomer were calculated and found as follows: for AN, Q= 0.539,         e = 1.67, for VA, Q= 0.0339, e= -0.189 these values are in good agreement with values in literature(8). The copolymer

composition (F1) vs initial composition (f1) (fig 6), shows no resemblance between the feed and the copolymer compositions. From the values of  rAN  and rVA  one can deduce that AN is more reactive than VAc to go into copolymer.

This behavior can be explained on the basis that AN radical is more stable than VAc radical so the growing  macroradical prefer to add to AN more than VAc.

f1

F1

Fig (6) The relation between mole fraction of acrylonitrile in feed (f1) and in copolymer (F1).

Finally, we can conclude that the two methods for reactivity ratio measurement used in the present work are good methods for prediction of copolymer composition and reactivity ratios.

465

References :

1- Baharmi, S. K; S. Bajaj, S.H. in High performance Acrylic Fibers, in J.M. S. Review of Macromolecular chemistry and physics Marcel Dekker Inc.; New York,1996,36,1-7 .

2- Herman F.M ; Norman G.G, “Encyclopedia of polymer Science and Technology”, vol. 6, John Wiley and Sons Inc., New York, (1967).

3- Herman F.M, Norman G.G, “Encyclopedia of Polymer Science and Technology”, vol. 1, John Wiley and Sons Inc., New York, (1985).

4- Herman F.M, Norman G.G, “Encyclopedia of polymer Science and Technology”, vol. 4, John Wiley and Sons Inc., New York, (1960).

5- Ajaib S. B., Rajeev K., Eur. Polym J.,2001, 37,1827 .

6- Nursel P., Nureltin S., Olgan G., Zakir M. O. Rzaev, Eur. Polym. J., 2001, 37, 2443 .

7- Gan L.H., Roshan G.D.,  GanY.Y., Eur. Polym. J.,1998, 34, 33 .

8- Brandrup J., Imnergut E.H., and Gruke E.A., "Polymer Handbook" wiley interscience, New York 1999.

466