Synthesis  and Characterization of Imine-Azo Polymer Ligands Derive a from Azo compounds , Acetylacetone and Amines and Their Metal Complexes with (Mn+2,Ni+2,Zn+2)

Nagham Mahmood Aljamali                      Huda Sabah               Jihan Razzaq

Dr.Nagham_mj@yahoo.com(to corresponding).

Chem.Dept., College of Education ,Univ.Kufa.

(NJC)

(Received on 23/6/2013)            (Accepted for publication 23/2/2014)

Abstract :

In this work, series of compounds (ligands and polymers) were synthesized from reaction of azo compound with acetylacetone to produce compound diimine azo [NAP], which reacts with (4-aminoethoxy aniline, 2-amino thiophene ,2-amino thiazole , 4-amino benzamide) to produce four ligands [MAP , TAP, PAP, BAP] respectively . The ligand (TAP)  was reacted with (Mn2+,Ni2+,Zn2+)to form metal complexes the optimal conditions of complexes (stoichiometric study , mole ratio, job method ,pH ,concentration of metals and ligand ,molar conductance), were also studied All ligands and complexes and were tested for antibacterial and antifungi activity.All ligands with complexes were characterized  by ( 1H.NMR–spectra ,FTIR–spectra (CHN)-analysis) , Sehiff base .

Keyword: polymer-of-polyester ,schiff-ligand, complexes

الخلاصة :

تضمنت الدراسة تحضير سلسلة مركبات ( ليكاندات وبوليمرات) من تفاعل مركب آزو مع الأسيتايل أسيتون  ليُنتج مركب ثنائي إيمين-أزو[NAP]  والدي بدوره يتفاعل  مع ( 4-ميثوكسي أنيلين , 2-أمينوثايوفين ,2-أمينو ثيازول , 4-أمينو بنزامايد ) لينتج ليكاندات[BAP, PAP, TAP ,MAP]  على التوالي .المركب  (TAP) أُسُتخدم كليكاند مع أيونات  (Mn2+,Ni2+,Zn2+) لتكوين معقدات ودراسةالظروف المثلى لتعقيدها ( تكافؤية المعقدات, النسب المولية, طريقة جوب , الدالة الحامضية ,تركيز الليكاند وألأيونات ,التوصيلية المولارية ), مع تحضير بوليمرين . جميع الليكاندات المحضرة مع المعقدات والبوليمرات دُرست فعاليتها البكتيرية والفطرية وكذلك ,شُخصت بتقنيات ( طيف الاشعة تحت الحمراء, طيف بروتون  الرنين النووي المغناطيسي ,التحليل الدقيق للعناصر) ودرجات الانصهار.

كلمات مفتاحية :بوليمربولي أستر ,ليكاند شيف ,معقدات.

Introduction:

The synthesized imine-azo in the present study are containing two imine groups which linked with azo-group and the hetero cyclic compounds bearing (imine-azo) in their structure have many applications in Biological science. These compounds were clinically known and have a wide range of bio activities such as antibacterial drugs (1,2),in synthesis of polymers(3,4), heterocyclic compounds (5,6) have applicatioons in several fields (7-10) which due to several methods for preparing imine compounds in literature , but the method which is carried out through condensation reaction of carbonyl compounds with primary aromatic amine is most used are chelating ligands in coordination chemistry ,they are also useful in catalysis and in medicine , the utility of schiff bases lay in their usefullness as synthons in the synthesis of bioactive molecules, schiff  bases belongs to a widely used group of organic intermediates important for production compounds as a ligand with transition metals to form complexes (11-13) and in synthesis of several polymers

Polyesters represent a class of polymers which contains the ester functional group in their main chain. Although polyesters do exist in nature (natural polyesters have been known since around 1830), the term polyester generally refers to the large family of synthetic polyesters (resins), which includes polycarbonates and polyethylene terephthalates (PET) (14-16).Polyesters are widely used materials with diverse applications (fibers, plastics and coatings). They are strong, colorfast, and resistant to corrosion and chemical attack. In general they have extremely good mechanical properties and are heat resistant .

Measurements  :

-All chemical used were supplied from Fluka and Merck-chemical company.

-All measurements were carried out by :

*Melting points :Electro thermal 9300 ,melting point Engineering  LTD ,U.K .

*FTIR-spectra:  fourrier transform infrared shimadzu (8300) ,(FTIR), KBr-disc was used .

*1H.NMR-Spectra in DMSO-solvent ,in ppm unit, and (CHN)-Analysis.

*Otuclave ,oven ,incubator in biology department ,college of education in kufa university.

Preparation of  ligands [ (NAP),(MAP) , (TAP), (PAP), (BAP) ]:

The ligand [(NAP) , (MAP), (PAP), (BAP)] prepared accordinds to procedure (5,17) , (13.8 g) of 4-nitro aniline disolved in (3ml) hydrochloric acid at (0-5)C ,(0.7 g) of sodium nitrite solution added to give diazonium salt, then (5 ml) acetylacetone added to the mixture yiled (4.5g , 0.01 mole) of [NAP]. The product was mixed individually  with [(0.02mole ,2.4g of 4-methoxy aniline) , (0.02mole ,1.8g of 2-amino thiophene),(0.02mole , 2g of 2-amino thiazole),(0.02mole ,2.6g of 4-amino benzamide)] respectively in presence of absolute ethanol  refluxing for (6-9)hrs .The precipitate was filtered and recrystallized to yield (87, 82,89 ,85)% of  [(MAP), (PAP) ,(TAP) ,(BAP)] respectively .

[MAP] : 3-(4-nito benzene azo)-2,4-bis (4-methoxy phenyl imine)-pentane .

[PAP] : 3-(4-nito benzene azo)-2,4-bis (2-thiophene imine)-pentane .

[BAP] : 3-(4-nito benzene azo)-2,4-bis (4-benzamide imine)-pentane .

[TAP] : 3-(4-nito benzene azo)-2,4-bis (2-thiazole imine)-pentane .

Preparation of complexes of ligands (TAP)with (Mn2+,Ni2+, Zn2+):

The complexes prepared according to procedure (5): hot ethanolic solution(5ml) of the metal halide (Mn2+,Ni2+, Zn2+)respectively with ethanolic solution of ligand (TAP) in (1:1) (ligand: metal) molar ratios were mixed ,respectively. After stirring for (2hrs) , precipitates formed , the solids were filtered ,dried , recrystallized from absolute ethanol to give complexes (Mn2+,Ni2+, Zn2+) respectively .

Preparation of  Polymers  [A] and  [B] :

The reaction was carried out in a 100 ml round bottom flask and fitted with a reflux condenser and thermometer. phthalic anhydride (0.1805 g, 0.0244 mole), maleic anhydride (0.073 g,0.015mole), 4(4-hydroxy phenyl)-imine phenol  (0.023 mole) were dissolved in 10 ml of acetone followed by addition zinc chloride (0.1662g , 0.0244 mol) of as catalyst . The mixture was heated to 60˚C with a continuous stirring for 6 h . The solution allowed cool to room temperature and the polymer dried after evaporation of solvent

Polymer  [A]

Polymer  [B]

Results and discussion :

This study involved ,synthesis ,characterization ,bio- chemical studies of structure of four ligands and two complexes with ligand (TAP) and study of optimal conditions for formation of complexes .all compounds were characterized by different methods :

Study of optimal condition :

The optimal conditions for formation of complexes were studied in this work . The optimal concentrations were found  to be ; TAP-ligand: (1x10-3M ) , Mn2+: 0.9x10-4  , Ni2+:   0.7x10-4  , Zn2+: 0.9x10-4  M . while the optimal pH was 7 .Figures(1-3) ,show that stochiometric of the prepared complexes (M:L) are (1:1) which measured by the molar conductance measurements .Table (1) shows melting points, molar conductance , λ max and the elemental analysis of the prepared ligands   and complexes.

The I.R -spectra of the prepared  ligands, shows bands: at  (1482-1492)cm-1 due to azo group (-N=N-)    (1610-1620)cm-1 assigned to imine(14) group (-CH=N) in ligands .The later showed ashift towards longer wave number (1635-1676) cm-1 due to complexation  of ligand TAP with (Mn2+ ,Ni2+   and Zn2+) ions via N-atom of azomethine group (CH=N). Appearance of bands at (439-472 ) cm-1 and (518-522) cm-1 are conform the coordination(15)  to nitrogen and oxygen atoms.Bands at (1667 and 1676) cm-1 in are attributed to imine group(17,18)  of polymers [A] and [B]. These data are summarized in Table (1) and showing in Figures (4-12).

The 1H.NMR-spectra  shown in polymers [A] and [B] show  signals at δ (8.65 -8.81) due to the  proton of azomethine(5,17) group ,doublet signals at δ (2.34 -2.44) due to protons of  (-CH2=CH2-COO-)  in polymer [A], and signals  at δ (6.93 -6.62) assigned to phenyl group in the two polymers ,figs (13and 14).

The suggestion Figures of complexes:

Structurally ,the above data indicate that NAP, MAP ,TAP, PAP and BAP are bi dentate ligands and TAP is coordinated to (Mn2+ ,Ni2+   and Zn2+) ions via N-atom of azomethine and thiazole group to form a tetrahedral complexes(2,6 ) .

Antimicrobial tests :

The antimicrobial activity of the prepared ligands and complexes against bacteria (staphyllococcus .aureus) and fungi (Aspergillus niger) were  studied using  holes  methods(17-20) ,the TAP -Mn2+ ,Ni2+, Zn2+  complexes  exhibited at (1x10-3)M concentration     higher activity towards bacteria  than fungi , as shows in Table (3).

Data in Table (3) shows that those complexes are more active compared to the ligands .This attributed to the presence of metal  while may be increase the breakage and penetration of bacterial cell wall.

Table(1): Melting point, Molecule Formla and Element analyses

| Compounds | M.p(c°) | Ώ-1.cm-1. mol-1 Molar conductance (DMSO - Solvent) | λmax | Calc ./ found |
| --- | --- | --- | --- | --- |
|  |  |  |  | C% | H% | N% | M% |
| C11H11O4N3 (NAP) | 190 | -- | 356 | 53.01 52.91 | 4.41 4.34 | 16.86 16.66 | / |
| C25H25O4N5 (MAP) | 202 | -- | 365 | 65.35 65.26 | 5.44 5.30 | 15.25 15.17 | / |
| C19H17O2N5S2 (PAP) | 210 | -- | 360 | 55.47 55.35 | 4.13 4.06 | 17.03 16.97 | / |
| C25H23O4N7 (BAP) | 207 | -- | 380 | 61.85 61.67 | 4.74 4.62 | 20.20 20.11 | / |
| C17H19O2N7S2 (TAP) | 220 | -- | 388 | 48.92 48.88 | 4.55 4.40 | 23.50 23.37 | / |
| C17H19O2N7S2 [Mn(TAP)] | 245 | 7.52 | 440 | 43.31 43.19 | 4.03 4.06 | 20.80 20.64 | 11.64 11.67 |
| C17H19O2N7S2 [Ni(TAP)] | 250 | 8.13 | 455 | 42.88 42.76 | 3.99 3.83 | 20.63 20.51 | 12.34 12.36 |
| C17H19O2N7S2 [Zn(TAP)] | 240 | 7.34 | 450 | 42.29 42.20 | 4.43 4.32 | 20.31 20.17 | 15.67 15.61 |

Table (2):FT.IR data (cm-1) of the prepared ligands, complexes and polymers.

| Compounds | Name of compounds | Only (Importance groups) |
| --- | --- | --- |
|  |  | (CH=N) Imine | (-N=N-) | (M-N), (M-O) |
| (NAP) | 3-(4-nitro phenyl azo)-2,4-dione-pentane | --- | 1492 | --- |
| (MAP) | 2,4-(bis(4-methoxy phenyl imine))-3-(4-nitro phenyl) azo pentyl | 1618 | 1490 | --- --- |
| (PAP) | 2,4-(bis(2-thiophene imine))-3-(4-nitro phenyl) azo pentyl. | 1620 | 1482 | --- |
| (BAP) | 2,4-(bis(4-benzamide imine))-3-(4-nitro phenyl) azo pentyl | 1620 | 1490 | --- |
| (TAP) | 2,4-(bis(2-thiazole imine))-3-(4-nitro phenyl) azo pentyl | 1610 | 1489 | --- |
| [Mn(TAP)] | Complex | 1644 | 1510 | 439 518 |
| [Ni(TAP)] | Complex | 1635 | 1489 | 472 518 |
| [Zn(TAP)] | Complex | 1647 | 1515 | 465 522 |
| Polymer[A] | Polymer | 1676 | ---- | --- |
| Polymer[B] | Polymer | 1667 | ---- | --- |

Table (3): biological activity of (1x10-3)M of ligands and complexes

| Compounds | Zone of Inhibition |
| --- | --- |
|  | Bacteria staphyllococus. Aureus | Fungi Aspergillus |
| (NAP) | 10 | 6 |
| (MAP) | 12 | 8 |
| (PAP) | 16 | 12 |
| (BAP) | 14 | 11 |
| (TAP) | 18 | 14 |
| [Mn(TAP)] | 27 | 21 |
| [Ni(TAP)] | 27 | 22 |
| [Zn(TAP)] | 29 | 26 |

Fig(1) :Mole ratio method and Various continuous method   of  ATP- Mn2+ complex

Fig(2) :Mole ratio method and Various continuous method   of  TAP- Ni2+ complex

Fig(3) :Mole ratio method and Various continuous method   of  TAP- Zn2+ complex

Fig(4):FTIR- of compound [ NAP]

Fig(5):FTIR- of compound [ MAP]

Fig(6):FTIR- of compound [PAP]

Fig(7):FTIR- of compound [ BAP]

Fig(8):FTIR- of compound [ TAP]

Fig(9):FTIR- of complex  [Mn (TAP)]

Fig(10):FTIR- of complex  [Ni (TAP)]

Fig(11):FTIR- of complex  [Zn (TAP)]

Fig(12):FTIR- of polymer  [A]

Fig(13):FTIR- of polymer  [B]

Fig(14): 1HNMR- of polymer  [A]

Fig(15): 1HNMR- of polymer  [B]

Referencese :

- Cezar .S ,Maria . P and cristian .T., Turk .J.Chem .,2008, 32,487 -493.

- Nida .I ,Javed .I and Muhamed  . I ., J.Sci .Res .,2009, 9 ,1,(2009) .

- Javed .I,sharfuddin . S,Muhamad .I and Latif .S ., Turk .J.Biol .,2006,30,1-4.

- Raveen .R and Pal .S .,J.oxganometallic .Chem .,2007,692,824-83.

- Nagham .M .Aljamali ., Pharm . INN.J .,2012,(1,12) ,64-71 .

- Vladimir .A,Alexander .D ,lidiya .L, Vladimir . P,Igor . D ,Evgenii . N and Alexey . T ., Arkivoc.,2005,7,60-66.

- Arifuzzaman . M ,Rafiya .K and Rabiul .  M ., Bangladesh . J.Pharmacol.,2009, 4,96 -100.

- Raman . N ,Muthuray . V ,Ravichandran . S and Kulandaisamy . A .,Proc . Indian . Acad . Sci .(chem .Sci ).,2003, (115,3),161.

- Reyna . R,Rocio . M ,Jorge .A ,Herbert . H and Hugo.T.,Arkivoc,V., 2008,19-30.

- Rezvani . Z, Leili . R , Kamellia . N and Seyed . M .,Acta . Chem . Slov.,2004,51,675-686 .

- Anand . G ,Simi.K ,Venkatraman . S and Tavarekere .K ., Proc .Indian . Acad .Sci .,2003,115 ,711-720 .

- Amanda .J ,Joseph . K ,Federico . E,Yan . A and Mark . J ., J.Org .Chem .,2005,70,7936-7946.

- Handong.Y and Hong .L .,J.Org.Met.Chem.,2012,713,11-19  .,cited by IVSL*.

- Van B. R.; Van H.E. A.; van der S.C., Handbook of Thermoplastics, Marcel Dekker Ed. (1997).

- Young, R. J.; Lovell, P. A. Introduction to Polymers, Chapman and  Hall 2nd Ed. (1991).

- Maya Ziari , Ph.D. Thesis ,Technical University Eindhoven, (2009).

- Nagham .M.Aljamali., Pharm. INNJ.,2013,(1, 11), 73-79.

- Nagham. M. Aljamali., J. AlQadisya .Sci, 2005,(10, 1), 131-138.

- Asiri.A and Badahdah . K ., Molecules  2007, 4 .12 .

Cumhur . K , Murkat . K , Suleyman . S and seher . G ., T . J . Chem .,2009, 33,375-384.