Effect of EPDM Structure on the Properties of Babylon Tire Black Sidewall Compound

##### Mohammed Ali Mutter

Department of Chemistry, College of Education, University of Al-Qadisiya

(NJC)

# (Received on  6 / 4 /2005)		(Accepted for publication on  28/ 9 /2005)

# Abstract

The tire black sidewall is the outer surface that protects the casing against weathering. It is formulated for resistance to weathering, ozone aging, abrasion, tearing and cracking, and for good fatigue life by using blends of natural rubber and cis-1.4- butadiene rubber.

The tire black sidewall uses blends of natural rubber and cis-1.4-butadiene rubber are used to achieve desired physical properties; however, use of these elastomers requires protection against ozone aging in order to maintain desirable properties over the lifetime of the tire. Protection against ozone aging is of particular interest since reaction with these olefinically unsaturated elastomers results in polymer decomposition via chain scission. Ethylene propylene diene terpolymer has proved most effective. However, its use also results in a surface discoloration, and thus it can be used in sidewall compound when the tire appearance is also an important factor.

The best formulations are obtained in the presence of 40,50 phr EPDM to achieve desired physical properties. Improved ozone resistance was obtained by using 40 and 50 phr of EPDM rubber in the compound there is no cracking throughout the life of the black sidewall compound. Blends of NR/BR/ EPDM with up to 50 phr of EPDM rubber afforded adhesion levels greater than that of a natural rubber model sidewall. Compounds containing NR /BR/ EPDM blends with 2 phr of the 6PPD antiozonant provided the best dynamic ozone resistance.

Blending of EPDM with NR and BR enhances the abrasion resistance. However, elongation at break and tear strength values are highest for those compounds having high contents of NR and Butadiene rubber.

# الخلاصة

يمثل الجدار الجانب من الإطار السطح الخارجي الذي يحمي الإطار من العوامل الجوية. وهو مصمم لمقاومة تلك العوامل كالظروف الجوية، والتقادم الأوزوني، والقشط، والتمزق، والتشقق، كما يساعد في الحصول على إجهاد أفضل للإطار باستخدام مزائج من المطاط الطبيعي والمطاط البيوتاديين-1,4 -cis  وللحصول على الخواص الفيزياوية المطلوبة.

على أية حال أن استخدام هذه المطاطات المرنة  يتطلب الحماية ضد التقادم الأوزوني وذلك للمحافظة على الخواص المرغوبة طيلة فترة الحياة. حيث تكتسب تلك الحماية أهمية خاصة لأن التفاعل مع المطاطات المرنة الغير مشبعة الاوليفينية يؤدي إلى تحلل البوليمر  من خلال قص الأواصر. وقد أثبت بوليمر Ethylene propylene diene الثلاثي كفاءة جيدة مقارنة بغيره من البوليمرات ألا أن استخدامه يؤدي أيضا إلى عدم فقدان لون السطح ولذلك يمكن استخدامه في عجنة جدار الجانب عندما يكون مظهر الإطار عاملا هاما أيضا. ويمكن الحصول على أفضل الصيغ بوجود 40،50phr  من EPDM للحصول على الخواص الفيزياوية المرغوبة. كما أمكن تحسين المقاومة للأوزون باستخدام 40و 50phr من  EPDMفي العجنة.

وقد وجد أن مزائج EPDM/NR/BR مع ما يصل إلى 50  phrمن المطاط EPDM يعطي مستويات تماسك أفضل من تلك الموجود في جدار الجانب للمطاط الطبيعي من حيث أن العجنات الحاوية على مزائج EPDM/NR/BR مع2 phr من مضاد الاوزنة 6PPD أعطى أفضل مقاومة حركية للأوزون.

ومن جهة أخرى يؤدي مزج EPDM مع NR وBR إلى تحسين مقاومة القشط. ألا أن الاستطالة وقوة التمزق تكون هي الأعلى في حالة العجنات التي تحتوي على محتويات عالية من NR ومطاط البيوتاديين.

# Introduction

The tire is a high performance polymeric composite of many rubbery compon-ents consisting of a tread area which includes the tread, base and cushion compounds; and the casing which includes the bead, carcass plies and belts; and the side wall;inner liner apex and chafer compounds.1 Each component serves a specific and unique func- tion, synergistically to produce the desired performance. The black sidewall is the outer surface of the tire between its beads that protects the casing against weathering. It is formulated for resistance to weathering, ozone, abrasion, tear, radial, and circumfe-retial cracking, and for good fatigue life2. A blend of natural rubber butadiene rubber is generally used in the sidewall along with carbon black, curatives and a high concentration of antidegradants to provide weather resistance3. Protection of the tire from ozone aging is of particular interest since the reaction of ozone with elastomers having olefinically unsaturated backbone structures, such as natural rubber and butadiene rubber, results in scission of the polymer chain, as described in the reviews by Rhee, Lattimer and Layer,4 Layer and Lattimer,5 and Kuczkowski6. The most prevalent approach to achieveing a high- gloos black sidewall over the life of a tire is to use an inherently ozone-resistant, saturated-backbone polymer in blends with a diene rubber. The ozone-resistant polymer must be used in sufficient concentrations and also be sufficiently dispersed to form domaims that  effectively block the continuous propagation of an ozone-initiated crack through the diene rubber phase withen the compound. Elastomers such as ethylene-propylene-diene terpolymers, halogented butyl rubbers, or brominated isobutylene-co-para-methylstyrene elastomers have been used in conjunction with natural rubber and/ or butadiene rubber7.

High unsaturation ethylene- propylene-diene (EPDM) elastomers contain nonconjugated dienes affording carbon-carbon double bonds pendant to the backbone chain of the polymer which is completely saturated. As a result of this chemical struc-ture, EPDM rubber is characterized by its excellent heat, ozone, and weathering resistance; good low temperature flexibility and accepted cure characteristics8. EPDM polymers are generally described by ethylene/ propylene ratio, diene type and level, and molecular weight and distribution. Shulman9 has reviewed some of the uses of EPDM rubber, which include automotive parts (hoses, tubing), weather-strip (sponge, window channel), appliance parts, roof sheeting, and tire white sidewalls.

###### SCHEME 1 Ethylene-propylene-diene rubber

Sandstrom and Lal10 reported using EPDM rubber in a natural rubber/ butadie-ne rubber black sidewall composition along with a rubbery aloha-olefin interpolymer and various chemicals. Botzman11 reported use of an EPDM polymer modified with chlorothio-sulfonmide in order to improve crosslinking with the diene rubber. Von Hellens, Mohammed and Hallman12 reported that use of a high molecular weight EPDM rubber having an ethylene:propylene weight ratio of 47:26, a 9.5 weight percent ethylene nor- bornene (ENB) content, and being extended with 100 parts by weight of naphthenic oil  (EPDM5875) afforded improved compound aged fatigue life, dynamic ozone resistance, and higher resilience while maintaining excellent hot adhesion levels compared to an industrial natural rubber / butadiene rubber control sidewall. Von Hellens, Edwards and Lobos13 studied the adhesion of EPDM rubber –containing tire black sidewalls to a N550 carbon black –filled natural rubber cacass compound. Use of 10-40 phr of a 100 parts-by—weight oil-extended, high molecular weight and high non-conjugated diene (ENB)-content EPDM rubber (EPDM 5875) in blends with natural rubber and butadiene rubber eliminated the problem of poor adhesion to a carcass compound that was previously associated with use of EPDM rubbers.Neither high molecular weight, nor high non-conjugated diene content alone provided a satisfactory level of adhesion. Gorkina, Goncharova and Nikolaeva14 studied the same oil-extended, high molecular weight, high non-conjugated diene EPDM rubber (EPDM HMW / NO). They reported difficulties with processing rubber mixes (lower adhesion and cohesion), migration of oil to the surface of mixes, and also limited scope for varying the formulation factors. Use of the experimental non-oil extended, high molecular weight, high non-conjugated diene-content EPDM rubber afforded better compatibility with polyisoprene and resulted in improved crack growth resistance, heat resistance and stability. However, use of this EPDM rubber also gave a lower tear strength compound than that of the standard polyisoprene / polybutadiene (50 / 50) black sidewall.

In this paper, we have studied the use of inherently ozone-resistant polymer

(EPDM) to protect the natural rubber and butadiene rubber of conventional black sidewall compounds has been a successful technique. Ethylene-propylene-diene terp-olymer blended with natural rubber and / or butadiene rubbers have received consider-able attention. Adhesion to carcass compounds, aged fatigue life and dynamic ozone

resistance have been improved using EPDM rubber.Mixing of the elastomer blend is

an important variable in order to minimize the EPDM rubber and diene rubber dom-ains and also to control the carbon black distribution in the natural rubber phase.

# Experimental

## Materials

The polymers used as a matrix in this study are NR (SMR 20), BR-CIS and POLYSAR EPDM 345 is a terpolymer of ethylene, propylene and a non conjugated diene.The N-(1,3-Dimethylbutyl)-N- phenyl-P-phenylenediamine (6PPD) was used an antiozonant to be compared with EPDM (ozone resistant).

### Preparation on of the Rubber Compounds

Eleven rubber compounds with different loading amounts of EPDM were pre-pared. For rubber compounding, we used a laboratory mill: rolls dimensions are: outside diameter 150mm, working distance 300mm, speed of the slow roll 24 rpm and gear ratio 1.4.Compound recipes are summarized in Table 1 . After mixing, the compounds were carefully remilled into flat sheets on a two-roll mill.

Rheocurves were recorded using a Monsanto Rheometer ODR 200 at 160 C°. the t90 time, which denotes the time for 90% cure, and the maximum torque were determined from the rheographs.

When possible, standard ASTM tests were used to determine the cured compound physical properties. Sress / strain properties (tensile strength, elongation at break, modulus values,) were measured at room temperature using a tensometer 10.

Shore A hardness was measured at room temperature by using a Zwick duromatic. Abrasion loss was determined at room temperature by weight difference by an APH40 abrasion tester with rotating sample and rotating drum. Ozone aging of dumbbell specimens was accomplished according to ASTM D-395-82 by using an Orec Environmental Chamber at 40C° with samples undergoing cyclic deformation to 25 % elongation while being exposed to 50 pphm of ozone.Thermal aging of dumbbell specimens was accomplished at 70C° for 7 days. Adhesion to carcass was accomplis-hed at 100 C°.

### TABLE 1: RECIPES OF SIDEWALL COMPOUND WITH VARIOUS EPDM LOADING

Ingredients 1 2 3 4 5 6 7 8 9 10 11 phr phr phr phr phr phr phr phr phr phr phr

NR 50 30 50 60 50 10 - 50 60 50 80 BR-CIS 50 30 10 - - 50 50 40 20 30 - EPDM (345) - 40 40 40 50 40 50 10 20 20 20 Zinc oxide 5 5 5 5 5 5 5 5 5 5 5 Stearic acid 2 2 2 2 2 2 2 2 2 2 2 Sulfur 2.3 2.3 2.3 2.3 2.3 2.3 2.3 2.3 2.3 2.3 2.3 MBSa 0.8 0.8 0.8 0.8 0.8 0.8 0.8 0.8 0.8 0.8 0.8 6PPDb 2.4 - - - - - - - - - - Aromatic oil 10 10 10 10 10 10 10 10 10 10 10 HAF N326 50 50 50 50 50 50 50 50 50 50 50

a: N-morpholinothio – benzothiazole

b: N- 1,3 dimethylbutyl – N/ phenyl – p - phenylenediamine

Results and Discussion

### Cure Properties

The levels of the three ingredients (sulfur, zinc oxide,MBS ) used to cure the EPDM black sidewall compound were established via statistically designed experiments in order to afford a compound with a T90 cure time at 160 C° of 10-12 minutes, good scorch safety and no reversion. The cure property data of the EPDM elastomer evaluated in this study are shown in Table 2. Inspection of the data shows that there are small variations in these cure properties. Maximum torque values are the highest and scorch values are the lowest for those sidewall compounds having EPDM elastomer.

### TABLE 2: SIDEWALL COMPOUND CURE PROPERTIES

Compound 1 2 3 4 5 6 7 8 9 10 11 ML, ib-in 4.93 5.52 4.10 3.90 3.78 5.33 5.86 3.89 3.04 3.54 3.25 MH, ib-in 29.45 31.04 27.12 29.56 27.82 33.31 37.48 28.20 29.65 31.33 24.8 T52a, min. 1.15 1.14 1.12 1.06 1.02 1.17 1.17 1.06 1.01 1.01 1.00 T50, min 1.80 1.65 1.56 1.46 1.48 1.89 1.97 1.57 1.42 1.46 1.39 T90b, min. 2.49 2.53 2.65 2.83 1.35 2.87 3.32 2.72 2.92 2.45 2.98

a: Time required for 52% cure .

b: Time required for 90% cure .

Physical Properties of Sidewall Compound Containing EPDM Rubber

Tensile properties. Cured EPDM black sidewall compound physical property data are shown in table 3. Inspection of the data shows large variations in many of the properties. In particular, tensile strength (13.231 -19.571MPa), elongation at break (339-583%) and tear strength(6.895-11.351MPa ) values vary widely. Tensile strength values are lowest for those compounds having high EPDM content, see compounds2,3,4,5,6 and 7. However, elongation at break and tear strength values are highest for those compounds having high contents of NR and Butadiene rubber, see compounds 1, 8,9,10 and 11. EPDM rubber in blends with NR and butadiene rubber in black sidewall compounds showed improved resistance in abrasion.

### TABLE 3: EPDM SIDEWALL COMPOUNDS PHYSICAL PROPERTIES

Compound 1 2 3 4 5 6 7 8 9 10 11 Hardness, Shore A 56 60 58 59 59 60 61 58 60 58 55 Elongation, % 487 339 410 454 448 388 379 583 546 525 466 Tensile strength, 17.9 13.99 15.71 16.975 16.415 14.318 13.231 19.571 18.991 18.645 17.524 Mpa 100 % modulus, Mpa 2.433 2.253 2.310 2.323 2.311 2.289 2.111 2.860 2.793 2.647 2.415 200 % modulus, Mpa 5.446 5.025 5.185 5.421 5.354 5.226 4.446 5.910 5.830 5.720 5.433 300 % modulus, Mpa 9.889 7.356 8.205 9.567 9.471 8.154 7.225 11.323 10.541 10.471 9.779 Tear strength, Mpa 9.638 6.895 7.832 8.283 9.214 7.548 6.658 11.351 10.615 10.587 9.562 Abrasion resistance % 0.266 0.316 0.414 0.461 0.443 0.156 0.921 0.223 0.389 0.276 0.475

### Effect of Aging on Sidewall Physical Properties

The effect of aging on the physical properties of sidewall compounds containi-ng different loading of EPDM is illustrated in Table 4. It can be seen that compounds containing EPDM showed characteristically good retention of tensile strength, but rapid loss of extensibility after 7 days of aging. This may be due to the fact that main chains of the EPDM have no double and thus EPDM does not suffer deterioration due to molecular scission even after extended exposure to heat. On further aging, hardness increases and reaches high values after 7 days. This may be related to the increase in the crosslink density. The sources to cause the increase of crosslink density are the formation of new crosslinks between polymer chains. The new crosslinks are formed by the reaction of curing agents remaining in the vulcanizates and the combination reaction of the pendent sulfide groups.

### TABLE 4: EFFECT OF AGING ON SIDEWALL PHYSICAL PROPERTIES

Compound 1 3 7 8 9 Aged 7 days at 70 C° Hardness, Shore A 66 67 68 69 70 Elongation, % 301 356 373 327 289 Tensile strength, Mpa 13.804 15.207 13.160 17.177 17.794 100 % modulus, Mpa 3.392 2.916 3.343 2.968 2.860 200 % modulus, Mpa 7.899 6.331 7.544 3.310 6.858 300 % modulus, Mpa 13.648 9.982 10.953 11.857 11.768

### Effect of EPDM on Dynamic Ozone Resistance and Adhesion to  Carcass

Table 5 illustrates the effect of EPDM on dynamic ozone resistance and adhesion to carcass of sidewall compounds containing different loads of EPDM. Ozone resistance depended on the level of the EPDM rubber, ozone resistance also depended on good mixing of the EPDM rubber with natural rubber in order to achieve a polymer domain size of less than one micron, otherwise cracking can be severe. However, improved ozone resistance occurred at the expense of reduced cut growth resistance. Improved ozone resistance was obtained by using 40 and 50 phr of EPDM rubber in the compound there is no cracking throughout the life of the black sidewall compound. The adhesion mechanism involves the creation of radicals when long chains of EPDM rubber and natural rubber are broken down by shear and mechanical work. Grafting between the two elastomer is believed to occur. The graft polymer is thought to act as a compatibilizer15. Blends of NR/BR/ EPDM with up to 50 phr of EPDM rubber afforded adhesion levels greater than that of a natural rubber model sidewall.

### TABLE 5 : EFFECT OF EPDM ON DYNAMIC OZONE AND ADHESION TO CARCASS OF SIDEWALL COMPOUNDS

## Compound 1 2 3 4 5 6 7 8 9 10 11 Dynamic ozone, 50 pphm, 25 % ext., 40C° after 72 continous hours Cracking ratinga b OK OK OK OK OK OK S VS VS VS Adhesion to Carcass @ 100C° Adhesion, KN/ m c 24.6 25.8 26.3 26.9 24.7 26.6 19.6 21.3 20.5 22.2

a  OK-no cracks; VS-very slight cracks; S-slight cracks.

## b  Broke @ 72 hours

## c  Test simple slipped out of one the grips

### Effect of Antiozonant on EPDM-Sidewall Properties

In order to protect the tire black sidewall from cracking, chemically reactive antiozonants are generally added to sidewall formulation at levels tested for effective- ness under both static and dynamic conditions16. N-1,3- Dimethylbutyl,-N-phenyl-para- phenylenediamine is presently the most widely used chemical antiozonant. It is known by the name 6PPD. However, para-phenylenediamine antiozonants are highly staining and discoloring materials, and therefore can only be used in limited amounts where tire black sidewall appearance is also an important factor. 6PPD mixed with the natural rubber and butadiene rubber to form a masterbach followed by blending with the EPDM rubber and other ingredients, afforded the most effective processing in order to protect the natural rubber phase. Compounds containing NR /BR/ EPDM blends with 2 phr of the 6PPD antiozonant passed all of the requirements of the tire black sidewall(see Table 6).The presence of 6PPD did not affect adhesion.

### TABLE 6: EFFECT OF 6PPD ANTIOZONANT ON EPDM-SIDEWALL PROPERTIES

## Compound 8 9 10 11 Dynamic ozone, 50 pphm, 25 % ext., 40C°, after 72 continuous hours Crack rating OK OK OK OK Adhesion to carcass @ 100C° Adhesion, KN/m 20.7 22.5 21.7 23.4

#### Concolusions

Tire black sidewall compounds are formulated to resist weathering by heat, oxygen, ozone and ultraviolet light, to resist abrasion, tearing, and radial and circumferential cracking, and for fatigue life. In this study, we studied the use of EPDM as ozone-resistant polymer to protect the natural rubber and butadiene of conv- entional black sidewall compounds has been a successful technique. EPDM blended with natural rubber and / or butadiene rubber with different loading of EPDM. EPDM black sidewall compound give rise to good scorch safety and no reversion.

Adhesion to carcass compounds, aged fatigue life, elongation at break, abrasion resistance and dynamic ozone resistance have been improved in presence of EPDM in sidewall compound.

N-1,3- Dimethylbutyl,-N-phenyl-para- phenylenediamine (6PPD) was used as antiozonant.This enhanced the dynamic ozone resistance for compounds containing NR/BR/ EPDM blends with 2 phr of 6PPD passed all of the requirements of the tire black sidewall. The presence of 6PPD did not affect adhesion.

# References

- R.S. Bhakuni, S.K. Mowdood, W.H. Waddell, I.S. Rai, and D. L. Knight, “Tires” in “Encyclopedia of Polymer Science and Engineering,” Second Edition, J.I. Kroschwitz, Ed., John Wiley & Sons, New York, 1989, v. 16, p.834.

- R.F Shaw, Z.T Ossefort, and W.J Touhey, Rubber World, 1954, 130, 636.

- W.L. Cox, Rubber Chem.Technol., 1961, 34, 816.

- C.K. Rhee, R.P. Lattimer, and R.W. Layer, “Antiozonants” in “Encyclopedia of Polymer Science and Engineering,” Second Edition, J.I.. Kroschwitz, Editor, John Wiley & Sons, New york, 1989, v. 2, p. 91.

- R.W. Layer and R.P. Lattimer, Rubber Chem. Technol., 1990, 63, 426.

- J.A. Kuczkowski, “The Inhibition of Oxidative and ozonic Processes in Elastomers,” in Inhibition of Oxidation in Organic Materials,” P.P. Klemchak and J. Pospisil, Eds., CRC Press, Inc., Boca Raton, Florida, 1990, p. 24.

- M. Ogawa, Y. Shiomura, and T. Takizawa (to Bridgestone Corporation), 1989, U.S. 4,801,641, Jan. 31.

- S.W. hong, Rubber Plast. News December 25, 1989, p. 14.

- C.B. Shulman, “Unique Features of High Unsaturation EPDM Polymers,” paper no. 90 presented at a meeting of the Rubber Division, American Chemical Societty, Cleveland, Ohio, October 1-4, 1985, abstract in Rubber Chem.Technol., 1986,  59, 180.

- P.H. Sandstrom and J. Lal (to The Goodyear Tire & Rubber Co.), 1977, U.S. 4,004,627, Jan. 25.

- T.J.Botzman (to The Goodyear Tire & Rubber Co.), 1989, 4, 804, 028, Feb. 14.

- W.Von Hellens, S.A. H. Mohammed, and R. Hallman (to polsar Limited), U.S. 4,645,793, Feb. 24, 1987

- W.Von. Hellens, D.c. Edwards, and Z.J. Lobos, Rubber Plast., 1990,  (5), 61.

- E.E. Gorkina, L.T. Goncharova, and N.S. Nikolaeva, Int. Polm. Sci. Technol, 1994, 21, T/ 27.

- A.J.M. Sumner and H. Fries, Kautsch. Gummi Kunstst., 1992,  45, 558.

- ASTM D 1149-91, 1997 Annu.Book., Section 9 Rubber, p. 213; ASTM D 3395-86 (reapproved 1991), 1997 Annu. Book ASTM Stand., Section 9 Rubber, p.551.