Thermal Decomposition of Lanthanum

O-Hydroxybenzoate and O-Bromobenzoate

Hadi Hessen Jusim, Abed Al- Kader. M.N and Mustaffa .Taha

Chemistry Department, College of Science, Mustansiriah University, Baghdad, Iraq.

(NJC)

# (Received on     15/4 /2006)          (Accepted for publication on   15/11/2006)

Abstract

The conditions of thermal analysis of Lanthanum -O-Hydroxybenzoate and Lanthanum -O-Bromobenzoate were studied .

The Hydrated complexes lose water of crystallization in two steps . Lanthanum -O-Hydroxybenzoate starts to lose water of crystallization between (60-230)oC  , but Lanthanum -O-Bromobenzoate loses water of  crystallization between (100-320)oC .

The intermediate products La2O3(OHC6H4COO)5 and La2(BrC6H4COO)6 were obtained by heating the two complexes at(320-350)oC and (320-380)oC respectively . In the fourth step , anhydrous structures of the complexes decomposed in one step and then were transformed to La2O3 . These results are using TG,DTG,DTA,IR and (X – ray) diffraction techniques . DTA curves revealed exothermic peaks for the decomposition steps , but endothermic peaks were obtained from the dehydration of complexes .

الخلاصة

درست في هذا البحث ظروف التحلل الحراري لكل من المعقدين اورثوهيدروكسي بنزوات اللنثنم المائية واورثوبروموبنزوات اللنثنم المائية . وتبين ان المعقدين يفقدان ماء التبلور في خطوتين منفصلتين ، وان المعقد اورثوهيدروكسي بنزوات اللنثنم يفقد ماء التبلور عند التسخين ما بين (60-230)oم ولكن المعقد اورثوبروموبنزوات اللنثنم فقد ماء التبلور عند التسخين ما بين (001-320)oم ، وتم الحصول على نواتج وسطية هي La2O3(OHC6H4COO)5 , La2(BrC6H4COO)6  كخطوة ثالثة عند تسخين المعقدين منزوعي الماء ما بين (350-320) oم و (380-320) oم  على التوالي .

اما الخطوة الاخيرة فتضمنت تحلل التراكيب في الخطوة السابقة بخطوة واحدة انتهت بتكوين اوكسيد اللنثنم La2O3 . تم الحصول على هذه النتائج باستخدام تقنيات كل من  IR,DTA,DTG,TG  وحيود الاشعة السينية  (X-RAY) ، واظهرت منحنيات التحليل الحراري التفاضلي DTA قمماً باعثة للحرارة في خطوات التحلل في حين اظهرت قمماً ماصة للحرارة في خطوتي نزع ماء التبلور من المعقدين .

Introduction

Lanthanum-O- Hydroxybenzoate ( La(OHC6H4COO)3.3H2O) was known by Soge et. al (1,2) and lost water of crystallization at 220oC Sove et.al(3,4) have obtained anhydrous complexes of Lanthanum -O-Hydroxy-benzoate at 320 oC . Prozorovskaya et al.(5,6)  studied the thermal decomposition of Lanthanum-O- Bromobenzoate by TG and IR spectra and determined its density and solubility in water and dilute acids. Matyukhin et al (7-9) studied water of crystallization in Lanthanum –O-Hydroxybenzoate and Lanthanum –O- Bromobenzoate by TG , DTG , DTA , X-ray , and IR spectra. The aim of this work is to anextension the study of thermal decomposition of these complexes in air atmosphere .

Experimental

Lanthanum -O-Hydroxybenzoate precipitate(3) was prepared in decomposition reaction by adding equivalent amounts of 0.2 M solutions of O-Hydroxybenzoate at pH 4.3 to a hot solution of La(NO3)3 at pH 3.8 .

The precipitate formed was heated in water solution for two hours , filtered off , washed with water and dried at 50 oC .

Lanthanum -O- Bromobenzoate precipitate(3) was prepared by adding equivalent amounts of 0.2 M solution of O-Bromobenzoate at pH 4.2 to a hot solution of La(NO3)3 at pH 3.8 . The precipitate was heated in water solution for two hours , filtered off , washed and dried at 60oC .

The stability of the prepared complexes was studied by thermal decomposition in air atmosphere by TG , DTG , and DTA .

The TG , DTG and DTA curves were recorded . The measurements were made on a derivatograph at a heating rate of 10 deg. Min-1 . The samples were heated in air atmosphere in platinum crucibles .

The results are compiled in table (1) and the typical thermograms are illustrated in fig(1) . The water content was determined from the TG and DTG curves and the elemental analysis data are given in table (2) .

The carbon and hydrogen content of the prepared complex were determined by elemental analysis using V2O5 as an oxidizing agent(6) .

The bromine content was determined by the schoniger method(4) . The Lanthanum content was determined from the TG and DTA curves by converting the complexes into La2O3 at 550oC .

The thermal decomposition of the compounds were studied by Derivatograph (Q- 1500 D ) Hungarian Optial works MOM Budapest , in platinum crucible , at temperatures 20-1000 oC and heating rate of 10 deg / min , FTIR Spectroscopy using ( Perkin – Elmer 684 infrared Spectro-photometer , and X-ray diffraction using (Philips Corporation type PW 1051 / 30 ) on the data in cluded in the ASTM cards .

Result and discussion

Thermal studies of Lanthanum -O- Hydroxybenzoate (La(OHC6H4COO)3. 3H2O ) were obtained by heating in air atmosphere and the decomposition occurred in four steps .

In the first step it begins to lose water of crystallization at low temperature (60-170 oC ) which lost two molecules .

60-170 oC

La(OHC6H4COO)3. 3H2O                         La(OHC6H4COO)3. H2O + 2 H2O

The third water molecule is lost at 210-230 oC and the anhydrous salt is formed . Therefore , the water molecules are bound in different forms .

210-230 oC

La(OHC6H4COO)3. H2O                               La(O    HC6H4COO)3 + H2O

The water molecules of crystallization lost between 60-170 oC may be outer sphere , but the third water molecule is coordinated in the inner sphere .

The two steps of dehydration are endothermically steps , as shown in DTA curve ( fig 1 ) .

The anhydrous Lanthanum -O- Hydroxybenzoate that was heated at the third step between 320-350oC is transformed exothermally to La2O3(OHC6H4COO)5 in the presence of air , as follows :

16.5 O2

4La(OHC6H4COO)3                              2La2O3(OHC6H4COO)5 + 14CO2 + 5H2O

These results suggest that Lanthanum -O- Hydroxybenzoate exists as a dimer in this temperature range . Which was confired by the X-ray diffraction .

Table (1) Elemental analysis of La2O3(OHC6H4COO)5 complex .

| Elemental analysis | La % | C % | O % | H % |
| --- | --- | --- | --- | --- |
| Found | 26.52 | 42.71 | 28.39 | 2.39 |
| Calculated | 27.497 | 41.543 | 28.486 | 2.472 |

The DTA curve in this study recorded exothermic peak between 210 oC due to polymorphic transformation(6).

The fourth step , the anhydrous Lanthanum Hydroxybenzoate decomposes exothermically to La2O3 between 400-550 oC , Which were obtained in TG and DTA curves , (Fig 1) were observed by X-ray diffraction and ASTM cards .

Lanthanum -O-Bromobenzoate [La2(BrC6H4COO)3.2H2O] was studied on heating in air at mosphere in five steps .

In the first two steps , the molecules are dehydrated endothermically in the temperature range 100-180 oC which lost one and half molecules of water .

100-180 oC

La(BrC6H4COO)3.2H2O                                La(BrC6H4COO)3.0.5H2O + 1.5 H2O

The third step involves the loss of the remaining half water molecules between 220-320 oC and the anhydrous salt is formed .

220-320 oC

La(BrC6H4COO)3.0.5H2O                                   La(BrC6H4COO)3 + 0.5H2O

Propably the water of crystallization at the first step is outer sphere water , but some molecules of complex have one water molecule coordinated in the inner sphere .

The three steps of dehydration are endothermically . The results are given by DTA curves ( fig 2) .

The anhydrous La(BrC6H4COO)3 compound between 320-380 oC DTA curve were observed exothermic peak , but endothermic peak were observed at the same range by DTG curve Brzyska(10) concluded that in this temperature range poly morphic transformation takes place .

320-380 oC

2La(BrC6H4COO)3                                 La2(BrC6H4COO)6

The fifth step of anhydrous La2(BrC6H4COO)6  decomposes exothermically to produce La2O3 between 450 – 600 oC , these results were obtained in TG and DTA curves(11) .

La2(BrC6H4COO)6 + 7O2                        La2O3 + 6HBr + 7CO2 + 9H2O

DTG curve gives endothermic peak at 540 oC .

Table (2) : Thermal decomposition results of  La(OHC6H5COO)3.3H2O

in air atmosphere

| TG Loss of weight | Types of decomposition | Loss of weight % |  | Temperature Range oC | DTG Peak oC | Exo or Endo reaction | Loss of H2O molecules |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Found | Calculated |  |  |  |  |
| First step H2O | Dehydration of outer sphere water molecules | 6.01 | 5.96 | 60-170 | 150 | Endothermic reaction | 2 |
| Second step H2O | Dehydration of inner sphere water molecules | 2.88 | 2.98 | 210-230 | 220 | Endothermic reaction | 1 |
| Third step | Oxidation and decomposition | 11.25 | 11.34 | 320-350 | 327 | Exothermic reaction | --- |
| Fourth step | decomposition | 55.01 | 54.718 | 400-550 | 516 | Exothermic reaction | --- |

Table (3) : Thermal decomposition results of  La(BrC6H5COO)3.2H2O

in air atmosphere

| TG Loss of weight | Types of decomposition | Loss of weight % |  | Temperature Range oC | DTG Peak oC | Exo or Endo reaction | Loss of H2O molecules |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Found | Calculated |  |  |  |  |
| First step H2O | Dehydration of outer sphere water molecules | 2.21 | 2.15 | 100-180 | 157 | Endothermic reaction | 1.5 |
| Second step H2O | Dehydration of inner sphere water molecules | 0.91 | 0.717 | 220-320 | 302 | Endothermic reaction | 0.5 |
| Third step Polymorphic transformation | Dimer formed | ---- | ---- | 320-380 | 362 | Exothermic reaction | --- |
| Fourth step O- Bromobenzoate | Decomposition of complex to metal oxide | 82.92 | 84.14 | 450-600 | 574 | Exothermic reaction | 9 |

Table (4) : Elemental Analysis of La2(BrC6H5COO)6 complex .

|  | La % | Br % | O % | C % | H % |
| --- | --- | --- | --- | --- | --- |
| Found | 18.1 | 33.01 | 12.68 | 34.3 | 1.59 |
| Calculated | 18.8 | 32.47 | 12.99 | 34.1 | 1.62 |

The FTIR spectra recorded for prepared complexes over the range 7000-200 cm-1 confirmed the elemental analysis results . The IR spectrum of the first complex heated at 350oC , the position of absorption bands of asymmetrical and you should mention these vibration, C=O ester and C–O do not change compared with the spectrum of Lanthanum -O- Hydroxybenzoate .

The bands for OH¯ in complexes (3550 cm-1) and from hydrated at (3450 and 1630 cm-1) disappear , but the bands of La-O- La bond appears at 620 cm-1 (4) .

It is preperred to give the spectra of at least the original complexes before thermal treatment in order to compare the absorption of the products .

Conclusion

The high temperatures of dehydration of  Lanthanum -O- hydroxybenzoate (60-230) oC ,  O- bromobenzoate (100-320 ) oC suggest that some of water molecules crystallization is inner sphere .

Lanthanum O- hydroxybenzoate at low temperature range of (60-170) oC it loses two molecules the remaining water molecules are lost at (210-230) oC these results indicat that water molecules are bound in different ways . Probably the water of crystallization lost at low temperature is outer sphere . These results suggest that Lanthanum -O- hydroxybenzoate exists as a dimer at the third step between (320-350) oC which was confirmed the results by the X-ray diffraction .

The anhydrous Lanthanum dimer decomposes exothermically to La2O3 between (400-550)oC which were obtained in TG and DTA curves (Fig 1).Lanthanum -O- bromobenzoate at low temperature range (100-180 ) oC  it loses one and half molecules of water which is outer sphere . The third step in volves the loss of the remaining half water molecules at (220 – 320 ) oC .

Polymorphic transformatiom takes place(10) at the fourth step between (320-380 )oC . Anhydrous Lanthnum -O- bromobenzoate decompose oxothermically to La2O3 between ( 450 – 600 ) oC .

Note : all the stractures were observed in study was confirmed by X-ray diffraction analysis .

ToC

Fig (1) TG , DTG and DTA curves of Lanthanum -O- Hydroxybenzoate

thermal decomposition ( La (OHC6H4COO)3.3H2O ) .

ToC

Fig (2) TG , DTG and DTA curves of Lanthanum -O- Bromobenzoate

thermal decomposition ( La (BrC6H4COO)3.2H2O ) .

References

1- K.Soge. Vecgum and S.V.Levchik , J.Appl. Polym., Sci , 2001, 21, 910.

2- K.Soge. Veegum ,  A.I.Lesnikovich and S.V. Levchik , J.Appl. Polym.,

Sci , 2000, 18 , 637.

3- R.Sove.Holler , E.G. Teterin and W.Archangelskiy , Reactions of the

solid state, Elserier , Amsterdam . April (2002 ) .

4- R. Sove . Ho, O.I. Baldova and Tomsk . Amsterdam Univ., 2001, 102 , 182.

5- Z.N. Prozorovskaya , T.W. shestakova and L.N. Komissarova

TesisyDoki-Vses . Chugaevskoe Sovesh . Khim. Komplekson . Soedin , 1994,

12 , 386 .

6-  K.O.d . Baran, Z.N.Prozorvskaya and L.N. Komissarova , Reaction of the

solid state, Amsterdam, (1995) .

7- A.A.Matyukhin and R.C.Mackenzie, Thermal analysis, Academic Press ,

London- New York (1972) .

8- A.A.Matyukhin and L. Stoch, J.Thermal Anal ., 1981,  20, 291.

9- J.Wame and A.A.Matyukhin, J. Thermal Anal., 1978, 14, 325 .

10-W.Brzyska and J.A. Motylow, J.Chem. Abst., 2002, 22, 362 .

11- J.Walczak and M.Kurzawa , Thermal Anal., 1988, 34 , 679.