Experimental and Analytical Study of Tensile Properties For Hyper Composite Material

Muhannad Al-Waily

Mechanical Engineering department

m_al_waily@yahoo.com

Ali S. Humod

Materials Engineering Department

Jasim_ali85@yahoo.com

University of Kufa  /  College of Engineering

- Abstract:

In this work, an experimental and analytical solution for tensile properties of hyper composite material is presented. The composite material consist of composite matrix, bounded from resin material and short fiber, and long reinforcement fiber.

The result for the tensile properties of composite material combined from composite matrix and reinforcement fiber, E1, E2, G12, and 12. In addition, the results showing the effect of volume fraction of short and long fiber, and the types of short and long fiber reinforcement, presented by analytical solution. And, the yield stress of hyper composite material is defined by experimental study with various of volume fraction of resin, short fiber, and long fiber.

الخلاصة

في هذا البحث, تمت دراسة خواص المواد المركبة المكونة من مزج ثلاثة مواد بالطريقة النظرية والعملية. المواد المركبة التي تمت دراستها هي المواد المكونة من تركيب الألياف المستمرة (الطولية) مع الأرضية المركبة المكونة من المادة الرابطة والألياف المتقطعة.

خواص المواد المركبة, المكونة من الألياف المستمرة والأرضية المركبة, التي تمت حسابها هي معامل المرونة بالاتجاه الطولي والعرضي للمواد المركبة ومعامل الجساءة ونسبة بوايسن. بالإضافة إلى حساب تأثير نسبة حجم كلا من الالياف المستمرة (الطولية) والمتقطعة ونسبة المادة الرابطة على خواص المواد المركبة, وتأثير نوع الألياف المستخدمة على خواص المواد المركبة. وتمت دراسة إجهاد الخضوع للمواد المركبة وتأثير نسبة حجم الألياف والمادة الرابطة على الاحهاد.

- Introduction

A lamina usually refers to a fiber reinforced composite. The composite consists of high strength and modulus fibers embedded in a matrix or bonded to a matrix. Both the fiber and the matrix retain their distinct properties and together they produce properties which cannot be achieved individually. The fibers are usually the principal load carrying element in the composite and the purpose of the matrix is essentially to keep the fibers in the desired location. The matrix also serves the purpose of protecting the fiber from heat, corrosion and other environmental damages.