Damaging of Steel-Oil Pipes by Erosion and  Erosion -Corrosion Phenomena

Asst. Prof. Dr. Sami Abulnoun Ajeel           Asst.lecturer MS.C.Mohammed Abdullateef Ahmed

Abstract

Erosion and erosion-corrosion have important role in oil fields especially in steel oil pipelines. Therefore; in the present work erosion and erosion-corrosion tests are studied individually to investigate the relation between erosion and erosion-corrosion processes and to quantify the synergy (that is caused by erosion) in realistic flow environments.

The experimental work tests were done using special device which was designed and manufactured according to (G 73) ASTM.

The experimental work tests were achieved using traditional weight loss technique to measure weight loss rates in (gmd) unit. Also the microstructure observations of the test specimens were studied.

It was observed that whole tests were conducted on oil pipe (X 60) made of low carbon steel in plate form, tests were made on  corrosion using 3.5 wt % sodium chloride. (NaCl) solution as sea water purged with CO2 gas as the corrosive medium in crude oil , but in erosion-corrosion 1 wt % silica sand was added as slurry to that medium, pure erosion using 1 wt % silica sand as the erodent in distilled water purged with N2 gas as anti corrosive medium to get erosion just during pure erosion , all tests above were done in pumped media and pumped media had constant pressure of 1 bar, flow rate Q = 36 L/min,   temperature ≈ 25 ºC and pH = 4.4 for erosive-corrosive media but  pH = 7.4 for erosive medium.

After traditional weight loss technique was achieved, it was found that  erosion rate (E.R) was smaller than that of erosion-corrosion rate(E-C.R).

الخلاصة

للتعرية والتآكل-التعرية للفولاذ دور مهم في المجالات النفطية وخصوصاً خطوط أنابيب النفط الفولاذية . لذلك تركز الدراسة الحالية على اجراء تجارب عن التعرية والتآكل-التعرية بصورة منفصلة لكل منها لبحث العلاقات المتداخلة بين عمليات التعرية والتآكل-التعرية ولمعرفة المقدار الكمي للتحفيز (الناتج بسبب التعرية) في أوساط الجريان الفعلية.

اجريت التجارب المختبرية بأستخدام جهاز خاص تم تصميمه وتصنيعه استناداً الى المعيار العالمي [ASTM (G 73)] ,

التجارب المختبرية أُنجزت باستخدام تقنية فرق الوزن التقليدية لقياس معدلات فرق الوزن بوحدة (gmd).

ومن ألجدير بالذكر ان التجارب أُنجزت بشكل كامل على أنبوب نفط نوع (X60) مصنوع من الفولاذ المنخفض الكاربون (المشكل على شكل صفيحة) , في التجارب المبنية على التآكل الصرف يتم استخدام محلول كلوريد الصوديوم بنسبة (3.5 wt %) . محلول كلوريد الصوديوم المشابه لماء البحر يكون مشبعاً أو مشّرباً بغاز ثاني أوكسيد الكاربون (CO2) لتكوين وسط أكال مشابه للوسط الأكال الموجود في النفط الخام ولكن في حالة التآكل-التعرية أُضيف رمل السيليكا بنسبة (1 wt %) كعالق في ذلك الوسط  ،في التعرية الصرفة تم استخدام رمل السيليكا بنسبة   (1 wt %) كمادة معرية في الماء المقطر المشبع أو المشرب بغاز النتروجين (N2) لتكوين وسط غير أكال وللحصول على تعرية فقط خلال التعرية الصرفة .

 Production & Metallurgy Eng. Dept., UOT., Baghdad, IRAQ.

