Aqueous Extract of Leaves of Ziziphus as an Eco-Friendly Inhibitor for the Corrosion of Mild Steel in Potable Water

Ahmed F.Hamza                            Sura K. Mohamed Hussein

University of Babylon – College of Materials Engineering – Metallic Materials Engineering Department

ABSTRACT

The inhibitive effect of the aqueous extract of Ziziphus leaves on the corrosion of mild steel in drinking water have been investigated by using an electrochemical polarization and weight loss method. The  results  obtained  shows, that, the extract of leaves of Ziziphus could work as  an effective  inhibitors  against  the  corrosion  of  steel  in drinking  water  network.  The  inhibition percentage    increases  with  the increasing  of the leaves of Ziziphus concentration at 30°C. The inhibitor percentage efficiency above (98 %) was attained  at  extract of Ziziphus leaves concentration  (1% v/v).  The  inhibition efficiencies  of  the  extract of leaves of Ziziphus obtained  from  weight loss method  and  polarization measurements  were  in  good  agreement.  electrochemical  polarization  studies  clearly reveal that the extract of leaves of Ziziphus behaves predominantly as an anodic inhibitor. The study also shows that the inhibition efficiency was insignificantly affected by the temperature rise of the medium.

Key words: corrosion; inhibition; organic inhibitor; extract of leaves of Ziziphus.

المستخلص المائي لورق السدر كمثبط ودي للبيئة لتآكل

الفولاذ في الماء الصالح للشرب

احمد فاضل حمزة                  سرى كامل محمد حسين

جامعة بابل / كلية هندسة المواد / قسم هندسة المواد المعدنية

الخلاصة

تم دراسة التأثير التثبيطي للمستخلص المائي لورق نبات السدر على تآكل الفولاذ في المياه الصالحة للشرب  باستخدام قياسات الاستقطاب الكهروكيميائي وطريقة فقدان الوزن . بينت النتائج ان المستخلص يمكن ان يعمل بشكل فاعل كمثبط لتآكل الفولاذ في شبكات مياه الشرب . كما وجد ان نسبة التثبيط تزداد مع زيادة تركيز المثبط المستخدم عند درجة حرارة (30°م) حيث ان نسبة التثبيط بلغت اكثر من (98%) عند تركيز من المستخلص  مقداره (1%) كنسبة حجمية .ان كفاءة التثبيط المحسوبة من كلا الطريقتين المستخدمتين في البحث كانتا متوافقتين ,كما ان دراسة سلوك الاستقطاب لمستخلص ورق السدر بين انه يمتلك سلوك المثبط الانودي بالدرجة الاولى ، كذلك بينت الدراسة ان كفاءة التثبيط تأثرت بشكل لايذكر بارتفاع درجة حرارة الوسط .