1. INTRODUCTION:

Friction materials are divided into two types, dry materials and wet materials. Dry materials are meant to be operating mostly under dry conditions but also under wet conditions such as braking a car in the rain. Wet materials are designed specifically for use in a wet environment only such as wet clutches and oil immersed brakes [B. K. Satapathy 2002,D Chann 2004].

The purpose of friction brakes is to decelerate a vehicle by transforming the kinetic energy of the vehicle to heat, via friction, and dissipating that heat to the surrounding.[Mikael Eriksson 2007] As a part of the commercial truck or automobile, brake material have additional requirements, like resistance to corrosion, long life, low noise, stable friction, low wear rate, acceptable cost, dimensional stability, appropriate thermal properties, and light weight that will enable new technologies to raise the fuel efficiency of a vehicle without compromising its safety and reliability [P. J. Blau2001,Masoomi 2006].

Brake pads typically comprise the following subcomponents [Lille 2004, D Chann 2004]:

- Frictional additives, which determine the frictional properties of the brake pads and comprise a mixture of abrasives and lubricants.

- Fillers, which reduce the cost and improve the manufacture ability of brake pads.

- A binder, which holds the components of a brake pad together.

- Reinforcing fibers, which provide mechanical strength.

brake pad are classified into metallic pads, semi metallic and non-asbestos .Steel fibers, glass fibers, ceramic fibers, and carbon fibers appear to be the most suitable for use as reinforcing fibers in brake friction material while the high cost of the ceramic fiber lead to use a mixture of different types of reinforcing fibers with complementing properties such as using a mixture of steel fiber with glass fiber [Maurice 1973,Zhaobin 2007].

Binder is the heart of a system which binds the ingredients formally so that can perform the desired function in the friction materials. [Philip , 2004,D.Suryatama 2007,]Quick mast 108 (Epoxy ) used as binder in friction materials due to a good combination of mechanical properties such as high hardness, compressive strength, moderate thermal resistance, and creep resistance and very good wetting capability with most of the ingredients.[Rawa 2007].Abd al fatah 2000]

Semimetellic brake pads with a mixture of metallic and organic compounds having varying thermal expansion coefficients would require large amount of molybdenum trioxide to prevent cracking. molybdenum trioxide behave as lubricant at high temperature by reacting with sulfide to produce molybdenum sulfide therefore the wear lost decrease [ B. K. Satapathy 2002].

The aim of the work is to improve the friction material mechanical properties by increasing fiber ratio also using molybdenum trioxide as new filler and comparing it with calcium carbonate to use it high application temperature.

2. EXPERMENTAL ANALYSIS:

Sample preparation is made by mixing materials which contain chopped fibers as indicated in table (1) with using a technique suitable mixing and then the sample is placed in molds and special tests are shed pressure on the sample and is placed in the oven at a temperature and for a 100oC for 1 hour.

To prepare the specimens for impact tests, a die made of carbon steel (65mmX30mmX12.7mm) was used to cut the sample according to ASTM (D256) [6-8]. Impact test was conducted by Izod method. The cylindrical mold used for wear test was with 6mm diameter, and 10mm height as shown in figure (1).The wear test system (pin on disc) was used in the present study.compression sample die was made with the dimension (20×10×10).the shore hardness A test was used to measure the samples hardness.  The average particles size range of calcium carbonate powder is (90-900) μm to determine the required size [D50:199.4] while molybdenum trioxide is(50-700)µm determined by        using LBZA device to determine the required size [ D50 :41.88μm] as shown in figures (3,4).Table (2) represent the properties of Molybdenumtrioxide, zirconiumoxide, calcium carbonate and copper sulphides. Figure (2) represent wear test samples.   The shore hardness A test was used to measure the samples hardness. The compression device was used to measure the compression strength and young modulus.

3. RESULT AND DISCUSSION:

Figure (6) shows the relation between the wear lost and the time for the sample (1) which contain calcium carbonate under (4) kN load.  When compared between the samples as shown in figures (3, 4, 5 and 6), the wear lost increase when the time increase. The ratio of the fibers is 2.5 percent which represent the minimum weight ratio of fibers as shown in figure (5)samples(1.c,1.m). The maximum wear lost occurs at the minimum weight ratio of fibers because of the decrease of the plateaus formed by the fibers. When the wear time increased the work done by the friction force is increased too. That’s led to transform the friction work to heat energy which increases the wear lost by the development of the circle fatigue cracks led to remove the material by brittle fracture. Epoxy matrix being thermoset the energy absorption is less as compared to the thermoplastics. Thermosetting composites cracks initiate at the filler–matrix interface and propagate very easily through the matrix towards the other filler–matrix interfaces. When the network of cracks intersects, the filler particles become loose and are removed in the form of wear debris. The resin also gets removed in the form of fine wear debris caused by brittle fracture of the resin.

The wear loss in the  sample (1-m,2-m, 3-m and4-m) which contain molybdenum trioxide   increase with time increased for the sample  reason discussed ,Also the maximum wear lost occurs at the minimum weight ratio of fibers because thedecrease  of plateaus formed by the fibers . The wear lost increased as the contact area increase and vice versa as in equation (1).

Δw=wear rate *ρ*L*A                                                                   (1)[Abeer 2009]

Δw=Wear lost (kg)

L= sliding distance (m)

ρ= Density (kg.m-3)

A= real contact area (m2)

Filler particle are considerably harder than the surrounding matrix and can thus insulate the matrix against wear. Filler size, shape and matrix adhesion therefore also affect abrasion resistance. Loss of large or poorly bound filler particles by abrasion exposes the relatively soft surrounding matrix to wear. The effect is acute on the edge of the depression left by the dislodged particle. This is the area most susceptible to elongation, crack initiation and ultimate loss as shown with calcium carbonate therefore the wear lost increase when the speed increase as shown in table(3).

The wear loss in the samples which contain calcium carbonate close to the wear loss in the samples which contain molybdenum trioxide as Shawn in figures (6,7,10,11) because the minimum ratio of fiber when fiber ratio 5% and 10 %  . The values of the wear loss for the samples which have fiber ratio 15% and 20% which contain molybdnumtrioxide get more sable state then that of calcium carbonate as shawn in figures (8,9,12,13) due to the good compatibility between epoxy and molybdenum trioxide because its behave as lubricant at high tempreture.

The hardness of the samples increases with the increases of the ratio of the fibers as shown in figure (14) The reason behind that is the  high fiber ratios lead to increase the contact area between the matrix and the fibers due to the high aspect  ratio of fibers so the density increase and hardness increase.

The samples that contain MoO3fillers have higher hardness from the samples containing CaCO3fillers. The reason behind that is the minimum average particle size of MoO3 (50-700) µm  compared with CaCo3(90-900)µm  and it has orthorhombic structure therefore it has good contact area with epoxy matrix and it has high density as shown in figures (1,2).

The impact strength of the samples which contain MoO3 decrease when MoO3 content decrease as shown in figure (15) because that filler have minimum particle size and high surface area which inter between molecules chains and fill the spaces so the impact strength decreasein spite of the fiber ratio increase.

The impact strength of the samples which contain CaCO3increase when CaCO3 decrease because it have average particle size(90-900) µm which may far between the molecules chains so the impact strength increase when CaCO3 decrease as shown in fig (15).

The young modulus increase with fiber ratio increase because higher surface area, greater aspect ratio, and higher loading (the latter two effectively increasing the surface area exposed to the polymer) will all increase the modulus. Fillers with strong chain attachments, through active sites provide the most resistance to the chain extension and separation required for elongation as shown in fig (16).

The ultimate compression strength decrease with fiber ratio increase and filler decrease because the hardness increase and the density increase due to crosslinks decrease with fiber increase.. The samples which contain MoO3 have higher ultimate compression strength than CaCO3 because the minimum particle size and high surface area of MoO3 as shown in fig (17) .

Friction materials increase with fiber ratio increase because the fibers affect as abrasive materials .CaCO3 have high hardness than MoO3 therefore it have higher friction coefficients as shown in fig (18).

The comparative performance of Glass-Epoxy (G-E) composite systems interfaced with graded fillers has been examined by Suresha et al,  2006.  The influence of two inorganic fillers, silicon carbide particles (SiC) and graphite, on the wear of the glass fabric reinforced epoxy composites under dry sliding conditions has been investigated. For increased load and sliding velocity situations, higher wear loss was recorded. . It was observed that the Graphite filled G-E composite shows lower coefficient of friction than the other two composites irrespective of variation in the load/sliding velocities. SiC filled G-E composite exhibited the maximum wear resistance.

4-   CONCLUSIONS: CONCLUSIONS:

- The CaCo3 addition have lower wear lost than MoO3 in friction materials especially at  20% filler ratio.

- The CaCo3 addition have lower stable wear resistance than MoO3 in friction materials at high concentration of fiber content (20%).

- The MoO3 addition investigate hardnessat (15,10and 5) % of MoO3beter than CaCo3.

- The higher impact strength the larger of MoO3 content at 20% of MoO3 .

- The impact strength increase when fiber content increase in the case of using CaCO3

- The young modulus increase when fiber contentincrease.

- Wear lost,impact resistance hardness,young modulus enhanced when fiber ratio increased.

- Ultimate compression strength decrease with fiber ratio increase.

Table (1) Components of the samples batch

| Batch | Sample number | Glass fiber (wt. %) | Steel fiber (wt. %) | Copper sulphides (wt. %) | Zirconium oxide (wt. %) | Quick mast 108 (Epoxy ) (wt. %) | Molybdenum trioxide (wt. %) | Calcium carbonate(wt. %) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 1-c | 2.5 | 2.5 | 29 | 6 | 40 | - | 20 |
| 2 | 1-m | 2.5 | 2.5 | 29 | 6 | 40 | 20 | - |
| 3 | 2-c | 5 | 5 | 29 | 6 | 40 | - | 15 |
| 4 | 2-m | 5 | 5 | 29 | 6 | 40 | 15 | - |
| 5 | 3-c | 7.5 | 7.5 | 29 | 6 | 40 | - | 10 |
| 6 | 3-m | 7.5 | 7.5 | 29 | 6 | 40 | 10 | - |
| 7 | 4-c | 10 | 10 | 29 | 6 | 40 | - | 5 |
| 8 | 4-m | 10 | 10 | 29 | 6 | 40 | 5 | - |

Table (2) represent the properties

| Properties |  |  |  |  |
| --- | --- | --- | --- | --- |
| Molecular formula | MoO3 | ZrO2 | CaCO3 | CuSO4 (anhydrous) CuSO4•5H2O (pentahydrate |
| Molar mass | 143.94 g mol−1 | 123.218 g/mol | 100.0869 g/mol | 159.609 g/mol (anhydrous) |
| Appearance | yellow or light blue solid | white powder | Fine white powder; chalky taste | gray-white (anhydrous) |
| Odor | Odorless |  | Odorless |  |
| Density | 4.69 g/cm3, solid | 5.68 g/cm3 | 2.711 g/cm3 (calcite) | 3.60 g/cm3 (anhydrous)[1] |
| Melting point | 795 °C (1,463 °F; 1,068 K) | 2715 °C | 825 °C (aragonite) 1339 °C (calcite) | 110 °C decomp. (·5H2O)[1] <560 °C decomp |
| Boiling point | 1,155 °C (2,111 °F; 1,428 K) sublimes | 4300 °C | decompose |  |
| Solubility in water | 0.1066 g/100 mL (18 °C) 0.490 g/100 mL (28 °C) 2.055 g/100 mL (70 °C) | soluble in HF, and hotH2SO4 | 0.0013 g/100 mL (25°C) | 1.055 molal (10 °C) 1.26 molal (20 °C) 1.502 molal (30 °C |
| Structure |  |  |  |  |
| Crystal structure | orthorhombic |  | Isometric |  |
| Thermochemistry |  |  |  |  |
| Std molar entropy So298 | 77.78 J K−1 mol−1 | 50.3Jk-1mol-1 | 93Jk-1mol-1 | 1.502 molal (30 °C)[2] |
| Std enthalpy of formation ΔfHo298 | −745.17 kJ/mol | -10803Jk-1mol-1 | -12073Jk-1mol-1 | 159.609 g/mol (anhydrous)[1] |

Table (3) represent the weight loss at different speeds

| Sample No. | Weight loss at speed 20 m | Weight loss at speed 40 m | Weight loss at speed 60 m | Weight loss at speed 80 m |
| --- | --- | --- | --- | --- |
| 1-c | 0.0001 | 0.0002 | 0.0003 | 0.0005 |
| 1-m | 0.0002 | 0.0002 | 0.0003 | 0.0004 |
| 2-c | 0.0001 | 0.0002 | 0.0004 | 0.0006 |
| 2-m | 0.0002 | 0.0004 | 0.0006 | 0.0007 |
| 3-c | 0.0002 | 0.0002 | 0.0004 | 0.0005 |
| 3-m | 0.0002 | 0.0003 | 0.0004 | 0.0006 |
| 4-c | 0.0001 | 0.0002 | 0.0003 | 0.0005 |
| 4-m | 0.0002 | 0.0003 | 0.0005 | 0.0006 |

A)                                    b)

Figure(1)        a) wear mold        b) impact strength mold

Fig (2) wear test samples

Figure (3) LBZA chart of particle size analysis of CaCO3

Figure (4) LBZA chart of particle size analysis of MoO3

(1.c)                                                         (1.m)

(3.c)                                                                           (3.m)

(4.c)                                                  (4.m)

Figure (5) the sample surfaces after wear test.

Figure (6) the relation between the weight lost and time for the sample (1-c)

under load (4) KN and speed 20 m

Figure (7) the relation between the weight lost and time for the sample (2-c)

under load (4) KN and speed 20 m

Figure (8) the relation between the weight lost and time for the sample (3-c)

under load (4) KN and speed 20 m

Figure (9) the relation between the weight lost and time for the sample (4-c)

Under load (4) KN and speed 20 m

Figure (10) the relation between the weight lost and time for the sample (1-m)

under load (4) KN and speed 20 m

Figure (11) the relation between the weight lost and time for the sample (2-m)

under load (4) KNand speed 20 m

Figure (12) the relation between the weight lost and time for the sample (3-m)

under load (4) KN and speed 20 m

Figure (13) the relation between the weight lost and time for the sample (4-m)

under load (4) KN and speed 20 m

Figure (14) the relation between harness and samples number

Figure (15) the relation between the impact strength and sample number for the samples

Figure (16) the relation between the young modulus and sample number

Figure (17) the relation between the impact strength and sample number

Figure (18) the relation between the friction coefficient and sample number.

REFRENCES :-

Abeer"Evalution of Resins and Fibers Content for Friction Materials Industry,(2009).

B. Suresha, “The Role of Fillers on Friction and Slide Wear Characteristics in Glass-Epoxy Composite Systems” Journal of Minerals and Materials Characterization & Engineering, Vol. 5, No.1, pp 87-101, 2006.

ASTM D 256-02 “Standard Test Method for Determining the Izod Pendulum Impact          Resistance of Plastics” Annual Book of ASTM standards.

عبد الفتاح محمود طاهر, "أساسيات علم و تقنية البلمرات" دار المريخ للنشر, 2000.

B. K. Satapathy, and J. Bijwe, "Analysis of Simulations Influence of Operating Variables on Abrasive Wear of Phenolic Composites", Wear 253, pp. 787-794, 2002.

D Chann and G W Stachowiak, “Review of Automotive Brake Friction Materials", Proc. Instn Mechanical Engineering, vol. 218 part D: Journal of Automobile Engineering,( 2004).

D. Suryatama, R. P. Uhlig, S. Vallurupalli and F. Zweng, "Thermal Judder on Drum Brakes due to Mounted Radial Run Out", 2nd ANSA & µETA International congress, Greece, (2007).

Maurice Morton “Rubber Technology” Van Nostrand Reinhold Company,( 1973).

Masoomi, M., Katbab,A.,Nazockdast,H., “Damping Behavior of the Phenolic Based Composite Friction Materials Containing Thermoplastic Elastomers (TPEs)” Iranian J. Chem. Chem. Eng. vol. 25, No. 3, pp. 35-40, (2006).

Mikael Eriksson, "Friction and Contact Phenomenon of Disc Brakes Related to squeal", compressive summaries of Uppsala dissertation, Faculty of Science and Technology,( 2000).

P. J. Blau, “Compositions, Functions, and Testing of Friction Brake Materials and Their Additives", Oak Ridge National Laboratory, USA, ORNL/TM-2001/64, (2001).

P. V. Gurunath, and J. Bijwe, "Friction and Wear Studies on Brake Pad Materials Based on Newly Developed Resin", Wear 263, pp. 1212-1219, (2007)

Philip S. Sklad, "Application of Innovative Materials" FY Progress Report high strength weight reduction materials, (2004).

Rawa A. A. Hasan “Study of Impregnation Process of Preparation of Short Fiber Reinforced Poly Phenylene Sulphides Composites for Air Frame Structure”, M.Sc. thesis, Babylon University, College of Engineering,( 2007).

Zhaobin Chen, “Friction and Wear Mechanisms of PA66/PPS Blend Reinforced with Carbon Fiber” Journal of Applied Polymer Science, vol. 105, pp. 602–608, (2007).