IMPROVEMENT OF HOT CORROSION RESISTANCE OF AUSTENITIC STAINLESS STEEL 316L IN ASH BY CHROMIZING-SILICONIZING

Dr. Ali Hobi Halem          Dr. Hayder Hassan Jaber          Roaa Hatim Hatif

alialihhhobi@yahoo.com

ABSTRACT

The  simultaneous  deposition  of  Cr  and  Si  into  austenitic stainless steel 316L alloy using a halide-activated pack-cementation process is described, using a pack mixture containing (67 wt. % Cr, 8 wt. % Si, 2 wt. % NH4Cl, 23 wt. % Al2O3). The diffusion coating process is carried out at 950oC for 6hrs under Ar atmosphere. It was found that diffusion coating time produce coating thickness of 80-100µm, the corrosion resistant properties of austenitic stainless steel can be improved by enriching the surface composition in Cr and Si using pack cementation process, this study compare the hot corrosion performance of uncoated and coated austenitic stainless steel 316L with chromized-siliconized diffusion coating specimens in the presence of molten mixture of Na2So4and V2O5at 850oC and compare the micro-hardness between them. In the case of coated austenitic stainless steel 316L alloy with chromized-siliconized diffusion coating, specific weight gain will be observed while specific weight lose can be observed in the case of uncoated austenitic stainless steel 316L alloy. Diffusion coated austenitic stainless steel 316L alloy has shown excellent corrosion resistance and higher micro hardness than uncoated austenitic stainless steel 316L alloy because the coated layer that consisted mainly of CrSi2 and Cr3Si phases.

Keywords: diffusion coating, pack cementation, hot corrosion, stainless steel 316L, ash.

الخلاصه:

تشيرنتائج الدراسةالحالية إلى إمكانية زيادة مقاومة التأكل الحار للفولاذ المقاوم للصدأ الأوستنايتي  
(Austenitic  stainless steel AISI  316L) منخلا لزيادة محتوىا لكروم و السليكون عند سطح الفولاذ باستخدام تقنية الطلاء الانتشاري بالسمنتة   (Pack  Cementation). تم إجراء ترسيباً آنيا بالكروم والسليكون على سبيكة الفولاذ المقاوم للصدأ الاوستينايتي L 316 باعتماد ألية الطلاء الانتشاري، وذلك باستخدام خليط مكون من: (67%  Cr،8%Si ، 2%NH4Cl ،23%(Al2O3. جرت عملية الطلاء ألانتشاري عند درجة حرارة 950 مْ ولمدة (6 ساعات ) فيجومنالآركون . ولقدوجدإنسمكطبقة حوالي (80-100 مايكرومتر)،يمكن تحسين مقاومة التآكل للفولاذ الأوستنايتي من خلال زيادة محتوى الكروم والسليكون على السطح، تقوم هذه الدراسة باجراء مقارنة بين الفولاذالاوستنايتي316Lالغير مطلي والمطلي بطبقه من الكروم وبوجودخليطمنالمنصهر الملحيNa2So4و V2O5عند درجة حراره 850 مoوكذلك مقارنة قيم الصلادة بين طبقة الطلاء والمعدن الأساس. ففي حالة الفولاذ الغير مطلي نلاحظ فقدان بالوزن النوعي للفولاذ الاوستنايتي بينما نلاحظ زياده ملحوظه بالوزن النوعي عندما يكون الفولاذ مطليا بطبقه من الكروم والسليكون وكذلك نلاحظ زيادة قيم الصلادة بالنسبة لطبقة الطلاء أكثر من المعدن الأساس وذلك يعود الي التركيب الطوري حيث تتكون طبقة الطلاء بشكل رئيسي من CrSi2وCr3Si.