Influence of Alumina on Metallographic

and Mechanical Properties of

Carbide Cutting Inserts

Kahtan Alkhazraji                           Haydar Alethari                              Mushtaq Albdiry           Dept. of Materials Eng.                  College of Materials Eng.                Dept. of Mechanical Eng.         University of  Technology              Babylon University                   Univ. of Southern Queensland

Toowoomba, Qld, 4350, Australia

Abstract:

This investigation is aimed at understanding the role of adding ceramic inclusion, alumina (Al2O3) on the densification, microstructure and mechanical properties of cemented carbide cutting inserts. The samples were prepared of an initial mixture of 62 WC, 32 (Ti-W) C and 6Co wt% particulates; different additions of Al2O3 of 1, 2, 3, 4, 5 and 7 wt% were introduced to that mixture. The testing specimens were compacted via powder metallurgy at 200 MPa and sintered at 1410°C under vacuum. The green and sintered densities have decreased; the figures of macrohardness, Vickers hardness and transverse rupture strength have also deteriorated with the increase of alumina content. The macrohardness has almost declined of 30% at 3% alumina. This is ascribed to the interfacial grain-boundary decohesion between Al2O3 and carbide particles as can be observed from scanning electron microscopy images which depicts the monolithic clusters in the final consolidation of the compacts.

Keywords: powder metallurgy; cemented carbides; alumina; inclusion; microstructure and materials properties.

الخلاصة :

يهدف البحث إلى فهم دور إضافات متضمنات سيراميكية وهي الالومينا في تحديد التكثيف والبنية المجهرية والخواص الميكانيكية للقم الكاربيدية المفخورة.حضرت النماذج من مزيج أساس من (62 WC, 32 (Ti-W) C & 6Co) كنسب وزنية مع إضافات مختلفة من الالومينا بلغت (1, 2, 3, 4, 5 & 7 wt%). كبست النماذج بتقنية ميتالورجيا المساحيق تحت ضغط (200MPa) ولبدت في الفراغ في درجة حرارة (14100C).انخفضت الكثافة الخضراء وكثافة النماذج الملبدة كذلك فان الصلادة العيانية والصلادة المايكروية وإجهاد الكسر المستعرض قد تضررت مع زيادة محتوى الالومينا. انحدرت الصلادة العيانية بنسبة (30%) مع إضافة (3%) من الالومينا.يعود ذلك إلى غياب الارتباط البيني لحدود الحبيبات بين الالومينا والكاربيدات كما يلاحظ من صور الماسح الالكتروني الذي يصور التجمعات الانفرادية لقوام المكبوسات.