The experimental study and mathematical model of the effect of alumina particles reinforcement on mechanical

properties of epoxy

Dr. Ibtihal A. Mahmood 1   Jabbar H. mohmmed 2   Sarmad I. Ibrahim3   Muslim M. Ali4

ABSTRACT

This article describes some mechanical properties of alumina-filled epoxy composites. In this work, the epoxy matrix was reinforced with increasing amount of alumina particles in the range of 0-40% by weight with different particle size (d≤8, 18≤d≤25, 33≤d≤45, 50≤d≤62)µm. From the flexural test results, it was observed that the flexural modulus increases with increasing α-alumina content from 10 to 40 wt%. At the same time, the results indicated that there are no much effect on the flexural modulus with change the particle size in the range of (d≤8, 18≤d≤25)µm. The highest value of flexural modulus was recorded with 40 wt% of α-alumina content and (d≤8)µm particle size. It was also found that the 40 wt% alumina content and (d≤8)µm particle size recorded the highest value of fracture toughness (Gc), fracture toughness (Kc), hardness (HB), and wear resistance which were improved by (253%, 282%, 230%, and 82%), respectively. Also, in this work a mathematical modeling is implemented and regression equations are obtained by using ( SPSS ) software to predict the properties of alumina filled epoxy composites. Comparing the predicted and measured values gives high prediction accuracy. The accuracy of prediction has been (90.13%, 85.95%, 90.28%, 89.76%, and 84.36%) for flexural modulus, toughness, fracture toughness, hardness, and wear rate respectively.

Keywords: alumina filled composites, epoxy resin, flexural modulus, SPSS software.

دراسة عملية وموديل رياضي لتأثير التقوية بدقائق الالومينا

على الخواص الميكانيكية للايبوكسي

د. ابتهال عبد الرزاق محمود            جبار حسين محمد            سرمد عماد ابراهيم             مسلم محسن علي

الخلاصة

يصف هذا ألبحث بعض الخواص الميكانيكية لمتراكبات الايبوكسي المقواة بدقائق الالومينا. حيث تم في هذا البحث اضافة دقائق الالومينا لتقوية راتنجات الايبوكسي بنسب وزنية مختلفة (0-40)% مع احجام حبيبية مختلفة (d≤8, 18≤d≤25, 33≤d≤45, 50≤d≤62) مايكرومتر. بينت نتائج اختبار الانحناء زيادة قيمة معامل الانحناء بزيادة نسبة الالومينا. وفي نفس الوقت بينت النتائج عدم وجود تأثير كبير لتغيير الحجوم الحبيبية في حدود(d≤8, 18≤d≤25)مايكرومترعلى قيمة معامل الانحناء. أعلى قيمة