تقييم اداء الخواص الميكانيكية لمونة السمنت المقواة بالمشبك السلكي(الفيروسمنت)

جاسم عطية علوان / مدرس

المعهد التقني- بابل

هندسة مدنيه Jassimatiya @Yahoo.Com :        Email

الخلاصة :

هدف البحث معرفة خواص مونة الفيروسمنت وتأثير عدد طبقات التقوية بالمشبك السلكي من(1-6 ) طبقة على مقاومة الانضغاط ومعاير الكسر وامكانية تخفيض السمنت بمونة انهاء الجدران ذو الطبقة الواحدة  من المشبك . تطلب البحث (127) نموذج لفحوصات القوام القياسي لعجينة السمنت المرجعية ، مقاومة الانضغاط ومعاير الكسر للمونة المرجعية، وكذلك عمل نماذج لفحوصات مقاومة الانضغاط والكسر لمونة السمنت المقواة بطبقة من المشبك ولغاية (6) طبقات، بالإضافة الى نماذج لفحوصات المونة المقواة بطبقة من المشبك والمخفضة السمنت.

أظهرت النتائج ان تقوية المونة ب(5) طبقات من المشبك اعطت افضل النتائج وانها ادت الى زيادة مقاومة الانضغاط بنسبة (61.5%)ومعاير الكسر بنسبة (205.21%)عن مقاومتهما بالمونة المرجعية. تبين ايضا عند تقوية مونة  انهاء الجدران بطبقة واحدة من المشبك فأنه يمكن تخفيض السمنت فيها بنسبة %20)) من وزنه بالمونة المرجعية وان خواص هذه المونة حققت متطلبات المواصفات العراقية وبقابلية تشغيلية جيدة .

كلمات الرئيسية: مونة الفيروسمنت، مقاومة الانضغاط ومعاير الكسر، المشبك المعدني.

EVALUATION OF CEMENT MORTAR MECHANICAL PROPERTIES

PERFORMANCE STRENGTHENED BY WIRE MESH(FERROCEMENT)

Jassim Atiya Alwan

Lecturer- Babylon  Institute of Technology

ABSTRACT :

The research aim is to evaluate the properties of Ferro Cement mortar and the effect of  the Wire Mesh strengthening layers number from(1-6) layers on the compressive and flexural strength with cement decreasing ability of the wall finishing mortar with one mesh layer. (127) samples were required, samples for reference cement paste standard consistency ,reference mortar compressive and flexural strength tests in addition to that a Samples for the strengthened mortar compressive and flexural strength tests with one mesh layer up to (6)layers ,another samples also for the  strengthened mortar tests with one mesh layer and reducing the cement. Results showed that the strengthened mortar by (5) mesh layers was  increased in compressive strength by (61.5%) and flexural strength by(205.21%) more than their reference mortar strengths. When strengthening the walls finishing mortar by one mesh layer we can decreasing the mortar cement content by a ratio of(20%) of its weight in reference mortar and the mortar properties are satisfied the requirements of  the Iraqi specifications  with good workability.

Key Words: Ferro Cement mortar, Compressive Strength and Flexural                     Strength, Wire Mesh.