EFFECT OF HEAT TREATMENT FOR SUBMERGED ARC WELDING ON CORROSION RESISTANCE IN SEA WATER AT DIFFERENT TEMPERATURE

Jenan Mohammed Naje           Safaa Mohammed Hassoni         Nidhal Abdullah abdulwahab

Assistant lecturer                     Assistant lecturer                     Assistant lecturer

nagegenan@yahoo.com             as_5599@yahoo.com                   naa2006eng@yahoo.com

ABSTRACT

This paper is aimed to study the effect of heat treatment for submerged arc welding joint in the dimension of 100*50*16 mm on corrosion resistance in sea water at different temperatures.

Submerged arc welding is carried out for Low carbon steel  st37 under welding conditions of (750 Amp) DC current straight polarity (DCSP) and 32 volt, welding wire type EM12K.70-18  in diameter of 4mm  and wire  speed of 4.2m/min with Flux .

And a joint geometry of single V at 45⁰ Butt joint and weld two passes, the welded pieces were tested by X-ray radiography and Faulty pieces were excluded.

After welding, the joints without defects have be submitted to heat treat including   quenching where the joint heated to 900 C⁰ for one hour then water   cooled and   followed by normalizing heat treatment by heating to 900 C⁰ for one hour then air cooled Corrosion specimens prepared from the weld joint by the dimensions of (15*15*3) mm according to ASTM G71-31 then Optical microscopy was used to observe the welded joint microstructure.

Corrosion tests were investigated by electrochemical potential state cell in a prepared salt water (sea water) at different temperatures (25, 50.75) C⁰, Tafle equation was adopted to calculate the corrosion rate.

Results show that heat treatment contributed in reducing corrosion rate and normalizing gives better results than quenching but the effects of media temperature give the opposite

Keyword: submerged arc welding SAW, heat treatment, corrosion resistance

الخلاصة :

يهدف البحث الى دراسة تاثير المعاملات الحرارية لوصلات لحام تناكبية بالابعاد 100*50*16 ملم تم لحامها  بطريقة لحام  القوس الكهربائي المغمور على مقاومة التاكل في ماء البحر عند درجات حرارة مختلفة لفولاذ كربونيٍSt 37

تم اللحام عند ظروف لحام من تيار750ملي امبيرو فولتية 32 فولت وسرعة 4.2 م\ دقيقة  باستخدام سلك لحام نوع   EM12K.70-18 وقطر 4 ملم مع وجودFlux  كمادة عازلة و بعدد اثنان من التمريرات باستخدام تيار (DCSP)  للحصول على وصلة لحام تناكبية وعمل زاوية لحام تحضيرية من جهة واحدة مقدارها 45 درجة .

بعد عملية اللحام والتاكد من خلوها من العيوب من خلال فحصها بواسطة  جهاز X-ray radiography اجريت معاملة حرارية (تقسية ) اذ تم تسخين الوصلة الى درجة 900 درجة مئوية ثم التبريد السريع بالماء اتبعتها عملية معادلة حيث قمنا باعادة التسخين الى نفس الدرجة والتبريد البطيء بالهواء تم تحضير  عينات اختبار التاكل بعد قطعها من الوصلة بابعاد 15*15*3 ملم وفق المواصفة القياسية   ASTM G71-31 اتبعتها عمليات تحضير من تنعيم وصقل لاجراء فحص البنية المجهرية باستخدام المجهر الضوئي ذو كاميرا . ولإجراء اختبار تآكل كهروكيمياوي في وسط ماء البحر عند درجات حرارة متغيرة  25,50,75  درجة مئوية فيمثل تيار التآكل ، وتم حساب معدل التآكل اعتمادا على معادلة تافل في وسط ماء البحر

ومن النتائج التي تم الحصول عليها وجد ان مقاومة التاكل تزداد مع المعاملة الحرارية وان المعادلة اعطت افضل النتائج ولكن على العكس فقد اعطت درجة حرارة الوسط نتائج عكسية